A DETAILED METALLOGENIC STUDY OF THE MCFAULDS LAKE CHROMITE

DEPOSITS, NORTHERN ONTARIO

(Thesis Format: Monograph)

by

Jordan Elliot Laarman

CHAPTER 1: INTRODUCTION

1.1 McFaulds Lake Chromite Deposits
1

1.2 Thesis Objective
1

1.3 Location and Climate
2

1.4 Previous Work
4

1.5 Methods
5

1.5.1
XRF (X-Ray Fluorescence spectrometry) and ICP-MS
(Inductively Coupled Plasma-Mass Spectrometry) 6

1.5.2
Full Spectrum PGE analysis 6

1.5.3
Electron Microprobe Analysis 7

1.5.4
Laser Ablation ICP-MS 7

CHAPTER 2: GEOLOGICAL SETTING

 2.1 Oxford-Stull Domain
9

2.1.1 McFaulds Lake Greenstone Belt
12

2.2 Deformation
20

CHAPTER 3: PETROGRAPHY

3.1 Introduction
25

3.2 Footwall granodiorite
30

3.3 Dunite-harzburgite
33

3.4 Oikocrystic harzburgite
35

 3.5 Disseminated chromite
38

 3.6 Chromitite
43

 3.6.1 Heavily disseminated chromite
43

 3.6.2 Intermittent chromitite beds
43

 3.6.3 Semi-massive chromite
45

 3.6.4 Massive chromite
53

 3.7 Magmatic Breccia
58

3.8 Heterogeneous pyroxenite
63

3.9 Pyroxenite-olivine pyroxenite
63

3.10 Gabbro-leucogabbro
70

 3.11 Hangingwall mafic metavolcanic
74

CHAPTER 4: GEOCHEMISTRY

4.1 Introduction
75

4.2 Whole rock geochemistry
75

4.2.1.1 Major oxides
75

iv
4.2.1.2 Up section major oxide variation 78

4.2.1.2.1 Black Label: DDH BT-09-31 78

4.2.1.2.2 Black Thor: DDH BT-08-10 & BT-09-17 81

4.2.1.2.3 Big Daddy: DDH FW-08-19 86

 4.2.1.3 Binary major oxide variations 88

4.2.1.3.1 Black Label (Fig. 4.12) 88

4.2.1.3.2 Black Thor (Fig. 4.13) 88

4.2.1.3.3 Big Daddy (Fig. 4.14) 92

 4.2.2 Trace element earth geochemistry 94

 4.2.2.1 Primitive mantle-normalized multielement plots 94

4.2.2.1.1 Black Label 94

4.2.2.1.2 Black Thor 96

4.2.2.1.3 Big Daddy 99

 4.2.2.2 (La/Sm)cn vs. (Gd/Yb)cn 99

 4.3 Full spectrum PGE analysis 101

 4.3.1 Primitive mantle normalized PGE plots of host rocks 101

 4.3.2 Primitive mantle normalized PGE plot of chromitite 103

 4.4 Mineral chemistry of host silicates 105

4.4.1 Olivine 105

4.4.2 Pyroxene 105

 4.4.3 Amphibole 109

4.4.4 Phlogopite 116

4.4.5 Chlorite 120

CHAPTER 5: MINERALIZATION

 5.1 Introduction 130

5.2 Metal assay variation 130

5.2.1 Up section wt. % Cr2O3, Pt, Pd, Ni and Cu ppm variation 130

5.2.1.1 Black Label (Figs. 5.1 and 5.2) 131

5.2.1.2 Black Thor (Figs. 5.3, 5.4, 5.5 and 5.6) 133

5.2.1.3 Big Daddy (Fig. 5.7) 137

 5.2.2 Binary metal assay variation 139

 5.3 Chromite mineral chemical variation 143

 5.3.1 Up section mineral chemistry of chromite 145

5.3.1.1 Black Label 151

5.3.1.2 Black Thor BT-08-10 160

5.3.1.3 Black Thor BT-09-17 161

5.3.1.4 Big Daddy 176

 5.3.2.1 Black Label binary chromite chemistry 199

 5.3.2.2 Black Thor BT-08-10 binary chromite chemistry 204

 5.3.2.3 Black Thor BT-09-17 binary chromite chemistry 209

 5.3.2.4 Big Daddy binary chromite chemistry 213

 5.4 Laser ablation ICP-MS analysis of chromite 222

 5.4.1 Chromite/Chromite in MORB trace element plots 222

 5.4.2 Binary trace element variation 224

v
CHAPTER 6: DISCUSSION

6.1 Introduction
230

 6.2 Tectonic discrimination of chromite
230

6.2.1 The Cr# vs. Mg# plot
230

6.2.2 The Ternary Cr-Fe3+-Al plot
233

 6.3 Origin of chromite: An Evaluation of Irvine’s 1975 model
233

 6.4 Silicate Inclusions in Chromite
239

 6.5 Origin of chromite: Irvine’s 1977 magma mixing model
249

 6.6 Evidence for magmatic differentiation by double diffusive convection:
The electron microprobe results 255

6.6.1 Magmatic differentiation
255

6.6.2 Double diffusive convection mineralization
257

 6.6.3 Formation of massive chromite by post-cumulus growth 261

6.7 Evaluation of the conduit model
264

6.8 Retrogression of chromite with hydration of the intrusion
267

CHAPTER 7: CONCLUSIONS
274

7.1 Conclusions
274

 7.2 Summary
277

REFERENCES
281

APPENDIX 1:
Core logs for DDH BT-09-31, BT-08-10, BT-09-17 and
FW-08-19 296

APPENDIX 2:
Sample List – BT-08-10 315

BT-09-31 & BT-09-17
320

FW-08-19
326

APPENDIX 3:
Whole rock geochemistry & Full Spectrum PGE 330

APPENDIX 4: Silicate mineral chemistry data -337
Olivine 338
Orthopyroxene 342
Clinopyroxene 344
Amphibole 350
Phlogopite 377
Chlorite 385

APPENDIX 5: Chromite mineral chemistry data - 401
BT-09-31 402
BT-08-10 423
BT-09-17 439
FW-08-19 442

APPENDIX 6:
Chromite laser ablation data

459

List of Figures

vi
Figure 1.1 Location map of the McFaulds Lake chromite deposits

3
Figure 2.1 Geological map of the Superior Geological Province

10
Figure 2.2 Aeromagnetic map of the Oxford-Stull Domain

11
Figure 2.3 Simplified geological map of the McFaulds Lake area

13
Figure 2.4 Geological map of the Ring of Fire Intrusion 15
Figure 2.5 Generalized stratigraphic column of the Ring of Fire Intrusion 15
Figure 2.6 Geology of the Blackbird chromite deposit 17
Figure 2.7 Geology of the Big Daddy chromite deposit 18
Figure 2.8 Geology of the Black Label and Black Thor chromite deposits 19
Figure 2.9 Quartz monzonite diapirism at the Koitelainen Intrusion 21
Figure 2.10 Drill section through Big Daddy DDH FW-08-19 23
Figure 2.11 Drill section through Black Thor DDH BT-08-10 23
Figure 2.12 Dextral strike-slip faults in the Black Thor chromitites 24
Figure 3.1 Drill section of Black Label DDH BT-09-31 26
Figure 3.2 Drill section of Black Thor DDH BT-08-10 27
Figure 3.3 Drill section of Black Thor DDH BT-09-17 28
Figure 3.4 Drill section of Big Daddy DDH FW-08-19 29
Figure 3.5 Photograph of granodiorite drill core 32
Figure 3.6 Photograph of dunite drill core

32
Figure 3.7 Photomicrograph of dunite with disseminated chromite-a

34
Figure 3.8 Photomicrograph of dunite with disseminated chromite-b

34
Figure 3.9 Pyroxene replacement of dunite in drill core-a

36

vii
Figure 3.10 Pyroxene replacement of dunite in drill core-b

36
Figure 3.11 Pyroxene replacement of dunite in drill core-c

37
Figure 3.12 Photograph of oikocrystic harzburgite drill core

37
Figure 3.13 Photomicrograph of tremolitization of pyroxene

39
Figure 3.14 Photomicrograph of primary olivines and pyroxenes in talc

39
Figure 3.15 Photograph of disseminated chromite in dunite 40
Figure 3.16 Photomicrograph of interstitial chromite 40
Figure 3.17 Photomicrograph of net-textured chromite in dunite 41
Figure 3.18 Photomicrograph of interstitial chromite in oikocrystic harzburgite 41
Figure 3.19 Photograph of kaemmererite vein alteration 42
Figure 3.20 Photomicrograph of talc-rimmed olivines in net-textured chromite 42
Figure 3.21 Photograph of an intermittent chromite bed 44
Figure 3.22 Photograph of alternating intermittent chromite beds 44
Figure 3.23 Photograph of cumulus pyroxene interbanded with chromite 46
Figure 3.24 Photograph of net-textured semi-massive chromite 46
Figure 3.25 Photomicrograph of chain-like net-textured chromite 47
Figure 3.26 Photomicrograph of silicate inclusions in chromites 47
Figure 3.27 Photomicrograph of the incomplete annealing of a chromite grain 49
Figure 3.28 Photomicrograph of the concentric annealing of chromite grains 49
Figure 3.29 Backscatter image of multiple silicate inclusions in chromite

50
Figure 3.30 Backscatter image of minerals within a silicate inclusion

50
Figure 3.31 Photomicrograph of silicate inclusions in igneous amphibole

51
Figure 3.32 Backscatter image of silicate inclusions in igneous amphibole

51

viii
Figure 3.33
Photomicrograph of the incomplete annealing of chromite around
a phlogopite grain

52
Figure 3.34 Photomicrograph of chromite with interstitital phlogopite

52
Figure 3.35 Photograph of Black Thor massive chromite

54
Figure 3.36 Photograph of Big Daddy massive chromite

54
Figure 3.37 Photograph of oikocrystic pyroxene patches in massive chromite 55
Figure 3.38 Photograph of chicken-track texture of pyroxene in chromite 55
Figure 3.39 Photomicrograph of tremolitized oikocrystic pyroxene in massive
chromite 56
Figure 3.40 Photomicrograph of interstitial chlorite in massive chromite 56
Figure 3.41 Photomicrograph of chlorite in brittle failure of massive chromite 56
Figure 3.42 Photograph of Black Label massive chromite 57
Figure 3.43 Photomicrograph of interstitial carbonate in massive chromite 59
Figure 3.44 Photograph of occluded silicate in chromite 59
Figure 3.45 Photograph of silicate layering in massive chromite 60
Figure 3.46 Photograph of deformation fabrics in chromite 60
Figure 3.47 Photomicrograph of adcumulus fracturing in massive chromite 61
Figure 3.48 Photograph of magmatic breccias 61
Figure 3.49 Photograph of sulphides in magmatic breccias 62
Figure 3.50 Photograph of heterogeneous olivine pyroxenite 64
Figure 3.51 Photograph of filter pressed layers in heterogeneous pyroxenite

64
Figure 3.52 Photograph of pyroxenite

65
Figure 3.53 Photograph of original bronzite in pyroxenite

65
Figure 3.54 Photomicrograph of pyroxenite

67

ix
Figure 3.55 Photograph of disseminated chromite in pyroxenite

67
Figure 3.56 Photomicrograph of disseminated chromite in pyroxenite

68
Figure 3.57 Green aphyric ultramafic units in pyroxenite

68
Figure 3.58 Photograph of gabbro

71
Figure 3.59 Photomicrograph of green tremolite with surrounding biotite in
gabbro 71
Figure 3.60 Photomicrograph of titanite alteration in gabbro 72
Figure 3.61 Photomicrograph of igneous amphibole in gabbro 72
Figure 3.62 Photograph of leucogabbro 73
Figure 4.1 Plot of Mg % vs. depth from assays of Black Label DDH BT-09-31 79
Figure 4.2 Plot of Fe % vs. depth from assays of Black Label DDH BT-09-31 79
Figure 4.3 Plot of Ca % and Al % vs. depth from assays of Black Label
DDH BT-09-31 80
Figure 4.4 Plot of Mg % vs. depth from assays of Black Thor DDH BT-08-10 82
Figure 4.5 Plot of Fe % vs. depth from assays of Black Thor DDH BT-08-10 82
Figure 4.6 Plot of Ca % and Al % vs. depth from assays of Black Thor
DDH BT-08-10 83
Figure 4.7 Plot of Mg % vs. depth from assays of Black Thor DDH BT-09-17 84
Figure 4.8 Plot of Fe % vs. depth from assays of Black Thor DDH BT-09-17 84
Figure 4.9 Plot of Ca % and Al % vs. depth from assays of Black Thor
DDH BT-09-17 85
Figure 4.10 Plot of Ni, Fe %, Mg and Al % vs. depth from assays of Big Daddy
DDH FW-08-19 87
Figure 4.11 Plot of Ca % vs. depth from assays of Big Daddy DDH FW-08-19 87
Figure 4.12 Binary plots of Cr vs. Mg, Cr vs. Al, Cr vs. Fe, Al vs. Mg, Fe vs. Mg

 and Ca vs. Mg from assays of Black Label DDH BT-09-31.

89

Figure 4.13 Binary plots of Cr vs. Mg, Cr vs. Al, Cr vs. Fe, Al vs. Mg, Fe vs. Mg
and Ca vs Mg from assays of Black Thor DDH BT-08-10. Binary plots
of Al vs. Mg and Ca vs. Mg from assays of Black Thor DDH BT-09-17 90

x
Figure 4.14
Binary plots of Cr vs. Mg, Cr vs. Al, Cr vs. Fe, Al vs. Mg, Fe vs. Mg
and Ca vs. Mg from assays of Big Daddy DDH FW-08-19

 93
Figure 4.15 Primitive mantle multielement plot of dunite-harzburgite in DDH
BT-09-31 95
Figure 4.16 Primitive mantle multielement plot of pyroxenite in all three
deposits 95
Figure 4.17 Primitive mantle multielement plot of dunite-harzburgite in DDH
BT-08-10 and FW-08-19 97
Figure 4.18 Primitive mantle multielement plot of gabbro in DDH BT-09-17 97
Figure 4.19 Plot of (La/Sm)cn vs. (Gd/Yb)cn for Black Label, Black Thor and
Big Daddy host rocks 100
Figure 4.20 Primitive mantle PGE plot of dunite-harzburgite in DDH
BT-08-10 and FW-08-19 102
Figure 4.21 Primitive mantle PGE plot of dunite-harzburgite in DDH
BT-09-31 102
Figure 4.22 Primitive mantle PGE plot of pyroxenite from all three deposits 104
Figure 4.23 Primitive mantle PGE plot of chromitite from all three deposits 104
Figure 4.24 Plot of Mg/(Mg+Fe2+) vs. depth for chromite and olivine in Black
Label DDH BT-09-31 106
Figure 4.25 Ternary plot of pyroxene compositions 107
Figure 4.26 Ternary plot of clinopyroxene compositions in sample 486211 108
Figure 4.27 Ternary plot of orthopyroxene compositions in sample 486211 108
Figure 4.28 Plot of Ti vs. Al total for pyroxene in five samples

110

Figure 4.29
Plot of Mg # vs. Si for amphiboles with (Na+K)A = 0.50;

(Ca+NaB) = 1.00; 0.50< NaB < 1.50 with nomenclature of Leake

 et al. (1997). A winchite is plotted for amphiboles with (Na+K)A

< 0.50; (Ca+NaB) = 1.00; 0.50 < NaB < 1.50

111
Figure 4.30 Plot of tetrahedral Al vs. A site Na and K for all the amphiboles 113

xi
Figure 4.31
Plot of tetrahedral Al – A site Na and K vs. octahedral Al+2Ti+Cr
for all the amphiboles

113
Figure 4.32 Plot of Mg # vs. Si for amphiboles with CaB = 1.50; (Na+K)A >
0.50; Ti < 0.50; AlVI =Fe3+ with nomenclature of Leake et al.
(1997) 114
Figure 4.33 Plot of Mg/(Mg+Fe2+) vs. depth (m) for pargasite-edenite in Black
Label DDH BT-09-31 115
Figure 4.34 Plot of Mg # vs. Si for amphiboles with CaB = 1.50; (Na+K)A < 0.5
with nomenclature of Leake et al. (1997). 117
Figure 4.35 Plot of wt. % Al2O3 vs. wt. % TiO2 for phlogopite compositions 118
Figure 4.36 Ternary Ba-K-Na plot for phlogopites 119
Figure 4.37 Plot of wt. % MgO vs. depth for phlogopite in Black Label
DDH BT-09-31 121
Figure 4.38 Plot of wt. % Cr2O3 vs. depth for phlogopite in Black Label
DDH BT-09-31 122
Figure 4.39 Plot of wt. % Cr2O3 vs. wt. % MgO for phlogopite 123
Figure 4.40 Plot of wt. % Cr2O3 vs. wt. % TiO2 for phlogopite 123
Figure 4.41 Classification of McFaulds Lake chlorites after Hey (1954) 124
Figure 4.42 Classification of chlorites in DDH BT-09-31 after Hey (1954) 125
Figure 4.43 Classification of chlorites in DDH BT-08-10 and BT-09-17 after
Hey (1954) 126
Figure 4.44 Plot of wt. % Cr2O3 vs. wt. % Al2O3 for chlorite 128
Figure 4.45 Plot of wt. % Cr2O3 vs. wt. % MgO for chlorite 128
Figure 5.1 Plot of Cr2O3, Fe and Pt + Pd vs. depth from assays of Black Label
DDH BT-09-31

132
Figure 5.2 Plot of Ni and Cu vs. depth from assays of DDH BT-09-31

132
Figure 5.3 Plot of Cr2O3, Fe and Pt + Pd vs. depth from assays of Black Thor

DDH BT-08-10

134

xii
Figure 5.4
Plot of Ni and Cu vs. depth from assays of DDH BT-08-10

134

Figure 5.5
Plot of Cr2O3, Fe and Pt + Pd vs. depth from assays of Black Thor
DDH BT-09-17

135
Figure 5.6 Plot of Ni and Cu vs. depth from assays of DDH BT-09-17

135
Figure 5.7 Plot of Cr2O3, Fe and Pt + Pd vs. depth from assays of Big Daddy
DDH FW-08-19 138
Figure 5.8 Binary plots of Ti, V, Zn, Mn and Ni vs. Cr from assays of Black
Label DDH BT-09-31 140
Figure 5.9 Binary plots of Ti, V, Zn, Mn and Ni vs. Cr from assays of Black
Thor DDH BT-08-10 141
Figure 5.10 Binary plots of Ti, V, Zn, Mn and Ni vs. Cr from assays of Big

 Daddy DDH FW-08-19 142
Figure 5.11 Backscatter image of massive chromite with sample points shown 144
Figure 5.12 Backscatter image of sample 486044, chromite #1 with sample

 points shown 146
Figure 5.13 Plot of chromite evolution in Black Thor sample 486044, chromite

#1 146
Figure 5.14 Backscatter image of sample 486044, chromite #2 with sample

 points shown 147
Figure 5.15 Plot of chromite evolution in Black Thor sample 486044, chromite

#2 147
Figure 5.16 Backscatter image of sample 486129 with sample points shown 148
Figure 5.17 Plot of chromite evolution in Black Thor sample 486129 148
Figure 5.18 Plot of major oxide variation from disseminated to massive

 chromite in the chromite cores of the first fifty samples analysed in

Black Thor DDH BT-08-10

150
Figure 5.19 Variation of wt. % major oxide with height up section (down hole)

 in Black Thor DDH BT-08-10 for chromite cores of first fifty samples

analysed
150

xiii
Figure 5.20
Plot of Cr2O3 wt. % vs. depth for Black Label DDH BT-09-31 152

Figure 5.21
Plot of MgO wt. % vs. depth for Black Label DDH BT-09-31
with various zones and pulses shown

153
Figure 5.22 Plot of Cr/(Cr+Al+Fe3+) vs. depth for Black Label DDH BT-09-31 154
Figure 5.23 Plot of Mg/(Mg+Fe2+) vs. depth for Black Label DDH BT-09-31 155
Figure 5.24 Plot of FeO wt. % vs. depth for Black Label DDH BT-09-31 156
Figure 5.25 Plot of Cr/Fe vs. depth for Black Label DDH BT-09-31 157
Figure 5.26 Plot of Al2O3 wt. % vs. depth for Black Label DDH BT-09-31 158
Figure 5.27 Plot of Fe2O3 wt. % vs. depth for Black Label DDH BT-09-31 159
Figure 5.28 Plot of Cr/Fe vs. depth for Black Thor DDH BT-08-10 162
Figure 5.29 Plot of MgO wt. % vs. depth for Black Thor DDH BT-08-10
with various zones and pulses shown 163
Figure 5.30 Plot of Mg/(Mg+Fe2+) vs. depth for Black Thor DDH BT-08-10 164
Figure 5.31 Plot of Cr2O3 wt. % vs. depth for Black Thor DDH BT-08-10 165
Figure 5.32 Plot of Cr/(Cr+Al+Fe3+) vs. depth for Black Thor DDH BT-08-10 166
Figure 5.33 Plot of FeO wt. % vs. depth for Black Thor DDH BT-08-10 167
Figure 5.34 Plot of Al2O3 wt. % vs. depth for Black Thor DDH BT-08-10 168
Figure 5.35 Plot of Fe2O3 wt. % vs. depth for Black Thor DDH BT-08-10 169
Figure 5.36 Plot of Cr2O3 wt. % vs. depth for Black Thor DDH BT-09-17 170
Figure 5.37 Plot of MgO wt. % vs. depth for Black Thor DDH BT-09-17 171
Figure 5.38 Plot of Cr/(Cr+Al+Fe3+) vs. depth for Black Thor DDH BT-09-17 172
Figure 5.39 Plot of Mg/(Mg+Fe2+) vs. depth for Black Thor DDH BT-09-17 173
Figure 5.40 Plot of Cr/Fe vs. depth for Black Thor DDH BT-09-17

175
Figure 5.41 Plot of Al2O3 wt. % vs. depth for Black Thor DDH BT-09-17

177
Figure 5.42 Plot of FeO wt. % vs. depth for Black Thor DDH BT-09-17

178

xiv
Figure 5.43 Plot of Fe2O3 wt. % vs. depth for Black Thor DDH BT-09-17

179
Figure 5.44 Plot of Cr2O3 wt. % vs. depth for the first part of Big Daddy DDH
FW-08-19 180
Figure 5.45 Plot of MgO wt. % vs. depth for the first part of Big Daddy DDH
FW-08-19 181
Figure 5.46 Plot of Cr/(Cr+Al+Fe3+) vs. depth for the first part of Big Daddy
DDH FW-08-19 182
Figure 5.47 Plot of Mg/(Mg+Fe2+) vs. depth for the first part of Big Daddy
DDH FW-08-19 183
Figure 5.48 Plot of Cr/Fe vs. depth for the first part of Big Daddy DDH
FW-08-19 184
Figure 5.49 Plot of Al2O3 wt. % vs. depth for the first part of Big Daddy DDH
FW-08-19 186
Figure 5.50 Plot of FeO wt. % vs. depth for the first part of Big Daddy DDH
FW-08-19 187
Figure 5.51 Plot of TiO2 wt. % vs. depth for the first part of Big Daddy DDH
FW-08-19 188
Figure 5.52 Plot of Fe2O3 wt. % vs. depth for the first part of Big Daddy DDH

 FW-08-19 189
Figure 5.53 Plot of Cr2O3 wt. % vs. depth for Big Daddy DDH FW-08-19 190
Figure 5.54 Plot of MgO wt. % vs. depth for Big Daddy DDH FW-08-19

 with various zones and pulses shown 191
Figure 5.55 Plot of Cr/(Cr+Al+Fe3+) vs. depth for Big Daddy DDH FW-08-19 192
Figure 5.56 Plot of Mg/(Mg+Fe2+) vs. depth for Big Daddy DDH FW-08-19 193
Figure 5.57 Plot of Cr/Fe vs. depth for Big Daddy DDH FW-08-19

195
Figure 5.58 Plot of FeO wt. % vs. depth for Big Daddy DDH FW-08-19

196
Figure 5.59 Plot of Al2O3 wt. % vs. depth for Big Daddy DDH FW-08-19

197
Figure 5.60 Plot of Fe2O3 wt. % vs. depth for Big Daddy DDH FW-08-19

198

xv
Figure 5.61 Binary plot of Cr2O3 vs. MgO wt. % for Black Label DDH
BT-09-31 with paths of chromite evolution shown 200
Figure 5.62 Black Label Layers 1 and 2 of DDH BT-09-31 200
Figure 5.63 Binary plot of Al2O3 vs. MgO wt. % for Black Label DDH
BT-09-31 202
Figure 5.64 Binary plot of FeO vs. MgO wt. % for Black Label DDH
BT-09-31 202
Figure 5.65 Binary plot of TiO2 vs. Fe2O3 wt. % for Black Label DDH
BT-09-31 203
Figure 5.66 Binary plot of TiO2 vs. Cr2O3 wt. % for Black Label DDH
BT-09-31 203
Figure 5.67 Binary plot of TiO2 vs. FeO wt. % for Black Label DDH
BT-09-31 205
Figure 5.68 Binary plot of ZnO vs. Cr2O3 wt. % for Black Label DDH
BT-09-31 205
Figure 5.69 Binary plot of NiO vs. Cr2O3 wt. % for Black Label DDH
BT-09-31 206
Figure 5.70 Binary plot of Cr2O3 vs. MgO wt. % for Black Thor DDH
BT-08-10 with paths of chromite evolution shown 207
Figure 5.71 Binary plot of Al2O3 vs. MgO wt. % for Black Thor DDH
BT-08-10 207
Figure 5.72 Binary plot of FeO vs. MgO wt. % for Black Thor DDH
BT-08-10 208
Figure 5.73 Binary plot of TiO2 vs. Cr2O3 wt. % for Black Thor DDH
BT-08-10 208
Figure 5.74 Binary plot of ZnO vs. Cr2O3 wt. % for Black Thor DDH
BT-08-10 210
Figure 5.75 Binary plot of NiO vs. Cr2O3 wt. % for Black Thor DDH
BT-08-10 210

xvi
Figure 5.76
Binary plot of MnO vs. Cr2O3 wt. % for Black Thor DDH
BT-08-10 211

Figure 5.77
Binary plot of Cr2O3 vs. MgO wt. % for Black Thor DDH
BT-09-17 with paths of chromite evolution shown

212

Figure 5.78
Binary plot of Al2O3 vs. MgO wt. % for Black Thor DDH
BT-09-17 212

Figure 5.79
Binary plot of FeO vs. MgO wt. % for Black Thor DDH
BT-09-17 214

Figure 5.80
Binary plot of TiO2 vs. Cr2O3 wt. % for Black Thor DDH
BT-09-17 214

Figure 5.81
Binary plot of ZnO vs. Cr2O3 wt. % for Black Thor DDH
BT-09-17 215

Figure 5.82
Binary plot of NiO vs. Cr2O3 wt. % for Black Thor DDH
BT-09-17 215

Figure 5.83
Binary plot of MnO vs. Cr2O3 wt. % for Black Thor DDH
BT-09-17 215

Figure 5.84
Binary plot of Cr2O3 vs. MgO wt. % for Big Daddy DDH
FW-08-19 with paths of chromite evolution shown 217

Figure 5.85
Binary plot of Al2O3 vs. MgO wt. % for Big Daddy DDH
FW-08-19 217

Figure 5.86
Binary plot of FeO vs. MgO wt. % for Big Daddy DDH
FW-08-19 219

Figure 5.87
Binary plot of TiO2 vs. Cr2O3 wt. % for Big Daddy DDH
FW-08-19 219

Figure 5.88
Binary plot of ZnO vs. Cr2O3 wt. % for Big Daddy DDH
FW-08-19 220

Figure 5.89
Binary plot of NiO vs. Cr2O3 wt. % for Big Daddy DDH
FW-08-19 220

Figure 5.90
Binary plot of MnO vs. Cr2O3 wt. % for Big Daddy DDH

 FW-08-19
221

xvii
Figure 5.94 Chromite in MORB trace element plot of Black Label DDH
BT-09-31 223
Figure 5.95 Chromite in MORB trace element plot of Black Thor DDH
BT-08-10 223
Figure 5.96 Chromite in MORB trace element plot of Big Daddy DDH
FW-08-19 225
Figure 5.97 Binary plots of Cr vs. Ti, V, Zn, Mn, Ni, Co, Sc and Ga ppm for
Black Label DDH BT-09-31 226
Figure 5.98 Binary plots of Cr vs. Ti, V, Zn, Mn, Ni, Co, Sc and Ga ppm for
Black Thor DDH BT-08-10 227
Figure 5.99 Binary plots of Cr vs. Ti, V, Zn, Mn, Ni, Co, Sc and Ga ppm for
Big Daddy DDH FW-08-19 229
Figure 6.1 Cr # vs. Mg # plot of McFaulds Lake chromites with other layered
intrusion and komatiite chromites of the world 231
Figure 6.2 Cr # vs. Mg # plot of McFaulds Lake chromites with other chromite
deposits of the world 231
Figure 6.3 Ternary Cr-Fe3+-Al plot of the McFaulds Lake chromites with other
layered intrusion and komatiite chromites of the world 234
Figure 6.4 The annealing process from Hulbert and Von Gruenewaldt (1985) 241
Figure 6.5 Phase Relations in the System Olivine-Silica-Chromite as
determined by Irvine (1977) 251
Figure 6.6 Differing primitive mantle trace element patterns of dunite and
pyroxenite 253
Figure 6.7 Differing primitive mantle PGE patterns of dunite and pyroxenite 253
Figure 6.8 Double diffusive convection model 258
Figure 6.9 Double diffusive convection cells in a magma chamber

258
Figure 6.10 Step-wise double diffusive chromite-PGE mineralization

260

Figure 6.11 Figure showing thickness, grade and wt. % Cr in the 36 m-thick ore

zone at Big Daddy 265
Figure 6.12 Residual gravity map with chromitite zones plotted 268

xviii
List of Tables
Table 3.1 Summary of drill holes 31
Table 4.1 Major oxide wt. % in DDH samples 76

1
CHAPTER 1

INTRODUCTION

1.1 McFaulds Lake Chromite Deposits
Three new chromite deposits have been discovered in the McFaulds Lake area of
the “Ring of Fire” District in the James Bay Lowlands region of northern Ontario. The
largest Black Thor deposit is up to 46 m thick with 40 % Cr2O3 in massive chromitite that
extends along strike for 2.6 km. These new discoveries of high grade chromite have
associated PGE enrichment and are only exceeded by deposits such as the Bushveld
Complex in South Africa, the Great Dyke of Zimbabwe and Kazakhstan for global
chromium resources. Historically, the main source of chromite has been in South Africa,
however this new resource will allow North America to sustain itself. Mining is planned
with a 30 year mine life predicted. This operation will have a major impact on the
economic development of Northern Ontario. These new chromite deposits are classified
with the group of stratiform magmatic Cr/PGE ores in layered complexes (Duke, 1988).
Better understanding of their formation will facilitate stratigraphic correlation, thus
instrumental in defining an exploration vector. The occurrence of multiple zones of basal
massive vs. disseminated styles of mineralization indicates primary magmatic cumulate
concentration of the chromite.

1.2 Thesis Objective
The objective of this project is to investigate the origin of the McFaulds Lake
chromite deposits. The chromite deposits have undergone an igneous crystallization
history that has in turn been modified by a pervasive hydration overprint. Therefore the
origin of the chromite deposits involves both a study of the magmatic crystallization of
the chromite and the retrogressive hydration that has since modified the grade of the ores.
The study provides a detailed geochemical profile of chromite in three deposits: the
Black Label, Black Thor and Big Daddy chromitites. It involves petrographic analysis of
primary igneous chromite and associated hydrous silicate mineralogy; whole rock

2
geochemical and full spectrum PGE analysis of chromite and chromite host rock; mineral
chemical analysis of host rock silicates and silicates in association with chromite; detailed
electron microprobe analyses of chromite in the three deposits and laser ablation trace
geochemical analysis of chromite minerals. Results will be discussed in the final chapter.

The project is both field and laboratory-based, focusing on drill core since there is
only sparse outcrop in the muskeg-covered lowlands. The logging of drill core allows
sampling of chromitite layers in igneous stratigraphy. Basal lithologies of the intrusion
consist of dunite-peridotite and oikocrystic harzburgite hosting disseminated to heavily
disseminated chromite with intermittent beds of semi-massive to massive chromite and
local magmatic chromite breccia. Overlying units include heterogeneous olivine
pyroxenite and pyroxenite capped by leucogabbro-gabbronorite. These lithologies are
pervasively hydrated with essentially complete serpentinization of olivine; the serpentine
coexists with talc, tremolite, chlorite, kaemmererite, and magnetite.

The mineral chemistry of the various chromitites at Big Daddy, Black Label and
Black Thor needs to be documented for metallurgical purposes. The higher and more
consistent Cr# in the more massive chromitite makes such zones most profitable to mine.
Cr# measured in 3 strategic drill holes can be correlated to trends of chromitites in other
drill holes along strike. In addition to bulk rock wt. % Cr2O3, microprobe data is crucial
in documenting the complex chromite mineral chemistry of the ore.

1.3 Location and Climate (from Aubut, 2010)
The McFaulds Lake chromite deposits are located in an area of complete muskeg
cover in the James Bay Lowlands (Fig. 1.1). The site location for core storage is at Esker
Camp serving as a hub for helicopter supported drill programs. It is located in
northwestern Ontario, Canada, approximately 250 km north of the town of Nakina and 80
km east of the native village of Webequie. The camp is situated in the Porcupine Mining
Division in area BMA 527861 (G-4306) with UTM NAD 83 coordinates of 547544E,
5843918N. The Black Label and Black Thor deposits are held by Cliffs Natural
Resources Inc. while the Big Daddy deposit is 75 % owned by Cliffs and 25 % owned by
KWG Resources Inc.

The James Bay Lowlands area has a typical continental climate with extreme
temperature fluctuations from the winter to summer seasons. During the summer months

3
Figure 1.1. Location map of the McFaulds Lake chromite deposits. Source from
www.kwgresources.com.

4
this can be moderated by the maritime effects of James and Hudson Bays. Summer
temperatures range between 10ºC and 35ºC, with a mean temperature of 13ºC in July.
Winter temperatures usually range between -10ºC and -55ºC with an average January
temperature of -23ºC. Lakes typically freeze-up in mid-October and break-up is usually
in mid-April. The region usually receives approximately 610 mm of precipitation per
year, with about 1/3 originating as snow during the winter months. On a yearly basis the
area averages about 160 days of precipitation per year.

1.4 Previous Work
Previous work relevant to this thesis include several investigations that provide
petrographic and microprobe data in private company reports, NI-43-101 reports are
available on both the Black Label-Black Thor and Big Daddy deposits (Aubut, 2010,
2012; Barrie, 2010; Gowens, 2009; Karagas, 2009; Metsaranta, 2010, 2011, 2012;
Scoates, 2008a, 2008b, 2009a, 2009b; Tuchscherer, 2010). The junior companies
involved in this early phase of work before being bought out by Cliffs Natural Resources
Inc. include: Freewest Resources Inc. which held Black Label-Black Thor, Spider
Resources Inc. who owned 25 % of Big Daddy and KWG Resources Inc. still owns 25 %
of Big Daddy. The drilling of Black Label-Black Thor was carried out by Freewest
Resources Inc. while Big Daddy was first drilled by Spider-KWG. The drilling history
relevant to the drill holes of this study is as follows: In November 2008, DDH BT-08-10
was drilled as one of the first holes that cored Black Label-Black Thor. Subsequent
drilling programs containing DDH BT-08-17 and BT-09-31 were drilled in the winter of
2008-2009. DDH FW-08-19 was drilled as one of the first nineteen drill holes at Big
Daddy in the winter of 2008. Drilling continued in 2008 for DDH FW-08-05 to FW-0823
and up to FW-09-60 into 2009. The drill program for Black Label-Black Thor
continued in 2009 to DDH BT-09-113. The 2010 Black Thor holes drilled under Cliffs’
operation include DDH BT-10-114 to BT-10-174. The 2011 Black Label-Black Thor
drill holes include DDH BT-11-175 to BT-11-203. Big Daddy drilling under Cliffs’
operation occurred in fall-winter 2011-2012 for DDH FW-11-61 to FW-11-112.

During the early 2008-2009 drill programs by Freewest and Spider-KWG, several
technical reports were written on the petrography and preliminary whole rock assays of
the host rocks and chromitites to Black Label-Black Thor and Big Daddy (Scoates,

5
2008b, 2009a, b). This preliminary work involved the first classification of the host
rocks and chromitites for drilling purposes and included considerable detailed
petrographic descriptions supplemented with hand sample and thin section photographs,
as well as core logging notes that proved useful for the petrography chapter of this thesis.
Scoates (2008a) cites several whole rock analyses similar to the whole rock geochemistry
reported in this thesis.

As a component of the 2008 Freewest drill program, XRF, XRD and SEM-EDS
analyses were performed on 27 samples from three drill holes. Sixty-nine single element
determinations were performed by Karagas (2009). These analyses provided the initial
framework for the undertaking of electron microprobe work reported in this thesis. Other
technical reports that proved useful included the technical draft drill report to Freewest by
Tuchscherer et al. (2010), an NI-43-101 on Black Label-Black Thor by Aubut (2010) of
the Sibley Basin Group, and NI-43-101 reports on Big Daddy by Gowens (2009) of
Micon International Ltd. and by Aubut (2012). Whole rock geochemical and metal assay
data was provided by Spider-KWG and Freewest for the 3 strategic drill holes chosen for
this study. Barrie (2010) reported on PGE mineralogy of the Black Thor deposit.
Tuchscherer (2010) compiled a map of the Black Label-Black Thor zones on the basis of
drill core information and a similar map was also provided by Spider-KWG. Metsaranta
(2010, 2011 and 2012) has several reports for Summary of Field Work of the Ontario
Geological Survey and these were considered in the writing of the geology chapter.

1.5 Methods
The four holes drilled by Freewest Resources and Spider-KWG Resources,
including BT-08-10, BT-09-17, BT-09-31 and FW-08-19 were logged by the author.
Representative lithologies were sampled for petrographic, whole rock XRF (X-ray
Fluoresence Spectrometry) and ICP-MS (Inductively Coupled Plasma – Mass
Spectrometry), electron microprobe mineral, laser ablation ICP-MS and full spectrum
PGE analyses. Details of the logging and number of samples analysed are found in the
following chapters. Polished thin sections of 30 µm thickness were made for petrographic
and mineral chemical analysis, 100 µm thick slides were made for the laser ablation
work.

6
1.5.1 XRF (X-Ray Fluorescence Spectrometry) and ICP-MS (Inductively Coupled
Plasma-Mass Spectrometry)
The samples chosen for XRF and ICP-MS were first slabbed and polished thin
sections were made for preliminary examination of texture and mineralogy utilizing both
transmitted and reflected light microscopy. The rock samples were later crushed into
powders and analysed by XRF and ICP at Activation Laboratories in Ancaster, Ontario.
Sample preparation included the crushing to a nominal minus 10 mesh (1.7 mm),
mechanically split (riffled) and then pulverized to 95 % minus 150 mesh (105 microns).
In preparation for XRF whole rock geochemical analysis, the samples were homogenized
by lithium metaborate/tetraborate fusion. The resulting molten beads were rapidly
digested in a weak nitric acid solution and then were analysed by XRF and ICP. A base
metal suite and sulphide sulphur were determined on an aquia regia extraction with an
ICP/OES (Inductively Coupled Plasma-Optical Emission Spectroscopy) finish. For the
aquia regia extraction, a combination of concentrated hydrochloric and nitric acids were
used to leach total sulphide, oxide and silicate. A partial extraction was also analysed by
ICP-MS for lower detection limits. ICP-MS analysis was also employed on samples for
trace elements and REE. In preparation, these samples were again reduced by lithium
metaborate/tetraborate fusion into beads that were digested in weak nitric acid to be
analysed by ICP-MS.

1.5.2 Full spectrum PGE analysis
The same samples analysed by XRF and ICP were analysed for full spectrum
PGE along with six other samples. Nickel sulphide fire assay was carried out on 50 g
samples. The samples were fired at 1100 degrees C whereby nickel sulphide droplets
scavenged the PGE and formed buttons at the bottom of the crucible. The nickel sulphide
buttons were dissolved in concentrated HCl and the resulting residues which contained all
the PGE and Au were collected on a filter paper. This residue undergoes 2 irradiations
and 3 separate counts to measure all the PGE and Au. An INAA (Instrumental Neutron
Activation Analysis) finish was later performed on the samples. Elements of Os, Ir, Ru,
Rh, Pt, Pd, Au and Re were analysed with the respective detection limits of 2, 0.1, 5, 0.2,
5, 2 and 0.5 ppb.

7
1.5.3 Electron Microprobe Analysis
Electron microprobe analysis was performed on over 300 samples mostly by R.L.
Barnett Geoanalytical Consulting Ltd using a JEOL Model 733 electron microprobe
equipped with five wavelength spectrometers and using the Tracor Northern Automation
System. A subset of the 300 samples was further analysed by Jim Renaud of Renaud
Geological Consulting Ltd using a similar JEOL Model 733 microprobe. Thin sections
were carbon coated to prevent charging during analysis. Samples were analysed with an
accelerating voltage of 45 kV, a beam current of 10 nÅ and an electron beam width of 2
µm. Standards from the Smithsonian Institute were used to calibrate for Si, Ti, Al, Cr,
Fe, Mn, Mg, Zn and Ni. Ferrous/ferric recalculations were later made for Fe.

1.5.4 Laser Ablation ICP-MS
Laser ablation ICP-MS was performed on 37 samples at the Geological Survey of
Canada facility in Ottawa, Ontario under the supervision of Simon Jackson. Analyses
were made on 100µm thick polished thin sections. The thick sections were necessary to
reduce spalling and allow longer ablation times to improve detection limits. Before
analysis in Ottawa, an internal standard of FeOT was needed for calibration to correct for
variable ablation yield. Accordingly, polished chromites were analysed by microprobe
for FeOT before the LA ICP-MS analysis. After the microprobe work, the carbon coating
was removed from the sections so as to not interfere with the LA analyses. Scans were
made and circles drawn on the thin sections for select chromite grains prior to and in
order to speed up the choice of grains for ablating. The laser ablation was conducted on a
Photon-Machines Analyte 193 excimer laser ablation system (.=193 nm) with a Helex
ablation cell and an Agilent 7700x quadrupole ICP-MS. The software package used for
data reduction was GLITTERTM. The analyses were conducted using a 69 µm or an 86
µm spot size, a 14 Hz frequency, 40 % of 5 mJ energy during a total acquisition of 100
seconds (~40 seconds for the gas blank and ~60 seconds for the chromite). In addition to
the trace elements analysed (Sc45, Ti47, Ti49, V51, Mn55, Co59, Ni60, Zn66, Ga69, Ga71),
other elements (Mg25, Al27, Si29, Ca42, Cr53, Fe57, Cu63, Cu65, Ge73, As75, Sr88, Y89, Zr90,
Zr91, Nb93, Mo95, Mo98, Ru99, Ru101, Ru102, Rh103, Ru104, Pd105, In115, Sn118, Sb121, La139,
Ce140, Yb174, Hf178, Ta181, W182, Os189, Ir191, Os192, Ir193, Pt195, Pb206, Pb207, Pb208, Th232,
U238) were monitored during chromite ablation to control the nature of the ablated

8
material by identifying contaminants like the presence of included phases. Care was
taken in selecting isotopes where there was no interference with argides and where there
was acceptable range in uncertainty. For those elements where there were two isotopes,
the isotopes that were chosen that had a lower range of uncertainty were Ti49, Ga71, Zr91,
Mo95 and Pb206. For other elements with two isotopes, isotopes chosen on a basis of no
interference with argides were Ru102, Ir193, Os192, and Cu63. Standards used for
calibration include GSE-1G and Po726 for sulphide. The standards GOR 128 and BCR2G
were used for quality control standard and blanks.

9
CHAPTER 2
GEOLOGICAL SETTING

2.1 Oxford-Stull Domain
The McFaulds Lake chromite deposits are hosted in the Ring of Fire Intrusion,
located in the McFaulds Lake Greenstone Belt in Northern Ontario. Regionally, this
greenstone belt is located in the Oxford-Stull Domain of the former Sachigo Subprovince
in the greater Archean Superior Province (Fig. 2.1). The Neoarchean 2870-2707 Ma.
Oxford-Stull Domain is interpreted to form an intracratonic rift setting separating the
Mesoarchean North Caribou Terrane from the more northerly Hudson Bay Terrane (Stott
et al. 2010).

The Oxford-Stull Domain is a WNW-ESE striking granite-greenstone terrane that
is bounded to the north by the North Kenyon Fault and to the south by the Stull-
Wunnummin and Gods Lake Narrows shear zones. The latter are known to host several
lode gold occurrences (Tuchscherer et. al, 2009; Fig. 2.2). A larger SSW-NNE oriented
unknown fault also cross-cuts the terrane in the region of the Ring of Fire Intrusion
(Vaillancourt, 2003). These same faults control the emplacement of other mafic
intrusions in the region, including the Highbank Lake-Fishtrap Lake intrusive complex
and the Winiskisis Channel gabbros (Metsaranta and Houlé, 2012). The eastern
extension of the terrane is the La Grande Domain in Quebec which hosts chromite
occurrences in the Menarik Complex (Stott et al., 2010; Houlé, 2000; fig. 2.1).

The Big Trout Lake Complex, which is 50 km to the ESE, is a layered intrusion in
the Sachigo Greenstone Belt that may have formed in a similar setting to the Ring of Fire
Intrusion. It consists of a basal peridotite zone overlain by an anorthosite to quartz
gabbro and finally monzodiorite. The peridotite intruded as two distinct magmas in 5
pulses: 1 pulse forming lower peridotite followed by 4 pulses forming upper peridotite
higher in stratigraphy. The peridotite is generally olive green due to its high olivine

10
Figure 2.1. Geological map of the Superior Geological Province. The Oxford-Stull
Domain is found within the large dashed box. Another near-contemporaneous chromite
deposit is the Menarik Complex in the La Grande Domain (outlined in small box). From
Houle, Lesher and Metsaranta (2012).

Figure 2.2. Aeromagnetic map of the Oxford-Stull Domain showing emplacement of intrusios along large WNW-ESE
striking crustal faults. The Ring of Fire Intrusion is outlined in the box. From James Bay Resources Ltd. Website.

11

12
content, contains poikilitic orthopyroxene with interlayers of chromitite and magmatic
sulphides occurring at the base of the pulses. The one pulse of lower peridotite has a
trend of increasing olivine content with stratigraphic height due to the presence of
poikilitic orthopyroxene in its lower portion. Chromitite layers increase towards the base.
It is distinguished from the other pulses by greater increasing (MgO+FeO)/Al2O3 with
SiO2/Al2O3 that parallels lesser increasing (MgO+FeO)/Al2O3 with SiO2/Al2O3 for the
successive pulses (Borthwick, 1984).

The Oxford-Stull Domain is made up of granitoids and greenstones that form
dome and keel structures where the supracrustal greenstone belts (keels) wrap around
central granitoid batholiths (domes). The batholith in the Winisk Lake-Muketei River
area is an unnamed quartz monzonite to trondhjemite with sinuous bodies of quartz
diorite in the Muketei River Area (Thurston et al., 1979). Such quartz monzonite diapirs
have been described in other parts of the world such as in the 2.8 Ga Kiviaapa Dome to
the Koitelainen Intrusion and associated chromite deposits in Finland (Mutanen and
Huhma, 2001 and Mutanen, 1997). Metsaranta and Houlé (2010) describe the pluton in
the Muketei River Area as a foliated biotite tonalite to granodiorite with cross-cutting
tonalite to quartz diorite bodies indicating multiple intrusive ages. Since there is the
presence of both biotite and amphibole varieties of tonalite, TTG (tonalite-trondhjemitegranodiorite)
suites in the North Caribou Terrane form from varying degrees of combined
melting of garnet-amphibolite subducting slabs and hornblende-dominated fractional
crystallization (Wyman et al., 2011). This batholith is the basement to the Ring of Fire
Intrusion. The granodiorite has a determined age of 2773.4±0.9Ma (Mungall et al., 2010).
Observation of drill core has shown it to be younger than the intrusion (see petrography
chapter). However, there are biotite xenoliths in the granodiorite that are possibly from
an older basement crust. The basement Kiviaapa batholith to the Koitelainen Intrusion
has been described by Mutanen (1997) to be a biotite-plagioclase mica gneiss. There
may be a similar foliated basement TTG to the Ring of Fire Intrusion.

2.1.1 McFaulds Lake Greenstone Belt
Volcanism began in the McFaulds Lake Greenstone Belt with the eruption of
various successions of mafic to felsic dominanted volcanics defining five different
packages (Fig. 2.3).

13
15

[

Figure 2.3. Simplified geological map of the McFaulds Lake area showing distribution of
the supracrustal packages. From Metsaranta and Houlé (2012).

14
The Muketei River supracrustal package is both footwall and hangingwall to the
synvolcanic Ring of Fire Intrusion. Locally, lower mafic volcanic and gabbros have been
found in the footwall to the Blackbird and Black Horse chromitites to the east of the
granodiorite contact. Volcanism began ca. 2770.7±0.8 Ma with the eruption of footwall
mafic volcanics (Mungall, Azar and Hamilton, 2011). Although geochemistry has not
been determined, the mafic volcanics are probably ocean floor MORB volcanics similar
to such MORB basalts of the Hayes River Group in the western part of the Oxford-Stull
Domain. The mafic volcanics locally show pillowed facies with intercalated cherty iron
formation (Metsaranta and Houlé, 2011).

The Ring of Fire Intrusion is a layered komatiitic sill that hosts the Eagle’s Nest
sulphide deposits and McFaulds Lake chromite deposits. The layered complex gives rise
to the arcuate shaped magnetic anomaly on the airborne aeromagnetic map (Fig. 2.2).
The southwest conduit to the intrusion hosts the Eagle’s Nest deposits (Fig. 2.4). The
Eagle’s Nest magmatic sulphides accumulated in a shallowly plunging or subhorizontal
keel structure at the base of a dike-like chonolith. It has been subsequently deformed into
a vertically plunging shoot of sulphide mineralization occurring on the west margin of a
north-south striking dike (Mungall et al., 2010). The Eagle’s Nest deposits are comprised
of disseminated, net textured and massive sulphides of pyrrhotite, pentlandite and
chalcopyrite with subsidiary accessory amounts of magnetite. Total measured and
indicated reserves are 11 Mt at 1.78 % Ni and 0.98 % Cu together with significant Pt and
Pd (Baldwin, 2012). This mineralization is attributed to sulphide saturation following
extensive contamination of the komatiitic magma by granodiorite country rock. The
presence of abundant magnetite-rich xenoliths in the intrusion records assimilation of
iron formation, which may have added sulphide to the magma to induce sulphide liquid
saturation (Mungall et al., 2010). Host rocks to the deposit include harzburgite, lherzolite
and marginal gabbro (Mungall et al., 2010).

The Ring of Fire Intrusion is a layered sill of dunite, peridotite, chromitite,
pyroxenite, gabbro, leucogabbro, and gabbronorite (Tuchscherer et. al, 2009; Fig. 2.5).
This ultramafic complex is up to 500 metres thick and has been traced for over 15
kilometres along strike (Aubut, 2012; Fig. 2.4). The Blackbird chromite deposit occurs
within the main dunite sequence near the Eagle’s Nest deposit. This deposit comprises a

1515
Figure 2.4. Geology map of the Ring of Fire Intrusion showing location of the Eagle’s
Nest sulphide and McFaulds Lake chromite deposits. Geology after Mungall.

Dunite
Dunite/lesser pyroxenite
Dunite
Pyroxenite/lesser dunite
Pyroxenite
Granodiorite
Figure 2.5. Generalized stratigraphic column of the Ring of Fire Intrusion at Black
Label-Black Thor. Modified from Tuscscherer (2010).

16
series of steeply dipping chromitite lenses that have been overturned and young to the
east (Fig. 2.6). Cr/(Cr+Al) ratios of chromite cores show little variability with an average
value of 0.68 for all five zones in the Blackbird deposit (Azar and Mungall, 2010).
Detailed electron microprobe analysis of chromite cores reveals Cr/(Cr +Al) atomic ratios
from 0.63-0.77 and Mg/(Mg + Fe2+) atomic ratios from 0.12-0.62 (Azar, 2010).
Generally Cr/(Cr +Al) is positively correlated with the Mg-number. The chromitites
have been hypothesized to have formed as a result of assimilation of banded iron
formation by a picritic ultramafic magma (Mungall, 2008).

The Black Horse and Big Daddy chromite deposits occur 5 km north of Blackbird
and 3 km south of Black Thor. The Big Daddy deposit was the first chromite deposit
discovered in the area and has a measured and indicated resource of 37.4 Mt at 28.5 %
Cr2O3 (Aubut, 2012). This deposit is stratiform between lower dunite and overlying
pyroxenite (Fig. 2.7). Various types of chromite mineralization have been observed
including disseminated chromite (1 to 20% chromite), semi-massive chromite and
massive >80% chromite. The main chromitite layer is up to 60 m thick and has been
traced over 1.4 km along strike (Aubut, 2012). The chromite is present as fine euhedral
grains typically 100 to 200 µm within peridotite and in the higher grade portions within
dunite. Chromite may be intensely fractured, with internal veinlets and spherical
inclusions of silicate gangue (SGS Minerals Services, 2009 in Aubut, 2012).

The Black Creek and Black Label-Black Thor mineralization occurs 3 km
northeast of Big Daddy. The Black Label deposits occur below the main dunite layer that
hosts the Big Daddy deposit and so was an earlier mineralizing event (Fig. 2.8). The
Black Label Chromite Zone has been drilled for over 2.2 km along strike. It is cross-cut
by a pyroxenitic body to the north. Chromite is generally fine grained and disseminated
in peridotite, locally forming chromite-bearing magmatic breccias and semi-massive
bands to massive chromitite bands. Silicate fragments, in the form of rip up clasts and as
ovoid blebs indicate chromite concentration in a highly dynamic magmatic environment.
Fine-grained disseminated sulphides are locally associated with the chromitite bands
(Aubut, 2010).

The Black Thor deposit has been traced along strike 2.6 km. It is the most
extensive chromite bearing body in the region. It has a measured and indicated resource

17
Figure 2.6. Geology of the Blackbird chromite deposit showing distribution of chromitite
lenses. From Azar and Mungall (2010).

FW-08-19
18FW-08-19
18
Figure 2.7. Geology of the Big Daddy chromite deposit. The chromite is between dunite
and pyroxenite in orange. Diamond drill hole of study is shown. Map courtesy of KWG
Resources Inc.

19
0 250 1,000
Metres
500
GEOLOGICAL LEGEND
Schist
Basalt
Iron formation
Gabbro2
Pyroxenite2
Gabbro
Heavily disseminated chromite
Disseminated chromite
Intermittent chromitite beds
Semi-massive chromite
Chromitite
Magmatic breccia
Pyroxenite
Peridotite
Dunite
Granodiorite
Black Label Black Thor
Figure 2.8. Geology of the Black Label and Black Thor chromite deposits. Diamond drill
holes of study are shown. After Tuchscherer, courtesy of Freewest/Cliffs Natural Resource
Inc.

20
of 111.9 Mt at 30.9 % Cr2O3 (Cliffs Natural Resources Inc., 2012 Annual Report, p. 54).
It strikes SW/NE and has an overturned sub-vertical dip ranging between 70 and 85
degrees NW. The zone typically contains two chromitite layers (lower and upper) that
can range in thickness from 10’s of meters to over 100 m (i.e. DDH BT-09-37; Aubut,
2010). These layers are separated by a band of disseminated chromite in
peridotite/dunite. Host lithologies consist of serpentinized peridotite, serpentinized
dunite, dunite, and pyroxenite. The chromite is present as fine to heavily disseminated
chromite in dunite/peridotite, intermittent chromite beds and semi-massive to massive
chromitite. Because of its lateral continuity and uniformity the Black Thor chromite
mineralization was likely deposited in a quiescent magmatic environment (Aubut, 2010).
The leucogabbro at the top of the Big Daddy-Black Thor stratigraphy grades into the
mafic volcanics of the Muketei River package. Hydration of the Ring of Fire Intrusion
caused retrogression of the olivine and pyroxene to greenschist facies serpentine, talc,
tremolite, chlorite, kaemmererite with trace to minor associated magnetite, sausserite,
zoisite and titanite.

Overlying intermediate volcanics have been age dated at 2737±7 Ma (Rayner and
Stott, 2005). The volcanics are composed of fine-grained tuff, rare coarse-tuff breccias
and more flow-like lithologies (Metsaranta and Houlé, 2011). These volcanics are host to
the McFaulds Lake VMS deposits. Intrusion of the mafic-dominated Thunderbird
intrusion to the east of the Ring of Fire Intrusion was coeval with intermediate to felsic
volcanism. This intrusion is one of a series of mafic intrusions in the area that are
composed of gabbro-anorthosite-ferrogabbro±pyroxenite (Metsaranta and Houlé, 2011).
An age of 2734.5±1.0 Ma has been determined for the ferrogabbro (Mungall et al., 2010).
Significant V-Ti-Fe mineralization has been discovered In the Thunderbird intrusion.

2.2 Deformation
The Muketei River supracrustal package overlying the Ring of Fire Intrusion is
overturned by the doming of the basement granodiorite batholith. An age of 2696±3 Ma
has been determined from granodiorite within the core of the batholith (Rayner and Stott,
2005). The central granodiorite represents the age of “Kenoran” diapiric plutonism.
Quartz monzonite diapirism is inferred to occur proximal to other intrusions such as the
Koitelainen Intrusion and associated chromite deposits in Finland (Fig. 2.9). The Ring of

21
Figure 2.9. Quartz monzonite diapirism occurred in the vicinity of the Koitelainen
Intrusion and associated chromite deposits in Finland. This is a similar scenario to the
granodiorite diapirism in the vicinity of the Ring of Fire Intrusion. From Mutanen
(1997).

22
Fire Intrusion hosting the chromitite dips steeply to the east as at Big Daddy or is
overturned steeply to the west as at Black Label and Black Thor (Figs. 2.10 and 2.11).
There is dextral strike-slip displacement of stratigraphic units in the intrusion (Fig. 2.12).
The highest chromite layer in the eastern part of the Black Thor stratigraphy intersected
in DDH BT-09-37 is a major zone of questionable provenance. This chromitite unit does
not have a western extension and is bounded by mylonite. Late faults transecting the
deposits give rise to incoherent fault gouges, fault breccias, coherent cataclastic breccias
and ductile phyllonitic and mylonitic shear zones (Poulsen, 2010). Foliation fabrics are
developed in serpentinized units. Late aphanitic green and grey to brown micaceous to
amphibole and feldspar-bearing lamprophyric dikes commonly intrude along these areas
of structural weakness.

23
Figure 2.10. Drill section
through Big Daddy DDH
FW-08-19 showing the
intrusion is plunging to the
east, looking northeast.

Figure 2.11. Drill section
through Black Thor DDH BT08-
10 showing the intrusion is
plunging to the west, looking
northeast.

24
Figure 2.12. Dextral strike-slip faults offset some of the Black Thor chromitites such as
the Upper-Upper zone chromitite in the northeast part of the Black Thor sequence. From
Poulsen (2010).

25
CHAPTER 3

PETROGRAPHY

3.1 Introduction
This petrographic study of the McFaulds Lake chromite deposits entails both host
lithologies to the chromite as well as the different styles of chromite mineralization. In
order to define the host rock igneous stratigraphy, 13 drill holes were logged and
photographs taken of key textures. Logging commenced in September 2009 and at this
time 3 strategic holes were selected, one from each of the 3 deposits Black Label, Black
Thor and Big Daddy. Detailed sampling resulted in selecting 600 samples of
representative drill core. These are Black Label DDH BT-09-31, Black Thor BT-08-10
and BT-09-17 and Big Daddy FW-08-19 (Figs. 3.1 to 3.4; see figures 2.7 and 2.8 for drill
plan, Appendix 1 for core logs and Appendix 2 for sample #s). Thirteen additional drill
holes were logged over the summer of 2010 at McFaulds Lake, these were sited on the
same section line as the initial strategic holes chosen for study. All three strategic holes
were re-examined at this time to better detail the textures of the lithologies hosting the
chromitite intervals. DDH BT-09-17 was re-examined in the summer of 2011 to
characterize the uppermost chromitite hosted in leucogabbro. From June 2011 to March
2012, 53 drill holes were logged in conjunction with infill drill programs performed by
Cliffs Natural Resources Inc. on the Black Label, Black Thor and Big Daddy chromite
deposits. Further textures of lithologies and mineralization were documented and
photographed to supplement the petrographic analysis. The petrographic investigation of
the lithologies was carried out in April/May 2011 and in the summer-fall of 2012.
Finally, textures of granodiorite and lamprophyres were investigated on a drill program
for the Black Horse chromitite for KWG/Bold Ventures Inc. in the spring of 2013.
Lithologies and chromitites in order of stratigraphy are as follows:

30
Hangingwall mafic metavolcanic
Gabbro-leucogabbro
Pyroxenite-olivine pyroxenite
Heterogeneous pyroxenite
Magmatic breccias
Massive chromite
Semi-massive chromite
Intermittent chromitite beds
Heavily disseminated chromite
Chromitite
Disseminated chromite
Oikocrystic harzburgite
Dunite-harzburgite
Footwall granodiorite

The characteristics of the lithologies from various drill holes that represent the
three deposits are described below. The thin section descriptions from the 4 drill holes
are supported by microprobe analyses. A list of all the drill holes with collar information
are in Table 3.1.

3.2 Footwall granodiorite
Granodiorite forms the footwall rock to the west of the Ring of Fire Intrusion.
The lithology is a massively textured, coarse-grained, quartz-rich hornblende
granodiorite. There is up to 30 modal % coarse 1 cm hornblende or finer biotite, about
20 modal % quartz and 40-50 modal % feldspar with equal proportions of plagioclase and
orthoclase (Fig. 3.5). The feldspars form tabular crystals up to 1 cm in size. Pink
granodiorite commonly grades into more salt and pepper quartz diorite. This phase
comprises 20 % quartz, 40 % feldspar and 30 % biotite or hornblende. Rounded quartz to
tabular feldspar phenocrysts are up to 0.7 cm, sheafy interstitial hornblende is up to 1 cm
sized crystals.

As observed in DDH BT-09-62, the dunite at the contact with granodiorite is
highly silicified suggesting assimilation of silica at the contact with the intrusion. Close
examination of the granodiorite contact with the ultramafic intrusion demonstrates the
granodiorite is likely younger than the intrusion and not older basement gneiss. At the
Black Horse chromitite (DDH FNCB-13-031 at 412.50 m), 0.4 cm acicular actinolite

33
occurs as randomly oriented crystals in pyroxenite in contact with granodiorite.
Actinolite growth in the bordering pyroxenite suggest thermal metamorphism due to heat
from intruding granodiorite. Coarse rounded blue quartz crystals occur near the
granodiorite contact. These quartz crystals are similar to silicified ultramafic occurring
at the contact in DDH BT-09-62 at Black Label. The blue quartz may be a silica
overprint from the granodiorite intrusion, rather than an assimilation texture.

Notably, the western granodiorite typically exhibits a fresh, undeformed
equigranular texture in contrast to gneissic basement. Also, several small granodiorite
dikes have been observed cross-cutting the dunite in DDH FNCB-13-033. As seen in
DDH FNCB-13-031, FNCB-13-030 and FNCB-13-032, there is a bull quartz zone in a
shear zone bordered by biotite and then chlorite alteration into pyroxenite. This is
analogous to the occurrence of younger granodiorite along a major fault zone such as the
late post-tectonic stocks to the Destor Porcupine Fault Zone in the Abitibi Greenstone
Belt (Kishida, 1984). Biotite alteration of pyroxenite suggests potassic metasomatic
fluids from the granodiorite. Also, biotite xenoliths observed in the granodiorite (eg. at
514.33m in DDH FNCB-13-031) are possible assimilated basement TTG inclusions by
the granodiorite. Such xenoliths are probably similar to those observed in the quartz
monzonite diapir to the Koitelainen Intrusion in Finland (Fig. 2.9). For geochemistry, on
the CaO/(Na2O+K2O) vs. SiO2 plot from Feng and Kerrich (1992), a single granodiorite
sample from Azar (2010) plots in the field of the syntectonic tonalite-granodioritegranite-
quartz monzodiorite series (TGGM) of the Round Lake Batholith to the Larder
Lake Group in the Abitibi Greenstone Belt. These are in contrast to the older synvolcanic
TTG which have higher CaO/(Na2O+K2O) and SiO2 contents.

3.3 Dunite-harzburgite
At Black Thor and Black Label, dunite is composed of totally serpentinized
olivine. Serpentinization of the dunite results in: 1) a light green colour of a highly
weathered unit; 2) a variation of aqua green to dark green colour with foliated dark
blue/black iowaite vein alteration; 3) a uniform dark/black; 4) or a uniform apple green
colour (Lesher and Houle, 2011) – see figs. 3.6, 3.7). Ultra fine magnetite is ubiquitous
in the serpentine (Fig. 3.8). Notably, the primary meso to adcumulate textures are well
preserved. Fine to medium grained round cumulus olivines form massive cumulates

35
cross-cut by serpentine-carbonate veins and scattered magnetite veinlets. Often there is
very fine cumulus chromite interstitial to olivine forming “olivine-chromite
heteradcumulate.” Interstitial magnetite occurs as a result of replacement of primary
cumulus chromite in heteradcumulate and may signify chromite replacement to magnetite
during serpentinization.

With increasing orthopyroxene, the dunite becomes harzburgite. The harzburgite
is similarly serpentinized, characteristically dark grey to green in colour. Intercumulus
anhedral pyroxene envelopes the olivine, most commonly occurring as an olivine-rich
meso to orthocumulate. Compositionally the harzburgite zones from near total olivine to
an 85:15 olivine to pyroxene ratio. Often there is increasing metasomatic pyroxene after
the primary pyroxene which gives patchy replacement of olivine. This is evident by
textures of medium to coarse patchy encroachment of pyroxene on protolith textures of
fine, often white talc-altered, round cumulus olivines in holes BT-11-197 and FW-11-87
(Figs. 3.9, 3.10 and 3.11). This leads to the talc/tremolite replacement on the rinds of
olivine observed in sample 486234 at 183.4 m in DDH BT-09-31. Notably, metasomatic
pyroxene was probed and results are presented by the mineral chemistry of pyroxene in
the geochemistry chapter.

3.4 Oikocrystic harzburgite
Oikocrystic harzburgite occurs above the main dunite sequence and below the
chromitites of the Black Label deposit and occasionally within the Black Thor sequence.
Serpentinized, fine cumulus olivine is surrounded by coarse, up to 1.5 cm diameter,
pyroxene oikocrysts that account for 35 modal % of the rock (Fig. 3.12). Oikocrystic
harzburgite often occurs in dunite-peridotite sequences above previous pyroxenite, such
as in DDH FW-09-34. The occurrence of common intercumulus minerals suggests the
presence of larger amounts of pore liquid material surrounding the cumulus olivine.
Jackson (1961), in his observation of the Stillwater Intrusion in Wager and Brown
(1967), noted that in areas where the amount of pore material was greatest, there was a
higher rate of crystal accumulation in the basin. Therefore, the intercumulus textures
must have formed in a more dynamic system which suggests the Black Label
harzburgites and chromitites formed under faster rates of crystallization. Like dunite, the
oikocrystic harzburgite occasionally contains interstitial very fine cumulus chromite.

38
In thin section, the serpentinized olivine is enveloped by talcose and tremolitized,
replaced pyroxene. Incipient to pervasive replacement by highly birefringent tremolite
occurs along the cleavage planes of the pyroxenes (Fig. 3.13). Electron microprobe
analysis of the tremolite shows Cr-bearing tremolite and non Cr-bearing tremolite. The
rarer Cr-bearing tremolites indicate chromite replacement to magnetite during hydration
supplied Cr content to the enveloping orthopyroxene. The few primary olivines,
pleochroic brown orthopyroxenes and igneous amphiboles microprobed have grains
yielding Fo #s of 83-90 for cumulus olivine and Mg #s of 0.87-0.99 for cumulus
orthopyroxene (Fig. 3.14).

3.5 Disseminated chromite
In the chromite mineralized dunite, fine grained cumulus olivine is bordered by
very fine, interstitial, cumulus chromite (Fig. 3.15). There is typically 5 to 10 modal %
disseminated chromite that occurs as interstitial chromite and thin bands. Up to 15 modal
% light grey intercumulus pyroxene accompanies the olivine. The interstitial chromite
often concentrates to form mm-scale layers. In thin section, minute equant intercumulus
chromites rim larger serpentinized cumulus olivine, thereby showing that it is second to
crystallize after olivine (Fig. 3.16). Intercumulus chromite is ofter associated with and
altered to brown platy chlorite grains after orthopyroxene (Fig. 3.17). Only rarely is
chromite included in olivine. The interstitial chromite is included within intercumulus
pyroxene indicating chromite crystallization before pyroxene (Fig. 3.18). The concentric
growth of fine cumulus chromite around olivine clearly demonstrates crystallization next
after olivine prior the pyroxene. Pyroxene crystallized as oikocrysts around the chromite
that rims the olivine. The order of crystallization for both dunite and oikocrystic
harzburgite is: cumulus olivine . cumulus chromite . intercumulus orthopyroxene.

Some of the intercumulus orthopyroxene has been hydrated to chlorite. This
chlorite has been confirmed by electron microprobe to be either chromian chlorite or
kaemmererite (for Cr2O3 of over 7 wt. %; Fig. 3.19). Orthopyroxene has also been
hydrated to talc as many of the olivines are surrounded by talc rims and then chromite
(Fig. 3.20). The talc was originally primary intercumulus pyroxene.

43
3.6 Chromitite
3.6.1 Heavily disseminated chromite
As with weak disseminated chromite described above, heavily disseminated
chromite also occurs interstitial to cumulus olivine. Heavily disseminated chromite
accounts for 25 to 40 modal %. At basal contacts with the massive chromitite there is
usually an increase in chromite to 50 modal %. The interstitial chromite is either
disseminated or weakly layered/foliated. The host generally is harzburgite with cumulus
olivines within intercumulus pyroxene. Intercumulus pyroxene minerals is darker grey
and commonly metasomatically replaces the cumulus olivine in patches throughout the
unit (Figs. 3.9 to 3.11). The olivine and pyroxene is pervasively serpentinized,
tremolitized and replaced by talc. Talc after the intercumulus pyroxene continues to
replace olivine until olivine is completely ghostly-grey talc-altered. The presence of talc
suggests there were CO2 fluids involved in the hydration of the pyroxene.

3.6.2 Intermittent chromitite beds
Intermittent chromitite beds generally, but not always, occur between
disseminated and semi-massive to massive chromite sequences. These beds range from
10 to up to 30 cm in thickness. Intermittent silicate layers form up to 50 cm to 1 m
intervals of dunite, or pyroxenite, often with disseminated chromite. Disseminated
chromite in intervening silicate layers generally contain 25 to 30 modal % chromite.
Hole DDH BT-10-128 intersected large-scale, 3 m thick, massively textured intermittent
chromitite beds separated by metre-scale sections of pyroxenite. These beds have
contacts and internal bands that well display primary igneous layering. The igneous
layers are later deformed, however, the primary layering often does not reflect the
foliation and plunge of the chromite ore shoots. The chromite textures are well
preserved, in contrast to the silicate lithologies. Chromite is not easily replaced, is denser
and more resistant to alteration than the surrounding olivines and pyroxenes.

As well displayed in DDH BT-08-10, the intermittent beds often have sharp basal
and grade upward into dunite. Excellent top directions are defined by sharp basal
massive chromitite contacts against cumulate dunite hosting minor intercumulus chromite
(Fig. 3.21). Upward increasing nodular olivine concentrates until cumulus olivine forms
dunite with diminishing intercumulus chromite, followed by another knife sharp contact

45
at the base of overlying massive chromitite (Fig. 3.22). The beds of sharp lower massive
chromite grading upward into interstitial chromite with increasing cumulus olivine are a
result of the settling of chromite layers (Kaçira, 1971). Higher up in the section, there are
cumulus contacts below the lower and above the upper contacts of the chromite layers
indicating a change in the order of crystallization from olivine back into chromite. Then
higher up, the beds are reversely graded with coarser cumulus olivine grading up to fine
interstitial chromite with sharp lower contacts of the chromite with the next cycle. This
demonstrates dominant crystallization in the olivine field followed by chromite.
Intermittent chromitite beds also show crystallization of cumulus chromite plus pyroxene
where pyroxene is the dominant host silicate before the overlying chromitite interval. An
example would be the layered beds with cumulus pyroxene in DDH BT-09-17 (Fig.
3.23).

3.6.3 Semi-massive chromite
Semi-massive chromite is olivine or pyroxene cumulate with 45 to 70 modal %
chromite (Fig. 3.24). Interstitial very fine cumulus chromite is disseminated within
cumulus olivine and/or pyroxene or as groundmass to dispersed cumulus olivine and/or
pyroxene. Layering is common, with up to 5 cm wide chromite bands. Disseminated
chromite grades to heavily disseminated to semi-massive, and finally to massive
chromite. There is no general pattern as to the location of the various types of chromitite.

An excellent example of semi-massive chromite in thin section is the Black Label
chromitite of BT-09-31. This chromitite has high silicate content, the chromite occurs in
chain-like textures interstitial to serpentinized olivine (Fig. 3.25). These chromites
contain more silicate inclusions, atoll textures, which are swiss cheese-like holes in the
chromite containing silicate (Fig. 3.26). The silicate inclusions at 155 m depth have the
same cleavage plane orientations as the surrounding tremolite, suggesting the chromites
underwent subsequent growth or annealing around the host silicate. Annealing/sintering
is a reequilibration of chromite around silicate melt has been postulated for the origin of
the swiss cheese-like textures in the Bushveld chromites (Hulbert and Von Gruenewaldt,
1985). These silicate inclusions have been investigated by detailed microprobe analyses.
They are of serpentine or tremolite composition, sometimes with the occurrence of both
mineral inclusions in one chromite grain. In some cases, either single chromites, or a few

48
fine chromites grown concentrically together, appear to partially envelop silicate from the
host rock (Figs. 3.27 and 3.28). The incomplete growth of chromite around the silicate
shows that the chromite primarily crystallized in equilibrium with the surrounding silicate

i.e. the olivine dunite. In some cases, the sintering would occur after cumulus olivinepyroxene-
chromite segregation as some of the chromites envelop both serpentine (after
olivine) and tremolite (after pyroxene).
The investigation of silicate inclusions demonstrates a larger range in mineral
species than has been reported in other chromites in the world. In addition to serpentine
and tremolite there are inclusions of Na-Ca amphibole, Ca amphibole, K and Naphlogopite,
chromian diopside, Ni sulphide and even albite. The silicate inclusions often
have unique compositions, as in the case of Na-phlogopite and albite, and are often
different than the cumulus minerals (Fig. 3.29). A single inclusion can contain igneous
amphibole (edenite) that displays retrogressive zoning to tremolite, along with the
occurrence of albite and phlogopite (Fig. 3.30). The suite of minerals constitute melt
inclusions that show a unique crystallization environment within the inclusion. In some
cases, however, amphibole such as pargasite can occur both within host cumulates and
within silicate inclusions in the chromite. Sample 486163 at 155 m in DDH BT-09-31
shows relic igneous amphibole in cumulate hosting chromite with silicate inclusions of
the same igneous amphibole composition (Figs. 3.31 and 3.32). Chromite probably
encapsulated residual melt that crystallized at lower temperatures. Phlogopite analysed in
the host cumulates is less Na-bearing than phlogopite in the silicate inclusions. Some
textures suggest phlogopite was also incorporated by the growing chromite rather than
being crystallized from fluids post entrapment. Sample 486353 at 260.6 m in DDH BT09-
31 shows chromite growing around a phlogopite grain (Fig. 3.33). Chromite in
association with igneous amphibole and phlogopite is found in other stratiform intrusions
such as the Stillwater Complex (Page and Zientek, 1987). In sample 486352 at 260.2 m
in DDH BT-09-31, there is the common association of chromite with surrounding
phlogopite (Fig. 3.34).

The silicate inclusions generally form large spheres within most chromite grains.
Silicate inclusions of different composition can inhabit growth planes in larger chromites.
The size of these central “swiss cheese” inclusions and also nature of growth within the

53
chromite suggests they were intimately encapsulated as melt while chromite was
growing. Chromite encapsulates amphibole, serpentinized olivine and tremolitized
pyroxenes by sintering. The melt responsible for the inclusions was residual within the
crystal mushes. There are often fractures around the inclusions and entry points where
melt was encapsulated in chromite. Negative crystal outlines of the inclusions reflect the
cubic symmetry of the host chromite. There was probably also the later H2O
autohydration inclusions. More details in the discussion of the silicate inclusions are
provided in chapter 6.

3.6.4 Massive chromite
Massive chromitite is composed of mesocumulus to adcumulus fine grained
granular chromite with minor intercumulus tremolite after pyroxene. At Black Thor, the
lower chromitites, between dunite and olivine pyroxenite, are the highest grade with over
90 modal % chromite and contain fewer oikocrystic pyroxene (Fig. 3.35). The Big
Daddy chromitite is similarly high grade as Black Thor (Fig. 3.36). Chromitites with
more intercumulus pyroxene show textures of lighter coloured/less dense chromite-
bearing intercumulus pyroxene patches in a darker/more dense chromitite adcumulate
(Fig. 3.37). The oikocrysts usually occur as large 1.5 to 5 cm wide patches of white to
grey depending on the concentration of included chromite. In some chromitites, there are
occasional chicken track textures of intercumulus pyroxene networks lacing the chromite
(Fig. 3.38). In thin section, the lighter coloured areas of the intercumulus pyroxene in the
massive chromite is characterized by birefringent tremolite after pyroxene. The darker
areas contain lesser altered tremolitized pyroxene (Fig. 3.39). Clinochlore, is locally
observed as a minor hydration product of original orthopyroxene (Fig. 3.40). Chromian
clinochlore preferentially occurs where there has been brittle failure of original chromite
(Fig. 3.41).

The Black Label chromitites are more heterogeneous than the Black Thor
chromitites and contain wavy, lensoidal and magmatic breccia textures indicating a
dynamic depositional environment (Fig. 3.42). Within the chromitites, the lighter areas
often appear as single cleaved oikocrysts overgrowing cumulus aggregates of olivine and
pyroxene. The lower Black Label (Layer 1) chromitite contains up to 15-20 modal %
oikocrystic pyroxene and cumulus olivine content, identifying host pyroxene-oikocrystic

58
cumulus olivine harzburgite. Not all pyroxene is oikocryst, some occurs as large
amoeboid patches in both Black Label and Black Thor chromitite. Some of the massive
chromitites also contain interstitial carbonate after pyroxene which is probably magnesite
(Fig. 3.43).

Often massive chromitites contain round aggregates of either olivine or pyroxene
(Fig. 3.44). Pyroxene aggregates in the chromitites appear medium grey whereas
cumulus aggregates of olivine appear white. The pyroxene hosts disseminated cumulus
chromite whereas the olivine does not. The silicate aggregates commonly form singular
“beaded” to composite layers, signifying primary magmatic layering.(Fig. 3.45).

Other features of massive chromitite include common deformation fabrics, rare
hematite alteration and a variety of veins. Foliations commonly overprint the primary
magmatic fabrics near faulted contacts (Fig. 3.46). In thin section, deformation is often
represented in the incipient fracturing of adcumulus chromite that may be a result of
compaction (Fig. 3.47). Chromitites are often wholesale hematite-altered as seen by the
red-brown colouration of the ores (Fig. 3.44). Thin talc-carbonate-serpentine veinlets are
often scattered within chromitites due to volume expansion related to serpentinization.
Some of the veins have kaemmererite on the fracture coatings, which is a chromian
chlorite alteration of the chromite (Fig. 3.19).

3.7 Magmatic Breccia
A few drill holes at Black Label intersect magmatic breccia developed after
crystallization of chromitite. In DDH BT-11-176, the magmatic breccia occurs after the
Layer 2 massive chromitite in the transition from oikocrystic harzburgite to dunite.
Magmatic breccia consists of rounded up to 6 cm fragments of dunite in a lighter
coloured pyroxenite and olivine matrix. Proportion of clasts to matrix is 70:30 or higher
with variable clast size. This unit is chromite mineralized with occasional up to 5 cm
massive chromitite clasts (Figure 3.48). This unit is also occasionally sulphide
mineralized with interstitial pyrrhotite-pentlandite-chalcopyrite, disseminations and
veinlets ranging from 0.5 to up to 8 modal % (Fig. 3.49).

In DDH BT-11-179, magmatic breccia occurs after the Layer 1 massive
chromitite in the transition from oikocrystic harzburgite to heterogeneous pyroxenite.
The fragments are dominantly fine grained cumulus olivine with intercumulus pyroxene.

63
The host is serpentinized pyroxene-oikocrystic harzburgite and individual oikocrysts
range up to 2 cm in size. From 290.40 to 290.70 m, there is coarse wispy pentlandite in
serpentinized dunite. Light grey pyroxenite occurs from 297.10 to 298.62 m. Then there
is oikocrystic magmatic breccia with more intercumulus pyroxene content and finer
olivine clasts to 306 m. Patchy chromite is disseminated in this section ranging up to 8
Cr % in a few 1.5 m intervals.

3.8 Heterogeneous pyroxenite
Heterogeneous pyroxenite is dark green and light grey-coloured and ranges from
olivine orthopyroxenite to harzburgite that consists of 50:50 dark olivine to light grey
orthopyroxene (Fig. 3.50). Olivine forms fine to medium grained cumulus aggregates in
diffuse patches up to 1 cm in size. Orthopyroxene occurs as light grey, up to 3 mm,
sheafy cumulus minerals that have been tremolitized. The patchy association of
pyroxene with olivine has been interpreted by Lesher (pers. communication, 2011), to be
the result of replacement of primary olivine by a pyroxenitic magma. Like the textures of
dunite-harzburgite, there is coarse patchy encroachment of pyroxene on fine cumulus
olivine.

Occasionally cumulus olivine occurs as filter pressed layers within a pyroxene
groundmass that may show a fabric orientation (Fig. 3.51). This filter pressed layering is
probably formed as pyroxene melt was pressed out leaving behind thin compact olivine
layers. Evidence of this being a form of compaction is the common occurrence of this
layered olivine pyroxenite at the upper contacts of chromitites below major pyroxenite
sequences, before the units grade into pyroxenite. The new pulse of pyroxenite would
press the underlying olivine into layers within the unit.

3.9 Pyroxenite-olivine pyroxenite
Pyroxenites above the main chromitite zones are light grey medium to coarse
grained massive units composed of sheafy to tabular, cumulus pyroxene (Fig. 3.52). The
units locally have a cumulus olivine content ranging from 10 to up to 35 modal %. In areas
where olivine pyroxenite is present, the crystallization sequence is dunite . chromitite •
olivine pyroxenite . pyroxenite. Otherwise crystallization is dunite . chromitite •
pyroxenite.

66
The pyroxenites have a variety of textures. Medium grained pyroxenite is
commonly comprised of orthopyroxene. Occasionally, bronzite primocrysts make up
segments of FW-12-108 (Fig. 3.53). Medium grey pyroxenite is mostly composed of
light grey tremolitized pyroxene. Wholesale replacement by green radial fibrous
tremolite can eradicate original pyroxene. In the bronzitite of FW-12-108, the
tremolitization of pyroxenes is displayed by minor veinlets (Fig. 3.53). Coarse grained
pyroxenite is commonly foliated and altered to talc. Large sections of the coarse grained
talcose pyroxenite has pink hematite alteration. Rather commonly large 1.5 cm, rounded
poikilitic pyroxene megacrysts enclose medium grained pyroxene. Poikilitic pyroxene
accounts for 8 to 15 modal % of the composition and are identified by a darker,
somewhat ghostly appearance.

Near the contacts with overlying leucogabbro, the pyroxenite is mylonitized and
distinguished from the leucogabbro in that it is more greenish in colour contains no
feldspar content. Leucogabbro, in contrast, is grey in colour with feldspar. It is unclear if
the pyroxenes in pyroxenite occur in a cumulus fabric as similar textures have been
reported in Pykes Hill komatiitic pyroxenites which could have a metasomatic origin
(Lesher, pers. communication 2011). Under thin section, pyroxenite comprises tabular,
anhedral, haphazardly oriented pyroxene that has been pervasively talcose-altered and
incipiently tremolitized (Fig. 3.54). Tremolite usually occurs along the cleavage planes
of pyroxene minerals that has been pseudomorphed by fine masses of talc. The
pyroxenites are usually devoid of interstitial chromite and cap the chromitite sequences.

Although they cap the sequences, it is still argued that the pyroxenite is related to
chromite mineralization. In DDH BT-10-17, pyroxenite above the first chromite
sequence (above the initial dunite) and the pyroxenite in pyroxenite-chromitite-dunite
cycles higher up in stratigraphy contain wispy interstitial and bands of chromite grading
up to cumulus pyroxene in some of the cycles (Fig. 3.55). In thin section, the chromite in
pyroxenite occurs in a vermicular habit and is retrogressed at the margins in contrast to
regular euhedral chromite (Fig. 3.56). This is similar to the vermicular habit of
pyroxenite-bearing chromites in ophiolites (Matsumoto and Arai, 2001). The gradation
of chromite to pyroxene probably indicates the pyroxenes are cumulus within these
chromitite zones. The occurrence of chromite mineralization with pyroxenite above the

69
dunite is probably indicative of chromite mineralizing with a pulse of pyroxenite. The
occurrence of chromitite above the pyroxenite can be explained by additions of new
pulses of dunite overlying the pyroxenite. All this is more akin to a mixture of magmas
involved with mineralization as proposed by Irvine (1977) and Irvine et al. (1983). In
thin section, the chromites in the pyroxenites, although inferred to be cumulus, do not
display igneous textures since the minerals have been obliterated at the edges and within
the grains by replacement pyroxene.

There are sometimes green, aphanitic chloritized to talc-altered aphyric layers
within the pyroxenite. Often these layers are found near the tops of the pyroxenites
proximal to the leucogabbro, but have also been found within the pyroxenite sequences.
The interlayers mostly have a green aphanitic chloritized groundmass that may contain a
few plagioclase phenocrysts in clumps (Fig. 3.57). These layers have been interpreted to
be komatiite by Lesher, C.M. (pers. communication, 2011). Sometimes there are
plagioclase phenocrysts in the layers as shown by white, up to 0.5cm wide augen to oval
shaped aggregates foliated in the pyroxenites at the tops of massive pyroxenite
sequences. Weathering of the feldspars leaves behind vesicles in an orange weathered
and talcose altered interlayer. Examples of these drill holes include DDH FW-12-93, -94,
-97, -106, and -112.

Another examination of these green aphyric units shows that they are products of
the hornfelsing of lamprophyre dikes against pyroxenite. In DDH FNCB-13-032, there is
an abundance of these units in a pyroxenite interval from 667 to 672 m depth in the hole.
Ultramafic-mafic dikes are described as consisting of light aqua-green, aphyric, aphanitic
chlorite with sharp margins with pyroxenite. In larger dike sets, there is first green
chlorite at the contact with pyroxenite and dark brown very fine grained biotite alteration
in the interiors of the dikes. Then inner from the biotite zone is a fresh textured
amphibole-feldspar fine grained lamprophyre dike. So zoning is from pyroxenite . talc
phyllonite pyroxenite . sharp contact . green chlorite . brown biotite . amphibolefeldspar
mafic dike to . brown biotite . green chlorite . sharp contact . talc
phyllonite pyroxenite . pyroxenite. The green chlorite-biotite seen in these units is
therefore the thermal aureole of a lamprophyre dike on the pyroxenite.

70
3.10 Gabbro-Leucogabbro
In DDH BT-09-17, there is biotite gabbro cross-cutting the chromitite in the upper
parts of the Black Thor deposit. The unit is a salt and pepper textured, medium- to
coarse-grained, massive gabbro that contains dominant white cumulus plagioclase and
lesser green rounded up to 5 mm cumulus tremolite after early crystallizing
orthopyroxene (Fig. 3.58). The green tremolites are in turn rimmed by and occur in
association with finer tabular to needly brown biotite after late igneous amphibole. In
thin section, the tremolites have high birefringence, two oblique cleavages and sometimes
have a radial fibrous habit. The tremolites are surrounded by tabular, brown pleochroic
biotite (Fig. 3.59). The plagioclase crystals occur as colourless twinned tabular crystals
with cloudy sausserite alteration and overprinted by blue epidote, zoisite and albite
alteration after primary plagioclase. Titanite and hexagonal to columnar apatite are
accessory (Fig. 3.60). There appears to be a zonation from brown primary biotite to
sericite on the margins to the central green tremolite. The tremolites contain centres of
dark green lamellae that are remnants to be from titanium of primary pargasitic
hornblende (Fig. 3.61). There is accessory magnetite.

The rock may be called leuconorite since there are a few occurrences of coarse
cumulus bronzite. The tremolite:biotite:plagioclase ratio is dominantly 40:30:30 and
ranges to 00:20:80 leucogabbro. The unit contains the coarsest bronzite orthopyroxene
with finer tremolite at the base of the sequence at 299 m depth. Upward, there is more
fine grained brown biotite in association with coarse green tremolite. Plagioclase
increases up to 80 modal % by 309.80 m and then the rock is finer grained tremolitedominant
with plagioclase at 30 modal %. Unlike the ultramafic layered series the
gabbro roof appears relatively fresh and unaltered. There is approximately 1-2 modal %
pyrrhotite + pyrite + chalcopyrite. The chromitites that are cross-cut by the gabbro are
massive and contain sharp contacts with the gabbro.

Leucogabbro is a massive light grey feldspar and quartz-phyric plagioclaseorthopyroxene
cumulate overlying the pyroxenite that dominates the upper differentiated
lithologies of the intrusion (Fig. 3.62). The contact of leucogabbro with pyroxenite is
often faulted with either a mylonite as in DDH FW-11-83 or a hematized fault breccia as
in DDH BT-11-185. In other drillholes such as DDH FW-11-87, the contact between

74
leucogabbro and pyroxenite is marked by the disappearance of feldspar in the pyroxenite,
but having a gradation from the pyroxenite to leucogabbro in terms of the same
tremolitized cumulus pyroxene.

The leucogabbro above the pyroxenite in DDH BT-11-185 begins with a fine to
medium grained dark vs. light pyroxene gabbro or gabbro which lacks the medium to
coarse feldspar. After the basal gabbro, there is leucogabbro with a feldspar content of
30 modal % in proportion to surrounding darker green tremolitized pyroxene. This is
followed by a coarse silicified section of feldspar and quartz veins in pyroxene from 47 to
40 m in that hole. From 43.26 to 37 m, the leucogabbro contains veiny to patchy coarser
grained feldspar-quartz silicification. From 37 to 31.53 m, there is leucogabbro with a

75:35 pyroxene to feldspar composition. Porphyritic feldspars are up to 0.5 cm wide
grains. This section continues to 29 m depth in that hole. Sometimes pink feldspar is
observed making the unit locally granophyric.
3.11 Hangingwall mafic metavolcanic
Mafic volcanic occurs when the leucogabbro loses its feldspar, becomes very fine
grained grading into mafic volcanic lithology. The appearance of a gradational contact
supports the idea that the gabbro is melted roof rock rather than being a differentiate of
the ultramafic intrusion. The gradation of gabbro into mafic volcanic could be due to
assimilation of wallrock mafic volcanic by gabbro. In DDH BT-11-200, the mafic
volcanic is first medium grey like the groundmass of the gabbro, but progressively
becomes darker green-grey chloritized down the hole. From 656.82 to 660.15 m, the unit
is a true dark green basalt with 12 modal % clotty pyrrhotite mineralization. From

660.15 to the end of the hole at 684 m, the basalt is light green-grey chloritized with
quartz banding, coarse quartz veins and interlayers of pegmatitic leucogabbro. In DDH
BT-11-194, the metabasalt is green chloritized and aphanitic with Cross-cutting pink
feldspar veins. From 678 to 684 m in DDH BT-11-200, the volcanic is recrystallized
with medium grained feldspar at a composition of 60:40 chlorite to feldspar.

75
CHAPTER 4
GEOCHEMISTRY

4.1 Introduction
The geochemistry of the McFaulds Lake Intrusion is presented as whole rock
geochemistry of major oxides, analyses of major element variation in previous assays,
trace element geochemistry, full spectrum PGE analysis of host rock and chromite and
electron microprobe mineral chemical analysis of silicates. Trace element and rare earth
element analyses were performed on the same representative whole rocks reported for the
three chromite deposits. Results are listed in Appendix 3.

4.2 Whole rock geochemistry
Whole rock geochemical analysis was carried out on 26 drill core samples from
four drill holes that represent the three deposits: DDH FW-08-19 for Big Daddy; BT-0810
for Black Thor; and BT-09-31 for Black Label. Two of the samples were collected
from DDH BT-09-17 to represent the upper gabbro at Black Thor. Previous bulk rock
geochemistry reported by Spider-KWG-Freewest and Freewest databases have been
examined and interpreted along with this data. Full results are listed in Appendix 3.
Discussion of bulk rock geochemical trends is for major element oxide and trace
element/REE.

4.2.1.1 Major oxides
The lithologies analysed for major oxides include dunite, oikocrystic harzburgite,
heterogeneous olivine pyroxenite, pyroxenite and gabbro. Results are displayed in Table

4.1.
The Black Label dunite is the most primitive of the intrusion with an MgO
content of 41 to 45 wt. % MgO. The Black Thor dunites is also primitive with 40 to 41
wt. % MgO. The Big Daddy dunite is more evolved with 36 to 41 wt. % MgO. The
evolution in the Big Daddy dunites is likely due to differentiation as there was a greater

77
subset sampled in that drill hole. The dunites show degrees of crustal contamination, as
evidenced by a source magma chemistry with high Cs, Ba and Rb contents. Notably, the
dunites from the Big Daddy suite are located more proximal to the basement tonalite. All
the dunites of the three deposits have low wt. % CaO and Al2O3 due to lack of pyroxene
crystallization. Notably, the wt. % FeO contents is more elevated in the dunite than
pyroxenite due to higher Fe in olivine.

The pyroxenites are distinctly more evolved than the dunites with 26 to 40 wt. %
MgO. The Black Thor pyroxenites are the most primitive with 30 to 40 wt. % MgO. The
more primitive pyroxenite combined with the primitive dunite at Black Thor makes this
the most primitive of the three deposits. In contrast, the Black Label pyroxenite sample
is much more evolved at 27 wt. % MgO. The Big Daddy pyroxenite is generally more
evolved like Black Label. Although, there are more evolved pyroxenites in Big Daddy,
the trace element geochemistry of the Big Daddy pyroxenites suggests they have a
primitive source like that at Black Thor. Therefore, although there is more contamination
in the Big Daddy suite, overall, the setting of the Big Daddy is more primitive and more
like Black Thor than Black Label in terms of geochemistry of the pyroxenite.

Transitional lithologies like heterogeneous olivine pyroxenite and oikocrystic
harzburgite are local to the Big Daddy and Black Label suites respectively.
Heterogeneous pyroxenite does not just occur at Big Daddy, but in the other deposits as
well. The sample selected from Big Daddy is representative of the transitional chemistry
between dunite and pyroxenite. As will be observed in the major element trends of Big
Daddy, the heterogeneous pyroxenite probably formed as a result of uptake of olivine in
pyroxenite from the lower dunite followed by the replacement of olivine by pyroxene in
these samples. The MgO content of the heterogeneous pyroxenite is at 38 wt. % and
contains more pyroxene with higher Al2O3 content at 2.0 wt. % and SiO2 content at 44
wt. %.

Oikocrystic harzburgite, an olivine cumulate with poikilitic pyroxene that is
transitional from the dunite to pyroxenite in Black Label, has 33 to 39 wt. % MgO.
Pyroxene is evident by the elevated Al2O3 and CaO contents of 4.9 and 9.0 wt. %
respectively. Although there is higher CaO content, this probably reflects the
tremolitization of primary orthopyroxene. Relic pyroxenes have parallel extinction

78
diagnostic of orthopyroxene. The Ca content of tremolite is derived from CO2 fluid
metasomatism

The two samples of gabbro proximal to the upper chromitite at Black Thor are
much more evolved than the other samples due to modal plagioclase. SiO2 contents vary
between 51 and 53 wt. % and Al2O3 contents vary between 16 to 18 wt. %.

4.2.1.2 Up section major oxide variation
4.2.1.2.1 Black Label: DDH BT-09-31
Geochemical trends in major oxide variation are best represented by the major
element plots based on reported assays for the three drill holes. A stratigraphic column of
lithologies is presented for each drill hole for all the following variation plots. The
legend for the lithologies is the same as that presented on the drill sections of the holes
(Figs. 3.1 to 3.4). Major element variation is demonstrated for the lithologies bordering
the chromitites of the three deposits. The Black Label interval begins at a depth of about
150 m (Figs. 4.1 to 4.3). From 150 to 164.70 m, there is elevated Mg % in heterogeneous
olivine pyroxenite. Then from 164.70 to 203.50 m, there is the main chromitite interval
composed of clasts of oikocrystic pyroxenite as wavy bands in a semi-massive
chromitite. There are various replenishments of chromitite in this interval as indicated by
peaks in Mg % content. Fe % varies inversely in the chromitite as it substitutes with Mg
%. After 203.50 m, there is pyroxenite that contains decreased Mg % while increased Ca
% and Al % content. The next interval begins at 228 m. From 228 to 237 m, there is
oikocrystic harzburgite with generally high Mg % content due to dominance of cumulus
olivine. Within this unit, Mg % decreases with height probably due to differentiation. Ca
and Al % contents are intermediate since there is both olivine and pyroxene in the unit.
From 237 to 270 m, there are intermittent chromitite beds with replenishments as
evidenced by peaks in Mg % and Fe % content. Al % is elevated as it varies with Cr
content. After 270 m, there is dunite that is characterized by decreased Al % and
increased Mg % content. The last interval from 306 to 320m intersects the last beds of
chromite within a dominant dunite sequence. Fe and Al % contents are elevated in
association with Cr content.

81
4.2.1.2.2 Black Thor: DDH BT-08-10 & BT-09-17
The major oxide variation across Black Thor is shown for DDH BT-08-10,
beginning with dunite at 94 m depth (Figs. 4.4 to 4.6). From 94 to 124.70 m, there is
general decreasing Mg % and Fe % with depth indicative of a differentiating dunite
pulse. From 124.70 to 168.20 m, there are various intermittent to semi-massive beds of
chromite alternating with cumulus olivine dunite. Mg % increases in the areas of
cumulus olivine and is lower in content within the chromite beds. Fe % peaks in these
chromite beds is due to more silicate exchange in disseminated chromite as opposed to
massive chromitite. From 155 to about 160 m, there is a trend of decreasing Mg %
indicative of magma evolution in a chromitite interval. Fe % is antipathetic to Mg % and
increases with substitution as the chromites become more evolved. Another Mg % and
Fe % trend occurs from 168.20 to 174.20 m, where there is a section of massive
chromitite with lower Mg % content. This shows a trend of decreasing Mg % and
increasing Fe % with depth in the chromite interval indicative of magma evolution in the
chromitite. Above the chromitite from 174.20 to 187.10 m, there is dunite showing a
large replenished increase in Mg % content. Al % generally increases directly with Cr
content within the drill hole sequence,.

Samples from DDH BT-09-17 are different than samples from the other drillholes
as chromitite is related to pyroxenite intruded by upper gabbro. The interval of interest
that contains the upper chromitite is from 290 to 345 m (Figs. 4.7 to 4.9). The interval
begins with a pyroxenite above the previous chromitite layer at 290 m. The pyroxenite
contains high Mg % but lower Al % and Ca % contents in comparison to the overlying
gabbro. From 296.30 to 298.80 m, there is the first chromitite horizon sandwiched
between pyroxenite and gabbro. The chromitite is dinstinguished by a peak in Fe % in
comparison to low Fe % in background pyroxenite and gabbro. Above the chromitite
there is gabbro with elevated Ca % and Al %. From 298.80 to 318.70 m, there is a trend
of decreasing Al % from 8.4 to 7.8 %. This represents evolution in anorthite content of
plagioclase to lower anorthite with height. A trough in Al % at 304 m coincided with
high Ca % which represents abundance of tremolitized pyroxene over plagioclase.
Higher up in the gabbro from 311 to 318.70 m, there is increased Ca % with the
fractionation of pyroxene is association with plagioclase. Notably, the wt. % SiO2 and

86
Na2O contents increase upward in this section with evolution of the gabbro, well
demonstrated by the increase in wt. % SiO2 and Na2O in the two gabbros analysed. The
increase in modal % pyroxene is also evident by increase in Mg % upward in the gabbro.
The main chromitite interval, from 318.70 to 337.90 m, is characterized by peaks in Fe
%. There appears to be a decreasing trend in Mg % in the first chromite pulse from

318.70 to 325 m which may be due to differentiation. However, in the above pulses there
is increased Mg %. The higher Mg % contents may be due to retrogression of the
chromites to higher Mg % along with higher Al % as there is reduction in Fe with heat of
the gabbro. Above the chromitite from 337.90 to 345 m, there is again pyroxenite with
high Mg % and low Ca and Al %.
4.2.1.2.3 Big Daddy: DDH FW-08-19
Big Daddy is represented by DDH FW-08-19. From 9 to 64.50 m, there are three
increases in Mg % that probably represent three replenishments of olivine cumulus
magma to form dunite that alternates with pyroxenite (Fig. 4.10 to 4.11). From 64.50 to
100 m, there appears to be a megapulse of dunite, as evident by an overall decreasing
trend in Mg %. Within this sequence are two pulses of decreasing Mg % with height
from dunite to pyroxenite. They are from 64.50 to 73.97m and 73.97 to 105.39 m. Two
replenishment trends of increased Mg wt. % occur in the interval of heterogeneous
olivine pyroxenite from 105.39 to 129 m and from 129 to 141.50 m. With increased Mg
%, there is generally elevated Fe % due to olivine content. From 141.50 to 144.14 m,
there is semi-massive chromite with cumulus pyroxene. From 144.14 to 159.37 m, there
is replenishment in Mg % with a dunite pulse. From 159.37 to 162.00 m, there is
massive chromitite characterized by no Si % along with Fe % and Al % peaks. There is
heterogeneous pyroxenite with elevated Mg %. from 162.00 to 164.20 m. From 164.20
to 183.00 m, there is a drop in Mg % in a new pyroxenite sequence. Notably, there is
increased Ca % in the pyroxenite due to presence of tremolite and also increased Al % as
Al substitutes into the pyroxene structure. From 183.00 to 229.64 m, there is the main
section of massive chromitite. Within this sequence, there is an overall decreasing trend
of Mg % while an increasing trend Fe % as Fe substitutes with Mg in the chromite
structure. The overall decreasing Mg % trend is due to evolution from bottom to top of

88
the chromite sequence. Although there are trends of Mg and Fe %, Al % stays relatively
constant at 6.5 wt. % Al. Above the chromitite is pyroxenite with elevated Ca %.

4.2.1.3 Binary major oxide variations
4.2.1.3.1 Black Label (Fig. 4.12)
The Black Label deposit displays variation to more evolved compositions, both in
more evolved chromite and more pyroxene in the system. On a Cr ppm vs. Mg % plot,
there is a general trend of decreasing Cr with increasing Mg %, reflective of more
cumulus chromite and less cumulus olivine. On a Cr ppm vs. Al % plot, there is a
convex upward trend of increasing Cr ppm with increasing Al % content. Again, with
increased Cr, there is increased Al with substitution. The leveling off at the high Cr end
of the plot is due to the effect of interstitial poikilitic pyroxene providing chromitite more
exchange with higher aluminous compositions.

For Cr ppm vs. Fe %, there is a large spread of values over a general increasing
Cr with increasing Fe % trend. There is increased Fe % with increased chromite content
as before. However, the large spread in compositions is due to the increase in the amount
of ferrichromite in the Black Label deposits as opposed to the other deposits. Since
ferrichromite is non-igneous, there is no general enrichment trend in its origin. Where
there is semi-massive chromite with interstitial silicate, there is greater amount of
enriched Fe-bearing ferrichromite due to silicate-oxide exchange during hydration.

Igneous evolution in the Black Label chromitite is displayed well by linear
negative correlative trends of decreasing Al and Fe % with Mg %. The decreases are due
to substitution with Cr and Mg respectively and the predominance of those elements in
more massive chromite-bearing vs. disseminated chromite-bearing cumulates.

There is no correlation on the Ca % vs. Mg % plot. There are however a large
amount of Ca-enriched lithologies on a broad range of Mg % due to tremolite in more
pyroxene-bearing lithologies. There is, in contrast, less pyroxene in the Big Daddy and
Black Thor intercepts. Notably, the pyroxenes were probably more affected by Ca
metasomatism during hydration to cause irregularity in the Ca signatures.

4.2.1.3.2 Black Thor (Fig. 4.13)
The Black Thor deposit shows more complete evolution in major element
variation between the less chromite-bearing disseminated and the more massive

91
chromite-bearing lithologies. On the Cr ppm vs. Mg % plot, there is a distinct negative
correlation of increasing Mg % with decreasing Cr ppm. This trend reflects the greater
Cr ppm in the more massive chromites vs. the more evolved disseminated chromites that
have undergone silicate exchange. The trend of decreasing Cr ppm with differentiation is
characteristic of chromite deposits of layered intrusions such as Bushveld (Stowe, 1994).
With increased evolution of the chromitite, there is increasing Al content as well due to
Cr-Al substitution in the individual chromites.

For Cr ppm vs. Fe %, there is also a trend of increasing Fe % with Cr ppm with
magma evolution in the chromitites – the more massive chromitites containing less Fe %
due to more primitive compositions. There is an increasing trend of Fe % in many of the
less Cr-bearing lithologies due to increased Fe % in the olivine of dunite. At the high Cr-
bearing end, there are also some high Fe-bearing chromitites or chromite-olivine
cumulates that plot off the trend. These are representative rims on primary chromites that
have been retrogressed leaving behind Cr-enriched and Fe-enriched ferrichromites on the
rims of the primary chromites.

The Al % vs. Mg % plot shows a distinct negative correlation of decreasing Al %
with increasing Mg %. This trend is also evident of the magma evolution in the
chromitites where the more massive chromitites have greater Al % than the more
primitive Mg-rich chromite-olivine cumulutes. This is again due to Cr-Al substitution,
the more chromite in the rock, the higher the Al content. Fe varies similarly with Mg as
it does with Cr, only in an inverse way. There is another evolutionary trend of the more
chromite-bearing lithologies containing more Fe % content. Again, some Mg-enriched
dunites contain elevated Fe within the olivine. Also, there is enrichment in Fe % at the
low Mg % end that goes above the trend due to enriched Fe in ferrichromite-bearing
chromitites.

The Ca % vs. Mg % plot, enrichment in Ca % shows no correlation. Enrichment
in Ca % is probably due to secondary tremolite replacement of pyroxene. Notably, there
are two outliers of high Ca-bearing lithologies which are intercumulus pyroxene-bearing
semi-massive chromitites.

A few binary trends are useful for analyzing the composition of the gabbro vs.
chromitite vs. pyroxenite in DDH BT-09-17. On a Al % vs. Mg % plot, igneous

92
evolution occurs with increasing Al % from pyroxenite to gabbro. The massive
chromitite plots with intermediate Al % and Mg % compositions between the gabbro and
pyroxenite. On a Ca % vs. Mg % plot, the gabbros plot at higher Ca % than the
pyroxenite due to plagioclase controlled fractionation. The relatively low Ca % of the
pyroxenite is indicative of predominant orthopyroxene fractionation.

4.2.1.3.3 Big Daddy (Fig. 4.14)
On binary variation plots, the Big Daddy deposit shows trends of magma
evolution from the most primitive dunite through to the heterogeneous olivine pyroxenite
to the chromitite and associated pyroxenite lithologies. Below the 2 % Cr mark on a Cr
ppm vs. Mg % plot, chromite increases slightly with increasing Mg % up to 21 % Mg.
Most of the data from the dunite plot in an area of chromite accumulation below a line of
increasing Cr with Mg %. However, with evolution of the units, there is also a large
negative correlation of Cr with Mg %. At the high Cr end of the trend, there is a cluster
representative of the samples in the massive chromitite interval. Between the massive
chromitite and the dominant cumulus olivine dunite lithologies are fewer intermediate
lithologies that contain intermediate (semi-massive) chromite with intermediate Mg
content between massive and disseminated chromite. This shows a direct negative
correlation of Cr with decreasing modal % chromite. The observation of there being high
Cr and low Cr-bearing clusters with few intermediate compositions shows the “it’s
massive or it’s not there at all” nature of the Big Daddy chromitite as seen in this drill
hole.

The Cr ppm vs. Al % plot shows a positive correlation of Cr ppm and Al %
content. Therefore, there will be more partitioning of Al into the spinel structure as
opposed to dunite that contains little Al %. Notably, the massive enriched chromitite
contains the highest Al % content. This is probably due to silicate exchange with the
surrounding dominant pyroxenite host lithology. The same correlation exists between Cr
ppm and Fe % as Fe % increases with evolution of the chromitites.

The Al % vs. Mg % plot shows Al % generally increases with decreasing Mg %
as there is more Al % in the chromitites than in the other lithologies. Pyroxenites with
lower Mg % content also have elevated Al % content due to Al substitution into
pyroxene. Fe % increase with decreasing Mg % content is not as obvious since many

94
samples contain more pyroxene which have lower Fe % contents. Generally, the more
chromite, the more Fe content due to its partitioning in the spinel structure.

The Ca % vs. Mg % plot identifies a broad increase of Ca % content in the more
evolved pyroxene-bearing lithologies as opposed to the dunites. The Ca is not admitted
into the spinel structure, so the olivine-chromite cumulus and massive chromite-bearing
lithologies have limited Ca % content.

4.2.2 Trace element geochemistry
4.2.2.1 Primitive mantle-normalized multielement plots
4.2.2.1.1 Black Label
The Black Label chromite deposit is hosted in the main dunite and pyroxenite
sequences stratigraphically lower than Black Thor. On a PM-normalized diagram, the
Black Label dunite is the most primitive with the lowest overall REE (Fig. 4.15). They
were probably the first units to crystallize among the host rocks to the three chromite
deposits. The dunites are enriched in light rare earth elements (LREE) relative to heavy
rare earth elements (HREE) and contain negative Nb-Ta, negative Zr-Hf, and positive Ti
anomalies. These collectively indicate crustal contamination of komatiite. For trends in
REE, the dunites and oikocrystic harzburgites show LREE enrichment over middle rare
earth elements (MREE) with (La/Sm)cn ratios between 1.94 and 4.70, MREE depletion
over HREE with (Gd/Yb)cn ratios of 0.68 to 1.05, and (Eu/Eu*)cn ratios of 0.41 to 1.50.
(La/Sm)cn ratios have an average ratio of 3.02 which is slightly larger than Big Daddy
and larger than Black Thor. The ratios are similar to Big Daddy, only the overall REE
are lower in the Black Label dunites.

LREE enrichment in Black Label identifies crustal contamination of an original
komatiite as such LREE and LILE enrichment is commonly linked to crustal
contamination (Lesher, 2005). LREE enrichment coinciding with negative Nb-Ta and
Zr-Hf anomalies is due to crustal contamination in komatiites by tonalite-tronjhemitegranodiorite
suites (Lesher, 2005 and Hollings & Kerrich, 1999). Low Al tonalities in
the North Caribou Terrane have been characterized by LREE enrichment and negative
Nb-Ta and Zr-Hf anomalies (Wyman et al., 2011). For the case of Black Label, the
LREE enrichment along with enrichment in Cs-Rb-Ba suggests greater degree of crustal
contamination in these dunites in contrast to Black Thor. Although the (La/Sm)cn ratios

96
are larger than Black Thor, the Black Label dunites are more primitive with lower
abundance in overall REE along with their signature MREE depletion characteristic of
primitive aluminum-undepleted komatiite (AUK).

Notably, the REE compositions of the oikocrystic harzburgite samples are
intermediate between Black Label dunite and Black Label pyroxenite (Fig. 4.15). The
origin of the oikocrystic pyroxene at the top of a dunite sequence is related to the
initiation of pyroxene crystallization, following the fractionation of pyroxene-laden
magma (pyroxenite) in this sequence. Intermittent beds of chromite have been found
associated with these wavy banded oikocrystic units and in DDH BT-11-176, oikocrystic
harzburgite units are found in association with the magmatic breccias. The dynamic
textures in these units indicate the chromite probably originated with a mixture of
pyroxene-laden magma to drive the magma into the chromite field for crystallization.
This mixing of pyroxene is suggested by the REE contents being intermediate that of
dunite and pyroxenite.

One sample of Black Label pyroxenite was analysed and shows a highly evolved
composition similar to the Big Daddy pyroxenite (Fig. 4.16). The sample displays LREE
and LILE content that is lower than that of Big Daddy, but higher than Black Thor. The
pyroxenite displays slight LREE enrichment relative to HREE and contains negative Nb-
Ta, negative Zr-Hf and negative Y anomalies suggestive of crustal contamination. There
is LREE enrichment over MREE with (La/Sm)cn of 1.59; MREE depletion over HREE
with (Gd/Yb)cn of 0.85, and the (Eu/Eu*)cn ratio is 0.57.

4.2.2.1.2 Black Thor
The Black Thor chromite deposit is hosted in main dunite with pyroxenite higher
in stratigraphy. On a PM-normalized diagram, the Black Thor dunites are enriched in
LREE relative to HREE and contain negative Nb-Ta, negative Zr-Hf, and positive Ti
anomalies (Fig. 4.17). The dunites display LREE enrichment over MREE with (La/Sm)cn
ratios between 1.68 and 2.11, MREE depletion over HREE with (Gd/Yb)cn ratios of 0.64
to 0.83, and (Eu/Eu*)cn ratios of 0.44 to 0.63. The (La/Sm)cn ratios are lesser than the Big
Daddy dunites and are depleted in MREE. The relative LREE non-enrichment is
probably reflective of primitive AUK komatiite (Lesher et al., 1999). HREE enrichment
over MREE is a characteristic signature of AUK komatiite or boninite (Lesher et al.,

98
1999, Kerrich, 1997 and Barnes, 1989). Like Big Daddy, the rocks show evidence of
crustal contamination by TTG with the negative Nb-Ta, Zr-Hf anomalies. However,
there is no local contamination as evidenced by depletion LILE of Cs-Rb-Ba, but
generally reflective of an AUK signature.

The Black Thor pyroxenites are depleted in overall REE compared to Big Daddy
and Black Label and are the most primitive pyroxenites (Fig. 4.16). These pyroxenites
are also enriched in LREE relative to HREE and contain negative Nb-Ta, negative Zr-Hf,
negative Y and positive Ti anomalies suggestive of crustally contaminated komatiite.
The pyroxenites display LREE enrichment over MREE with (La/Sm)cn ratios between

2.42 and 2.87, MREE depletion over HREE with (Gd/Yb)cn ratios of 0.28 to 0.70, and
(Eu/Eu*)cn ratios of 0.51 to 1.42. The MREE are strongly depleted relative to HREE
compared to Big Daddy which reflect that of HREE-enriched primitive AUK (Lesher et
al., 1999).
In Black Thor DDH BT-09-17, there is gabbro cross-cutting the chromitite and it
is located higher in stratigraphy than the pyroxenite. The gabbros are enriched in overall
trace elements and REE relative to the other lithologies due their more evolved
composition (Fig. 4.18). Although more enriched, the gabbros display similar REE
trends of LREE enrichment, negative Nb-Ta, Zr-Hf and Y anomalies as the other
lithologies which probably indicate they form an upper differentiate of the same layered
intrusion. The negative Nb-Ta along with negative Ti anomalies is related to TTG
contaminant. TTGs are considered to be formed by partial melting of hydrous basalt at
the base of a thickened oceanic island arc, leaving a rutile-bearing eclogitic residue
(Huang et al., 2012). The differences between the gabbros and the other lithologies are
that the gabbros do not have HREE enrichment and have negative Ti anomalies:
(La/Yb)cn ratios are 6.48 to 12.53 in contrast to an average (La/Yb)cn ratio of 3.60 in the
other lithologies. This shows that the gabbros are not komatiitic, but are rather melted
roof rocks after mafic volcanics. For REE ratios, the gabbros display LREE enrichment
over MREE with (La/Sm)cn ratios between 2.18 and 4.23, MREE enrichment over HREE
with (Gd/Yb)cn ratios of 1.74 to 1.89, and (Eu/Eu*)cn ratios of 0.99 to 1.26.

99
4.2.2.1.3 Big Daddy
The Big Daddy chromite deposit is hosted in main dunite and pyroxenite
lithologies along with transitional heterogeneous olivine pyroxenite. On a PM-
normalized diagram, the Big Daddy dunites and heterogeneous pyroxenite are enriched in
LREE relative to HREE and contain negative Nb-Ta, negative Zr-Hf, negative Y and
positive Ti anomalies (Fig. 4.17). The dunites display LREE enrichment over MREE
with (La/Sm)cn ratios between 2.49 and 9.19, MREE slight depletion or enrichment over
HREE with (Gd/Yb)cn ratios of 0.76 to 1.43, and (Eu/Eu*)cn ratios of 0.23 to 0.70. Five
of the samples have (La/Sm)cn between 2.49 and 4.18 while sample 232251 with
(La/Sm)cn at 9.19 is an exception. The enrichment of LREE to MREE and HREE reflects
crustal contamination like that in Black Label. Although HREE are depleted relative to
LREE, they are slightly enriched relative to MREE which could reflect an AUK signature
(Lesher et al., 1999 and Kerrich, 1997). There are also positive Ti anomalies which
would reflect the komatiite. For large ion lithophile elements (LILE) of Cs-Rb-Ba, there
is strong enrichment in the Big Daddy dunites reflecting crustal contamination by
continental crust. LILE are enriched in continental crust in contrast to depletion in
komatiites by themselves (Lesher, 1999). The heterogeneous pyroxenite displays the
higher REE content and LILE content than all the dunites and is notably transitional to
the higher REE and LILE contents of the Big Daddy pyroxenites.

The Big Daddy pyroxenites are also enriched in LREE relative to HREE, but have
more enrichment in overall REE than the dunites (Fig. 4.16). On a PM-normalized
diagram, the pyroxenites also contain negative Nb-Ta, negative Zr-Hf, negative Y and
positive Ti anomalies and are even more enriched in Cs-Rb-Ba. The samples display
LREE enrichment over MREE with (La/Sm)cn ratios between 1.94 and 6.52, MREE
slight depletion over HREE with (Gd/Yb)cn ratios of 0.80 to 0.92, and (Eu/Eu*)cn ratios
of 0.36 to 0.97. The negative Nb-Ta, Zr-Hf and positive Ti anomalies reflect crustal
contamination in komatiite. Local contamination of the pyroxenites, like the dunites, is
reflected by enriched Cs-Rb-Ba.

4.2.2.2 (La/Sm)cn vs. (Gd/Yb)cn
A (La/Sm)cn vs. (Gd/Yb)cn plot can be used to distinguish the different host rocks
to the three chromite deposits. Most of the samples plot in a (Gd/Yb)cn range from 0.75

100
0.001.002.003.004.005.006.007.008.009.0010.000.000.200.400.600.801.001.201.401.601.802.00(La/Sm)cn(Gd/Yb)cnBDduniteBDpyroxeniteBTduniteBTpyroxeniteBLduniteBLpyroxeniteBTleucogabbro
Figure 4.19. Plot of (La/Sm)cn vs. (Gd/Yb)cn for Black Label, Black Thor and Big Daddy
host rocks. Normalizing values of McDonough and Sun (1995).

101
to 1.0 (Fig. 4.19). This range for both dunite and pyroxenite suggests the host magmas to
the deposits are aluminum-undepleted komatiites or AUK. AUK at Pykes Hill, Quebec,
for example, plot between 0.8 and 1.2 mark whereas aluminum-depleted komatiites
(ADK) of the Tisdale suite plot between 1.2 and 1.6 (Kerrich, 1997). Although
(Gd/Yb)cn falls within the range, the (La/Sm)cn ratio will be more enriched in the samples
due to crustal contamination by TTG. The (La/Sm)cn ratios are from 1.5 to 4.0 rather
than near 0.5 for Pykes Hill. For the individual deposits, the Black Label dunites are the
most enriched in (La/Sm)cn while the Black Thor dunites are the most depleted. There
was probably more crustal contamination in Black Label. The Big Daddy dunites are
crustally contaminated in the range approaching that of Black Label. For (Gd/Yb)cn, the
Black Thor dunites contain less (Gd/Yb)cn than the others and are more primitive in
composition. For pyroxenite, Big Daddy and Black Label pyroxenites plot as similar
evolved with greater (Gd/Yb)cn compositions than the Black Thor pyroxenites.

4.3 Full spectrum PGE analysis
Full spectrum PGE analysis was performed on dunites, pyroxenites and
chromitites of the Black Thor, Black Label and Big Daddy deposits. The 26 samples
analysed for whole rock geochemistry were also analysed for full spectrum PGE. Six
more samples of chromitite were analysed for full spectrum PGE, two from each deposit.
Results are listed in Appendix 3.

4.3.1 Primitive mantle normalized PGE plots of host rocks
In comparing the dunites and pyroxenites hosting the three chromite deposits, the
dunites are more enriched in IPGE (Os, Ir, Ru) than the pyroxenites, but have similar
PPGE (Rh, Pt, Pd). Dunites have Pd/Irmn contents of 1.60 to 21.98 compared to
pyroxenites with Pd/Irmn contents of 0.65 to 26.2. This is similar to komatiites reported
by Barnes et al. (1985) where peridotitic komatiites have Pd/Ir of ~10 while pyroxenitic
komatiites have Pd/Ir of ~30. The more primitive PGE chemistry of the dunites
compared to the pyroxenites is probably due to the higher degree of partial melting in
magmas that fractionated the dunites. For individual deposits, the Big Daddy dunites are
more enriched in PPGE than the Black Thor dunites indicating there was more sulphur
saturation in the Big Daddy lithologies (Fig. 4.20). The Big Daddy dunites have Pd/Irmn
contents of 6.49 to 21.98 compared to Black Thor dunites with Pd/Irmn contents of 1.60 to

103
2.58. This is probably related to the Big Daddy lithologies being more evolved than the
Black Thor lithologies. The Black Label dunites are most enriched in IPGE with up to 30
ppm Ir and are enriched in PPGE like the Big Daddy dunites with up to 423 ppm Pt and
Pd (Fig. 4.21). The Black Label dunites have up to Pd/Irmn contents of 4.02 to 17.6.
Enrichment in IPGE reflects the more primitive PGE signatures of the Black Label
dunites. Along with enrichment in dunites, the Black Label pyroxenite is the most
enriched in PGE compared to the other pyroxenites (Fig. 4.22). The Black Label
pyroxenite is also the most fractionated pyroxenite with Pd/Irmn of 26.2. The Big Daddy
pyroxenites have Pd/Irmn contents of 2.32 to 21.97. The Black Thor pyroxenites are the
most primitive with Pd/Irmn contents of 0.65 to 14.17. The overall PGE are noticeably
different between the dunites and pyroxenites. The two lithologies probably reflect two
magmas – an olivine and a fractionated pyroxene magma - that were mixed to precipitate
the chromitites. The IPGE-rich dunites would reflect new S-saturated magmas that
mixed with less IPGE-bearing S-undersaturated pyroxenites, thus chromitites being
produced by magma mixing according to Irvine’s model.
4.3.2 Primitive mantle normalized PGE plot of chromitite
For the PGE signature of the chromitites, all the deposits are enriched in both
IPGE and PPGE with slightly more enrichment in PPGE (Fig. 4.23). These chromitites
appear to have similar PGE patterns in comparison to the Blackbird chromitite, reported
by Azar (2010),. The relatively low PGE of the chromitites suggests the intrusion is
largely sulphur undersaturated. Pd/Irmn contents range from 0.64 to 9.57. The
enrichment in IPGE is due to the presence of IPGE inclusions in chromite. Inclusions of
Rh, Ir, Os, Ru were detected in the chromite of Black Thor during the laser ablation
work. These are probably multiple PGE minerals including laurite and others. The Black
Label chromitite are the least enriched in Os, Ir, Ru and Rh compared to the Black Thor
and Big Daddy chromitites since they are the most evolved. Enrichment in Cu in Black
Label indicates the presence of sulphide in this deposit. For Pt contents, the Black Thor
and Big Daddy chromitites contain more Pt with contents of 279 ppm for Black Thor and
266 ppm for Big Daddy, compared to 133 ppm for Black Label. Although the Black
Label chromitites have proportional higher Pd with Pd/Pt ratio in one of the samples at
3.22, and usually have higher Pd contents e.g. assays of DDH BT-09-31.

105
4.4 Mineral chemistry of host silicates
Electron microprobe analysis was performed on primary host silicates, minerals in
silicate inclusions in chromites and on retrogressive silicate to the chromite. A total of
465 point analyses were determined for the silicates, not including serpentine, talc and
albite. These last three minerals were not included in the database. Of the 465 analyses,
32 point analyses were performed for olivine, 45 for pyroxene, 202 for amphibole, 61 for
phlogopite and 125 for chlorite. Analyses are listed in Appendix 4.

4.4.1 Olivine
Olivines were probed in only a few samples where there was remnant fresh
olivine and pyroxene in DDH BT-09-31. Since there is very little primary olivine
remaining due to pervasive hydration to serpentine, reporting of complete chemistries of
Mg # up section in the intrusion is not possible. However, the few remnant olivine grains
in the chromitites plot in compositions reflective of that layer, which gives evidence of
difference in Mg # between the chromitites (Fig. 4.24). The Layer 1 olivines have lower
Mg # between 85.7 to 90.77 compared to the Layer 2 olivines with Mg # between 90.68
and 94.41 reflective of the more primitive chromites in Layer 2 than in Layer 1.

4.4.2 Pyroxene
Primary intercumulus pyroxene has been pervasively retrogressed to
hydrothermal tremolite and talc. Fresh pyroxene was analysed where preserved in five
samples in Black Label DDH BT-09-31. Notably, no primary pyroxene is preserved in
the Black Thor and Big Daddy drill holes. On a pyroxene ternary plot, the pyroxenes are
classified as diopsides and augites for clinopyroxene and pigeonites and enstatites for
orthopyroxenes (Fig. 4.25). In sample 486211 at 174.4 m, there is a trend of ferrosilite
depletion in three pyroxenes from the main cluster of pyroxenes in the diopside-augite
field (Fig. 4.26). The three offset pyroxenes are due to magmatic metasomatism of the
primary pyroxene cluster. These pyroxenes have ferrosilite component at 2.83 to 3.39 %
whereas the primary pyroxenes have ferrosilite at 4.73 to 5.60 %. This trend in Mg
enrichment is due to replacement of the primary pyroxenes by metasomatic pyroxene.

Another trend evident in the diopside-augite cluster is the increase in wollastonite
component in the primary pyroxenes from 45.70 to 47.79 %. This trend is due to core to
rim diffusion in the relic pyroxenes due to melt metasomatism. Evidence of the core to

109
rim diffusion is the variation from a core pyroxene at point 4 in sample
486211image_0001 at 45.40 % Wo to a rim pyroxene at point 3 at 46.90 % Wo.
Diffusion to greater wollastonite component is also evident in the orthopyroxenes of
sample 486211 (Fig. 4.27). Wollastonite increases from core orthopyroxene at 2.46 %
Wo to rim orthopyroxene at 5.99 % Wo.

Primary pyroxenes occur as both poikilitic phases in the host olivine cumulate and
the chromitite and as minerals in the chromite-hosted silicate inclusions. The primary
pyroxenes are characterized by elevated non-pyroxene quadrilateral components such as
wt. % TiO2 and wt. % Cr2O3. The chromian diopsides have up to 0.33 wt. % TiO2 and

1.74 wt. % Cr2O3 while the orthopyroxenes have up to 0.22 wt. % TiO2 and 0.80 wt. %
Cr2O3. The trend of decreasing Ti from primary to metasomatic to hydrothermal
pyroxene is displayed on a plot Ti vs. total Al where the primary pyroxenes have higher
Ti and Al contents (Fig. 4.28).
Hydrothermal diopsides were also detected in sample 486155 at 151.8 m in Black
Label DDH BT-09-31. These represent higher T metamorphism of pyroxene into
diopside stability after tremolite at 450 °C temperature (Winter, 2001). These pyroxenes
have almost no non-quadrilateral components and high MgO at up to 21.71 wt. %.

4.4.3 Amphibole
The McFaulds Lake chromites have associated of both primary igneous and
secondary retrogressive amphiboles. The amphiboles probed in this study are from Black
Label DDH BT-09-31 and Black Thor DDH BT-09-17. All the amphiboles analysed are
divided into three groups according to the nomenclature of Leake et al. (1997). Noteably,
Cr is not accounted for in this classification scheme. There are three types of igneous
amphibole: the magnesiotaramites-magnesiokatophorites-winchites, the pargasitesedenites
and the tschermakites-magnesiohornblendes. On a plot of Mg # vs. Si for
(Na+K)A > or < 0.50; (Ca+NaB) =
1.00; 0.50 < NaB < 1.50, the first group of amphiboles
range from the bulk cluster of lower Si-bearing magnesiotaramites and
magnesiokatophorites with Si between 6.47 and 6.81 that trend in Si enrichment to four
winchite compositions with Si ranging from 7.49 to 7.819 (Fig. 4.29). The bulk cluster of
magnesiotaramites-magnesiokatophorites consists of silicate inclusion amphiboles found
in both the Layer 1 and Layer 2 Black Label chromitites. On a AlIV vs. NaA+K diagram,

112
these amphiboles plot in the range of igneous amphiboles with NaA+K greater than 0.5
which have relatively similar AlIV compositions of about 1.1 to 1.45 (Fig. 4.30). The
winchite is the only exception and occurs along the 1:1 magnesiohornblende to tremolite
trend and has a NaA+K value of 0.49. On a AlIV-(Na, K)A vs. AlVI+2Ti+Cr diagram, the
amphibole with the highest Ti number is a magnesiotaramite while the amphibole with
the highest Cr number is a magnesiokatophorite (Fig. 4.31). The winchite plotted on the
Mg # vs. Si diagram with Si of 7.49 is from a relatively bright silicate inclusion mineral
that occurs with albite in silicate inclusions at 273.6 m depth in the Black Label Layer 2
chromitite. The other three winchite compositions that did not run through the Papike
calculation with Si from 7.81 to 7.819 are three point analyses from a single silicate
inclusion amphibole from sample 486211 at 174.4 m.

 The pargasites-edenites plot on a diagram of Mg # vs. Si for CaB =
1.50; (Na+K)A
> 0.50; Ti < 0.50 (Fig. 4.32). There is one large cluster that plots in the range of Si
between 6.37 and 6.99 while one point analysis plots at Si of 7.24. Within the range of
these amphiboles, there is a trend of increasing Si and Mg # that probably reflects
igneous evolution of decreasing Mg # in the amphiboles. On a plot of Mg # vs. depth for
Black Label DDH BT-09-31, the amphiboles in Black Label Layer 2 from 232 to 321 m
in DDH BT-09-31 have a higher amount of high Mg # amphiboles than Layer 1
amphiboles from 155 to 186 m which probably reflects the more primitive chromite
compositions of Layer 2 (Fig. 4.33). A trend of decreasing Mg # with height from 255.6
m to 273.6 m in Layer 2 from 0.98 to 0.90 is suggestive of a differentiation trend.
Notably, two pargasite compositions were detected (analyses 33 and 34 at 155 m) for
igneous amphibole that surrounds silicate inclusion-bearing chromites with amphiboles
of the same composition in the silicate inclusions. On a AlIV vs. NaA+K diagram, the
pargasites-edenites have the highest range of AlIV compositions in the range of
amphiboles with NaA +K greater than 0.5 (Fig. 4.30). The AlIV compositions range from

1.01 to 1.66. On a AlIV-(Na, K)A vs. AlVI+2Ti+Cr diagram, the pargasites-edenites plot
in the large cluster of igneous amphiboles with high Ti and Cr contents (Fig. 4.31).
The tschermakites-magnesiohornblendes plot with and are replaced by
retrogressive tremolite as the third type of amphibole. On a Mg # vs. Si diagram for CaB
=
1.50; (Na+K)A < 0.5, there is a Si enrichment trend with associated Mg enrichment that

116
represents the retrogression of pargasite to magnesiohornblende and further to tremolite
(Fig. 4.34). This trend is better observed on a AlIV vs. NaA+K diagram where there is
decreasing NaA+K with decreasing AlIV from pargasite to tremolite (Fig. 4.30). Evidence
of this retrogression is the presence of chromian tremolite in analysis 71 of sample
486211 at 174.4 m that occurs as tabular grains adjacent to a crack in a silicate inclusion
with pargasite. Notably, relics of pargasite at 155 m are observed in poikiloblastic
chromian tremolite which represents replacement tremolite. Also, secondary zonation is
observed from edenite to tremolite from points 1 to 2 in zoned amphibole sample 486211
image_0010, 174.4m depth (see petrography chapter, silicate inclusions). The
retrogressive trend is also observed as decreasing AlIV-(Na+K)A with decreasing
AlVI+2Ti+Cr where the replacement tremolites have lower Ti and Cr contents than the
pargasites and other igneous amphiboles (Fig. 4.31). A large amount of the tremolites are
also replacement of primary chromian diopsides. One tremolite with elevated Cr
(analysis 40 in sample 486211) is a poikiloblastic tremolite that replaces poikilitic
chromian diopside that occurs as a patchy poikilitic pyroxene interstitial to massive
chromite. The Mg enrichment evident in the pyroxenes as a whole represents initial
retrogression toward more Mg-enriched tremolites. Finally, there are also high Mg
hydrothermal vein tremolites present at 321 m in Black Thor DDH BT-09-17 with Mg #s
of 0.96 to 0.99. These tremolites are zoned and their presence indicates higher T
prograde alteration of the upper chromitites in that layer.

4.4.4 Phlogopite
The phlogopite probed in Black Label DDH BT-09-31 is unusual due to Ti and Cr
enrichment similar to phlogopites found in other chromite-bearing rocks. On a plot of wt.
% Al2O3 vs. wt. % TiO2, the phlogopite plots with high Al2O3 at 6.89 to 15.49 wt. % and
enriched TiO2 in the primitive mantle box; and they plot with compositions below the
box on a kimberlite trend (Fig. 4.35). This would lead one to interpret that these minerals
to be sourced directly from the mantle. The phlogopites are hosted within round silicate
inclusions in the chromites and also in the surrounding matrix. The phlogopites in the
common groundmass are more regular K phlogopites while those in the silicate
inclusions are K and more Na-enriched phlogopites. Variation between the K and Na-
enriched compositions is seen on a ternary Ba-K-Na plot (Fig. 4.36). Since Na

120
phlogopites are in the silicate inclusions and not in the groundmass, this could lead one to
interpret that the silicate inclusion phlogopites are different than the groundmass
phlogopites, possibly encaptured as metasomatized mantle nodules within the chromites.

However, with variation of wt. % MgO and Cr2O3 with up section height, it is
shown that the phlogopites (with mostly silicate inclusion phlogopites being represented
here) have lower MgO/higher Cr2O3 contents in Black Label Layer 1 and higher
MgO/lower Cr2O3 in Layer 2 (Figs. 4.37 and 4.38). The Layer 2 inclusions are therefore
more primitive and reflect the trends of more MgO-rich chromites in Layer 2 than in
Layer 1. This trend is also seen in the plot of Mg # variation of pargasite-edenite with up
section height. A correlation of decreasing wt. % MgO with increasing wt. % Cr2O3 is
evident due to Mg-Cr substitution with igneous evolution in the phlogopites (Fig. 4.39).
On a plot of wt. % Cr2O3 vs. wt. % TiO2, there is a correlation of increasing Cr with Ti
that is similar to that observed in metasomatic phlogopites of the upper mantle (Fig. 4.40;
Erlank et al., 1987). In the case of these phlogopites, they were probably enriched in Cr
and Ti in the presence of residual melt. It appears therefore that the phlogopite
compositions define trends of igneous evolution in Ti and Cr phlogopites and are more
akin to ultramafic intrusive-hosting phlogopites in a layered intrusion. The Ti and Cr
enrichment in more Na-bearing phlogopites in some of the silicate inclusions has
probably been derived from the surrounding chromites themselves similar to phlogopites
in the Stillwater Complex (Page and Zientek, 1987). This is discussed in more depth in
chapter 6.

4.4.5 Chlorite
Chlorites were analysed from three drill holes: Black Label DDH BT-09-31,
Black Thor DDH BT-08-10 and Black Thor DDH BT-09-17. On a Fe # vs. Si plot, the
chlorites plot as a range of Si vs. Al with very magnesian compositions from sheridanite
to clinochlore to penninite (Figs. 4.41 to 4.43). The Mg content of the chlorites reflect
the Mg content of the chromites in the various zones. The Black Label chlorites are
divided between those found in the Layer 1 and Layer 2 chromite intervals. The Layer 1
chlorites are the four analyses that plot in a separate cluster of higher Fe # than the other
chlorites and reflect the higher Fe # of the host chromitites (Fig. 4.42). The Layer 2

127
chlorites, on the other hand, are more primitive with lower Fe # more similar to the Black
Thor chlorites (Figs. 4.41 and 4.42).

There is a large range of chlorite compositions in the Black Thor chromites
analysed. Three types of chlorite have been probed in the samples: 1) chlorites found in
the round silicate inclusions in chromite; 2) chlorites found in the matrix of host dunites
and chromitites; 3) and chlorites found as inclusions in the reaction margins of chromites.
The chlorites are distinguished on a plot of wt. % Cr2O3 vs. wt. % Al2O3 (Fig. 4.44). The
chlorites found in the round silicate inclusions plot as the four analyses 43 to 46 which
are from sample 486034 at 131.2m in DDH BT-08-10. Three of these chlorites have high
Al2O3 at 20 wt. % and elevated Cr2O3 at up to 2.63 wt. %. The fourth chlorite has lower
Al2O3 at 15.53 wt. % and higher Cr2O3 at 3.66 wt. % as Cr substitutes with Al. The high
Al2O3 and elevated Cr2O3 contents of these minerals are derived from the high Al and Cr
contents of the host chromites. They probably formed from retrogression of chromite and
host amphiboles and other minerals found within the round inclusions. The chlorites
found in the host silicate and surrounding chromites have lower Al2O3 contents of 13 to
15 wt. % and either do or do not contain elevated Cr2O3. Those with elevated Cr2O3
either replace interstitial chromian tremolite occurring interstitial in massive chromitites
or are found as chromian chlorites in fractures where there has been mobility of Cr. It
has been noted in the petrography chapter that the fracture chlorites all have elevated Cr
while other interstitial chlorites either do or do not have elevated Cr. The chlorites found
as inclusions in the reaction margins of chlorites are similar to the chlorites found in the
round silicate inclusions with elevated Al2O3 from 16 to 20 wt. % and elevated Cr2O3 up
to 2.55 wt. %. Some of these chlorites plot with lower Al2O3 and are similar to the
matrix chlorites but with higher Cr2O3, up to 5.75 wt. %. The high Cr, low Al is due to
substitution of Cr for Al, as in the round silicate inclusion-bearing chlorites.

On a wt. % Cr2O3 vs. wt. % MgO plot, there is an overall trend of decreasing
Cr2O3 with increasing MgO in the chlorites as a whole; however, there are two trends
within the Black Thor DDH BT-08-10 and Black Label chromites for increasing Cr2O3
with MgO (Fig. 4.45). Overall, the chlorites are found as very Cr-rich (up to 9.61 wt. %
Cr2O3) minerals coexisting with the upper chromites of DDH BT-09-17, lesser Cr-rich

(1.6 to 7.17 wt. % Cr2O3) chlorites co-existing with chromite in DDH BT-08-10 and

129
DDH BT-09-31, and low Cr-bearing regular chlorites coexisting with serpentine in the
host dunites to the chromitites.

The high chromian chlorites of DDH BT-09-17 have lower Mg contents since
there is Mg enrichment with higher T retrogression of these chromites from core to rim.
This would not result in as high Mg content in the resulting chlorite due to mass balance.
However, the high Cr enrichment of ferrichromite on the rims of these chromites serves
to also enrich the Cr contents in the resulting chlorites. On the wt. % Cr2O3 vs. wt. %
Al2O3 diagram, the DDH BT-09-17 chromites follow a separate trend of decreasing
Cr2O3 with increasing Al2O3 than the other chlorites (Fig. 4.44). The chlorites as a whole
generally decrease in Cr content with substitution with Al. However, the DDH BT-09-17
chlorites retrogressed at higher temperatures resulting in increased Cr and Al contents
and substitution of the two elements under these conditions.

The two lower trends of increasing Cr2O3 with MgO are a result of Mg and Cr
enrichment with the diffusion of Mg and Cr ions of the primary chromite as retrogression
in the resulting chromites (Fig. 4.45). It was also noted in the petrography chapter that Cr
is enriched in chlorites along fractures where there has been more retrogression of
chromites as opposed to some of the interstitial groundmass to the chromites where there
has not been this diffusion.

Finally the low Cr, high Mg chlorites are pristine clinochlores that occur with
serpentine in the dunite host to the chromites and as chlorites surrounding chromite
where there has not been mobility of Cr. Clinochlore is a result of low T greenschist
hydration of the silicates.

130
CHAPTER 5
MINERALIZATION

5.1 Introduction
The nature of the chromite mineralization at McFaulds Lake is defined by an
initial investigation of drillhole assay data, by electron microprobe analysis of major
element chemistry of chromite, and by a laser ablation study of trace element chemistry
of chromite.

5.2 Metal assay variation
Chromium oxide (wt. % Cr2O3), base and precious metals analyses are reported
for three DDH holes representative of the three chromite deposits: DDH FW-08-19 for
Big Daddy; BT-08-10 for Black Thor; and BT-09-31 for Black Label. These assays are
reported on the exploration drill programs by Freewest-Spider-KWG for Big Daddy, and
by Freewest for Black Thor and Black Label. Discussion of assay trends presented below
are divided into up section Cr2O3 wt. %, Pt, Pd, Ni and Cu variation. This is followed by
wt. % Cr2O3 vs. Ni, Ti, Zn and Mn variation for the Black Label, Black Thor and Big
Daddy deposits respectively.

5.2.1 Up section wt. % Cr2O3, Pt, Pd, Ni and Cu ppm variation
Assay values for whole rock wt. % Cr2O3, ppb Pt+Pd and ppm Ni were
investigated as a preliminary framework to performing electron microprobe work on
chromite. This data shows basic trends of replenishment and differentiation in terms of
Cr2O3 and Ni. Also, associated peaks in Pt+Pd mineralization provide evidence for
double diffusive convection processes being involved in PGE concentration in the
chromitites and host lithologies. Although helpful to understanding of gross trends
through each of the chromitite intervals, care must be taken as the whole rock wt. %
Cr2O3, ppm Ni and ppb Pt+Pd represent the content of chromite + silicate rather than
chromite alone; the variation in chromite chemistry is determined through electron

131
microprobe analyses. The up section variation in these metals is presented for the Black
Label, Black Thor and Big Daddy drill holes in sections 5.2.1.1 to 5.2.1.3.

5.2.1.1 Black Label (Figs. 5.1 and 5.2)
In Black Label DDH BT-09-31, there are trends of increasing wt. % Cr2O3
upward, identifying repeated pulsing of chromite layers within alternating lithologies in
three separate chromitite intervals. The first chromite interval at Black Label is from 154
to 206 m. From 154 to 165 m, there are two initial chromite replenishments with peaks at
14 wt. % Cr2O3. Between 165 to 210 m, there is an overall trend of differentiation with
decreasing wt. % Cr2O3. However, in the overall trend, there are individual chromite
replenishment peaks in wt. % Cr2O3 that increase in Cr2O3 with each successive
replenishment. Pt+Pd show peaks that are offset from the replenishments in Cr2O3,
usually beneath each Cr2O3 layer. These PGE peaks probably represent sulphur
saturation near the bottom and top boundaries of a convection layer.

PGE peaks at the tops and bottoms of convection layers have been known to
occur in other layered complexes such as the Bushveld Complex. They have been
attributed to represent initial sulphur saturation of a magma that initially convected near
the top and bottom boundary layers of double diffusive convection cells (Rice and von
Gruenewaldt, 1994). In the overall interval, Pt+Pd values have signatures of primary
Pt+Pd in the top silicate at 206 m and the bottom of the interval at 156 m. With increased
stratigraphic height between, there is a decreasing cascading upward trend of Pt+Pd
values due to saturations with each chromite replenishment upward in the sequence.

For Cr2O3, the individual replenishments of Cr2O3 in the overall differentiation
trend reflect massive to lensy and discontinuous beds of chromitite hosted in pyroxenite
between sections of dunite. Along with replenishments in Cr2O3, there are peaks in Ni
contents within the dunites that occur after each successive chromite layer. The Ni
contents of the dunites increase upward in the section due to replenishing supply of
magma. Cu contents show an overall increasing upward trend reflecting higher Cu
contents with increased fractionation.

The second chromite interval is from 229 to 277 m. At first there is silicate with
little chromite mineralization. Then from 248 to 270 m, there is a series of chromite
replenishments that increase in wt. % Cr2O3 upward from 248 to 257, followed by a

136
green serpentinized dunite. From 124 to 152 m, there is an interval of intermittent
chromitite beds that are variably 1 to 50 cm thick that alternate with dunite. The beds
contain layers of chromite that fine upward to chain textures of cumulus chromite and
olivine as chromite is filter pressed through the overlying dunite pulses. The individual
chromite beds are identified by replenishments in wt. % Cr2O3 that successively increase
upward from 124 to 130 m. From 130 to 152 m, replenishments in wt. % Cr2O3 of
individual pulses follow an overall decreasing trend in wt. % Cr2O3 due to more
dominant differentiation in the sequence. Pt+Pd peaks correspond with Cr2O3
replenishments. Ni ppm increases upward with each dunite pulse between the chromite
beds. At 149 m, there is a peak at 2790 ppm Ni along with elevated Cu that is possibly
due to sulphide.

From 152 to 165 m, there is another chromitite interval where there is a dominant
replenishment of wt. % Cr2O3 followed by decreasing wt. % Cr2O3 in replenishments
from 157.8 to 165 m. Ni ppm increases with each dunite pulse between the chromite
layers. From 162 to 168.20 m, there are cumulus contacts below the lower and above the
upper contacts of the chromite layers indicating a change in the order of crystallization of
chromite and olivine. Above 168.20 m, beds then contain cumulus olivine grading up to
chromite that indicate dominant cumulus olivine over cumulus chromite mineralization.
There are then upward replenishments of increasing wt. % Cr2O3 as the magma switches
back to the chromite stability field from 168.20 to 174.20 m. At 174.20m, there is a
sharp upper contact of the chromitite bed followed by the main dunite again. Notably,
there are peaks in Cu ppm at 175 m depth above the chromite layer which are probably
due to sulphur saturation at the upper contact.

The Black Thor deposit in DDH BT-09-17 intersects chromitite located within
host pyroxenite and gabbro lithologies which shows trends in greater enrichment in wt. %
Cr2O3 compared to the other chromitites in that particular drill hole. The sequence is
found from 290 to 345 m depth. At 290 m, there is first pyroxenite with elevated Ni
ppm. From 296.30 to 298.80 m, there is a pulse of chromite represented by up to 38.92
wt. % Cr2O3. Along with a peak in wt. % Cr2O3, there is a peak of 306 ppb Pt+Pd. From

298.80 to 318.70 m, there is gabbro. In contrast to the pyroxenite, there is little Ni in the
gabbro and the unit is devoid of Pt, Pd and chromite. From 318.70 to 339 m, there are

137
three chromite sequences that alternate with gabbro, giving rise to troughs in wt. %
Cr2O3. Cr2O3 contents reach a maximum of 43.63 wt. % and possibly show trend in
increasing Cr2O3 upward. These could be indicative of enrichment in wt. % Cr2O3 with
retrogression of the chromites. Pt+Pd ppb show the highest peak in the third sequence
where there is more silica for greater sulphur saturation. Above the sequence from 339 to
345 m, there is again pyroxenite similar to the first pyroxenite at 290 m.

5.2.1.3 Big Daddy (Fig. 5.7)
Big Daddy DDH FW-08-19 begins with a sequence of dunite with intervening
pyroxenites and heterogeneous olivine pyroxenite as the system changes from cumulus
olivine to pyroxene followed by chromite mineralization. There are a few intervals of
chromite mineralization before the main sequence from 141.50 to 144.14 m and from

159.37 to 162.00 m that show replenishments in wt. % Cr2O3 and associated peaks in ppb
Pt+Pd. In the interval of pyroxenite before the lower contact with the main massive
chromitite sequence, there is high ppb Pt+Pd within 20 m of the contact. This possibly
represents remobilized PGE since it is not in one horizon with visible sulphide, however
it is not fully understood. Some sulphide is present since there is a large peak of 8480
ppm Ni at 165 m (Fig. 4.10). In the company logs, sulphide has been noted with
predominately po with minor py and trace cpy. The mineralization style follows the
foliation where it is semi massive but it appears to be fine grained disseminated on
fracture surfaces. Notably, similar fracture pyrite has been noted immediately above the
chromitite/pyroxenite contact which shows a similar peak in Pt+Pd.
The massive chromitite begins after the pyroxenite at 183 m and continues to 229

m. Within the sequence, wt. % Cr2O3 is consistently high at between 33 to 39 wt. %
Cr2O3. The chromitite sequence is divided into three intervals. The first two there is
increasing wt. % Cr2O3 followed by decreasing wt. % Cr2O3 from 183 to 192 m and from
192 to 208.5 m. From 208.5 to 229m, there is an overall decreasing trend in wt. % Cr2O3.
The increases in wt. % Cr2O3 are due to replenishments while the decreasing trends are
differentiation trends. Pt+Pd values are offet by these increases and decreases probably
due to individual sulphur saturations in the top and bottoms of double diffusive
convection cells as at Black Label.

139
Above the upper contact of the chromitite, there is pyroxenite again. There is
high ppm remobilized Pt+Pd again in the background pyroxenite. Notably, there are
medium grained fracture pyrite sulphides just above the upper contact. The unit is
bleached due to talc, indicative of intense hydrothermal alteration.

5.2.2 Binary metal assay variation
Binary metal plots that represent association of Ti, Zn and Mn with modal %
chromite are displayed for Black Label (Fig. 5.8). Ni contents, on the other hand, do not
show a correlation. For Ti ppm vs. Cr ppm, Ti increases with Cr, demonstrating Ti is
partitioned into chromite grains than into silicate. Zn shows an even stronger correlation
as Zn partitions into chromite, however, there are also Zn contents that are above the
main trend due to sulphide mineralization. Mn generally correlates with Cr like Ti and
Zn, however, there is variable Mn content in host dunite vs. pyroxenite. Pyroxenite
contains more elevated Mn compared to the dunite. V contents are interesting in that they
show two trends of increasing V ppm vs. Cr ppm. These represent the two chromitite
intervals of Black Label. The first chromitite interval follows the lower trend plus the
higher sloped trend of increasing V ppm vs. Cr ppm. The second chromitite interval only
follows the lower sloped trend. The higher V in the first chromitite interval is due to
higher V with differentiation of the chromitite in the first chromitite interval while the
second chromitite interval is more primitive. These same trends can be shown for the Ti
% vs. Cr ppm for these two intervals. The third interval follows the same trend as the
second interval only with lower V and Cr contents.

Black Thor BT-08-10 shows well defined positive correlations of Ti, V and Zn
with Cr (Fig. 5.9). There is a strong association of these metals with modal % chromite.
Mn also shows a positive correlation but more diffuse. The consistent trend in Mn
reflects only one host lithology to the chromite which is dunite. Ni contents show a
diffuse negative correlation with Cr while an antipathetic positive correlation with Mg %.
Therefore, Ni in Black Thor is more strongly associated with Ni in olivine of the dunite
pulses.

Big Daddy also shows well defined correlations, although many of the samples
plot as either low in the various metal contents or at high metal contents in the massive
chromitite (Fig. 5.10). The fewer intermediary metal contents reflect increasing Ti, V, Zn

143
with increased modal % chromite. Mn show a broad correlation although many samples
contain Mn that do not follow the trend as there is considerable cumulus pyroxene-
bearing lithologies with elevated Mn and the chromitite is more varied in Mn with
evolution to bordering pyroxenite. The same variability in metals is reflected in Ti and V
as well for the massive chromitite interval. Ni shows negative correlation with Cr and
shows a subtle positive correlation with Mg % due to Ni in cumulus olivine-bearing
dunite.

5.3 Chromite mineral chemical variation
A major effort was made to define the mineral chemical variation in the McFaulds
Lake chromite deposits. Electron microprobe analysis has been carried out on 300
samples with over 4200 point analyses on samples spaced 20 cm to 1 m apart across
individual gravitational cycles. Generally, up to 8 point analyses are made of each
chromite sample. More point analyses are needed where there is evident textural
variation in modal chromite (i.e. mineral zoning), there is variation in grain size, and
higher ferrichromite content (Fig. 5.11). The microprobe work outlines the primary
differentiation sequences as well as the effects of secondary hydration on chromite
mineral chemistry. Results are listed in Appendix 5.

The microprobe analyses document original igneous compositions best preserved
in the cores of large chromite grains in massive chromitite. The smaller, more isolated
disseminated chromites have undergone greater silicate exchange. Primary compositions
retained in larger grains best define igneous fractionation. Ferrichromite developed on
the rims of original grains relates to secondary hydration. Specific chromite mineral
chemistry therefore relates to both primary adcumulate sintering and secondary hydrous
retrogression.

Current microprobe data shows Cr2O3 loss from 55 to 51 wt. % for centres of
grains up section. Grain margins and disseminated smaller grains show up section
chemistries of 49 to 47 wt. % Cr2O3. Disseminated chromites have generally undergone
more silicate exchange, reporting 48 wt. % Cr2O3. Other elemental variation in the
chromites includes increasing Fe, slightly decreasing Al and decreasing Mg due to
magmatic differentiation. Near constant low-Al compositions are characteristic of
komatiitic chromites. High grade chromite with higher wt. % FeOT forms as retrograde

145
ferrichromite rims. Original magmatic chromites are leached of Mg and Al leaving high
Cr and Fe behind as ferrichromite.

The ferrichromite content has the effect of increasing or decreasing the Cr content
of the ores. Cr-enriched ferrichromites are found as retrogression on the more primitive
chromitites while Cr-depleted ferrichromites are found as further retrogression on
disseminated chromite. The evolution of the chromites from core to rim to ferrichromite
is illustrated in ferrichromite-bearing chromitites in three samples of massive chromite in
DDH BT-08-10 (Figs. 5.12 to 5.17). In sample 486044 at 135.2 m, there is primary
chromite with 52.18 wt. % Cr2O3, 9.17 wt. % MgO, 19.78 wt. % FeO and 14.09 wt. %
Al2O3 (Figs. 5.12 to 5.13). Due to increased diffusion towards the margin of the grain,
there is then depletion of Cr2O3 and MgO to 50.04 and 8.87 wt. % respectively with
enrichment in Al2O3 and FeO to 14.69 and 20.19 wt. % respectively. In one intermediate
ferrichromite, there is enrichment in Cr2O3 and FeO to 57.84 and 22.27 wt. %
respectively while depletion in Al2O3 and MgO with substitution to 9.87 and 7.28 wt. %
respectively. In a more enriched ferrichromite, Cr2O3 and FeO increase to 59.94 and

21.53 wt. % respectively while Al2O3 and MgO decrease to 7.97 and 7.06 wt. %
respectively. The ferrichomite occurs in association with chromian chlorite. There is
later growth of Cr-depleted ferrichromite with relic grains of chlorite that decrease in
Cr2O3, Al2O3 and MgO to 48.90, 6.92 and 5.76 wt. % while FeO enriches to 23.50 wt. %.
Notably, Fe2O3 has a composition of 13 wt. % compared to the earlier Cr-enriched
ferrichromite at 2.47 wt. % Fe2O3. The same trend is seen in another chromite from
sample 486044 at 135.2 m, but there is an increase from core to rim in Cr2O3 in the
primary chromite grain (Figs. 5.14 to 5.15). In sample 486129 at 169.6 m, Cr2O3
enriches to up to 65.11 wt. % with FeO at 23.25 wt. % while Al2O3 and MgO decrease to
2.62 and 5.16 wt. % respectively (Figs. 5.16 to 5.17).
5.3.1 Up section mineral chemistry of chromite
Detailed electron microprobe analysis was performed on chromitite intervals
through the three deposits. Up section plots showing variation of wt. % Cr2O3 and wt. %
MgO vs. depth are provided for the three chromite deposits in section 5.2.1. Comparable
Cr #s (Cr/(Cr+Al+Fe3+)) and Mg #s (Mg/(Mg+Fe2+) are plotted to supplement the wt. %
Cr2O3 and wt. % MgO. Cr/Fe (Cr2O3/FeOT) diagrams are also indicators of magma

149
evolution, but more importantly provide economic grades of the three deposits. There is
a major difference from higher grade chromitites with Cr/Fe of 2 to 2.5 to lower grade
with Cr/Fe of 1 to 1.7. The lower Cr/Fe is an indicator of more modal silicate degrading
the ore. Also plotted are wt. % Al2O3 and wt. % FeO. Plots of wt. % Fe2O3 and wt. %
TiO2 for total chromite illustrate the range of spinel compositions between ferrochromite
and magnetite, due to primary igneous fractionation and secondary retrogression of the
chromites. Black Label analyses are from DDH BT-09-31; Black Thor from DDH BT08-
10 and Big Daddy from DDH FW-08-19. Another section of chromitite was probed
in DDH BT-09-17 for chromitite hosted in gabbro. Note that since the host sill is
overturned, increasing drill hole depths register increasing height in sill stratigraphy.

The microprobe analyses also show details of the deposits in terms of binary
variation of major oxides and metals as an aid in tectonic discrimination. Section 5.3.2
documents the binary variation of Black Label, Black Thor and Big Daddy in terms of
wt. % Cr2O3, Al2O3 and FeO vs. wt. % MgO along with the metals of wt. % TiO2, ZnO,
MnO and NiO vs. wt. % MgO.

In comparing trends of the three chromite deposits, the Black Thor chromites are
highest grade with more primitive magmatic compositions in terms of Cr and Mg than the
Black Label chromites. Heterogeneous pyroxene oikocrystic harzburgites host the Black
Label chromitite, and more heterogeneous textures are displayed by the chromite ores
themselves. With higher modal % silicate in the chromitite there is more silicate
exchange accounting for the lower 50 to 46 wt. % Cr2O3 in Black Label chromite
compared to 53 to 49 wt. % Cr2O3 in Black Thor. In addition to the more primitive
composition of Black Thor chromite, magmatic variation grossly accounts for the lower
wt. % Cr2O3 in disseminated chromite grains. Although lower Cr2O3 contents occur with
more silicate exchange in disseminated grains, a strong linear regression from massive to
disseminated grains reflects magmatic differentiation in forming massive through to
disseminated chromite (Fig. 5.18). In terms of trends of other oxides, wt. % Al2O3 varies
antipathetically with wt. % Cr2O3 and wt. % FeO varies antipathetically with wt. % MgO
(Fig. 5.19). TiO2 also increases with decreasing wt. % MgO, though there is less
variation in wt. % TiO2 in the deposits.

151
The massive chromitite at Big Daddy shows remarkable homogeneity at 50 to 51
wt. % Cr2O3. This is higher than reported assay data for wt. % Cr2O3, which is accounted
for by the minor silicate. The homogeneity of the massive ores is attributed to
development of chromite layers by double diffusive convection (Rice and von
Gruenewaldt, 1994). With little silicate in the massive zones there is less silicate
exchange, much less than observed in the exchanged chromitites of the Black Thor and
Black Label intersections. Variations from core to rim in all chromite is essentially due
to diffusion during secondary hydration.

5.3.1.1 Black Label
The two chromitite intervals probed in BT-09-31 have markedly different mineral
chemistries. First, from 158 to 161 m, the Cr2O3 and MgO values in disseminated
chromite are low with maximum contents of 42 to 44 wt. % Cr2O3 and up to 4.67 wt. %
MgO (Figs. 5.20 to 5.23). Notably, FeO contents are high ranging from 26 to 30 wt. %
(Fig. 5.24). The first chromitite interval from 161 to 203 m comprises 4 zones defined by
4 pulses of decreasing wt. % MgO with height (Fig. 5.21). Cr/Fe ratios are lower with
between 0.98 and 2.26 for magmatic compositions and as low as 0.41 for alteration rim
Cr-enriched to Cr-depleted ferrichromites (Fig. 5.25). Within this first interval, wt. %
Al2O3 contents are more elevated in these chromites than in the chromites from the
second interval, except for the low wt. % Al2O3 contents in the Cr-enriched to Cr-
depleted ferrichromites (Fig. 5.26). The trend in wt. % Al2O3 is also evident in wt. %
TiO2 where the first interval contains higher wt. % TiO2 than the second interval.

The first pulse from the first interval is from 161 to 164 m and contains the lowest
wt. % MgO and wt. % Cr2O3. The next two pulses are larger up to 20 m in thickness, and
contain well defined differentiation sequences of decreasing wt. % MgO. Within these
two pulses are individual replenishments with MgO peaks followed by decreasing wt. %
MgO. The second pulse contains two subzones with wt. % MgO decreasing in the
second subzone from 176 to 179 m. Notably, there is a large amount of Cr-depleted
ferrichromite detected at the top of this subzone as displayed by enriched Fe2O3
compositions (Fig. 5.27). There appears to be an association of Cr-depleted ferrichromite
with evolved chromite. This is due to more diffusion and leaching of ions to form the Cr-
depleted ferrichromite where there is a greater proportion of adjacent silicate.

160
The third pulse contains three subzones of decreasing wt. % Cr2O3 with height,
following the pattern of differentiation shown by the MgO contents. In the fourth pulse
of the chromitite interval, with each new replenishment the Cr2O3 contents remained high
at about 50 wt. % Cr2O3. However, individual differentiation sequences of decreasing
Cr2O3 wt. % with height can be picked out within up to 6m thick mini-pulses. These
mini cycles possibly formed by convection cells within the larger pulse of magma (Rice
and von Gruenewaldt, 1994; Naldrett et al., 2010).

The second chromitite interval is from 229 to 276 m and contains 3 zones from
229 to 257 m, 257 to 265 m and from 265 to 276 m characterized by separate subsets of
elevated wt. % Cr2O3 separated by troughs of low wt. % Cr2O3. Notably, the Cr2O3
values are consistently high at above 50 wt. % suggesting a primitive chromitite interval.
In the first zone, 3 pulses of replenished MgO are followed by decreasing MgO trends.
Cr/Fe ratios are higher and more primitive in this second interval with between 1.82 and

2.42 for magmatic chromite compositions and as low as 1.38 for alteration rim Cr-
enriched to Cr-depleted ferrichromites. With each successive replenishment, there is an
overall increase in the MgO values. This suggests the influx of more primitive magma.
The high peaks above 53 wt. % Cr2O3 with low wt. % MgO are Cr-enriched
ferrichromites due to secondary hydration. In the second zone, there are 2 pulses with the
second being larger, and having higher wt. % MgO and Cr2O3 than the second. Notably,
more secondary Cr-enriched ferrichromite has been detected in this first pulse. The
second pulse shows marked decreasing wt. % MgO with height while the Cr2O3 values
decrease to a lesser extent. The third zone contains 3 to 4 pulses on an overall trend of
decreasing Cr2O3 wt. % with height. The first pulse from 259 to 270 m contains higher
wt. % MgO than the others and is well differentiated. The second pulse is poorly
developed. The 3rd to 4th pulses from 272 to 276 m begin with more elevated MgO that
decreases past 274 m. The overall decreasing trend in Cr2O3 wt. % in this zone also
reflects igneous differentiation.
5.3.1.2 Black Thor BT-08-10
Black Thor DDH BT-08-10 contains chromite of more primitive but also more
variable composition due to diffusion processes accompanying greater ferrichromite
replacement during retrogression. Therefore, plots of core + margin of igneous chromite

161
have been separated from replacement ferrichromite. Cr/Fe ratios in the drill hole are
less for disseminated but more for primitive and higher grade overall than Black Label
with between 1.53 and 2.90 for magmatic compositions and as low as 0.74 for alteration
rim Cr-enriched to Cr-depleted ferrichromites (Fig. 5.28). Some Cr-enriched
ferrichromites in the upper part of the hole above 154 m have enriched Cr/Fe to the range
of 2.50 to 2.95, thereby increasing the grade of the ore. From 114 to 124 m there are two
zones of low MgO chromite disseminated in dunite (Figs. 5.29 to 5.30). The first zone
from 114 to 118.5 m, comprises two pulses with trends of decreasing wt. % MgO with
height. The second zone from 118.5 to 124 m also contains 2 pulses with decreasing wt.
% MgO with height.

Above 124 m, chromite shows elevated wt. % Cr2O3 in intermittent beds of
massive chromitite (Figs. 5.31 to 5.32). Between 124 and 127 m there is a well
differentiated sequence showing decreasing wt. % MgO and Cr2O3 with height. A large
zone of chromitite between 127 and 150 m can be subdivided into two zones from 127 to
136 m and 136 to 150 m based on Cr2O3 contents. These chromitites begin with high
Cr2O3 wt. % contents and show a marked trend of decreasing MgO and Cr2O3 with
height. In the first subzone, Cr2O3 contents reach 54 wt. % suggesting very primitive
magma.

The upper zone from 150 to 174 m, also show trends of decreasing MgO and
Cr2O3 wt. % with height. Notably, there is only a slight decrease in wt. % Cr2O3. This
may be explained by development of chromite convection cells. A number of
replenishments of high MgO may be also attributed to successive convection cells (Rice
and von Gruenewaldt, 1994). Also shown are variation of FeO, Al2O3 and Fe2O3 with
height (Figs. 5.33 to 5.35).

5.3.1.3 Black Thor BT-09-17
The Black Thor upper chromitite in DDH BT-09-17 displays trends in the mineral
chemistry of chromite that are different than DDH BT-08-10 and the other chromite
deposits. Instead of decrease in wt. % Cr2O3 and wt. % MgO from core to rim that is
most common with silicate exchange of chromite in the other deposits, there is
enrichment in wt. % Cr2O3 and wt. % MgO that effectively increases the grade of the ores
(Figs. 5.36 to 5.39). With enrichment in Cr2O3 and MgO, there is enrichment in Cr/Fe

174
from core to margin with ratios of between 1.88 and 2.44 for magmatic chromite (Fig.
5.40). In contrast to other drill holes, the Cr-enriched ferrichromites serve to enrich the
upper chromitites in Cr/Fe with compositions reaching up to 3.03 with retrogression. The
high Cr/Fe in the ferrichromites is due to the decrease in FeOT in these chromites.

In the drill hole sequence, there are two chromitite intervals, the first situated
between pyroxenite and gabbro and the second situated between gabbro and pyroxenite.
In the lower interval, from core to margin of the grains, there is an increase in Cr2O3,
Al2O3 and MgO while a decrease in FeOT that occurs due to silicate exchange with
retrogressive fluids. Evidence for retrogression is “zoning” toward the margins that also
occur along interior cracks and rims with associated alteration rim replacement chromite.
Along with these trends, retrogression has been observed with the occurrence of bright
alteration margins (similar to ferrichromite) with enriched 61.75 wt. % Cr2O3, low 6.45
wt. % Al2O3, low 4.62 wt. % MgO and elevated 23.84 wt. % FeOT. These are probably
Cr-enriched ferrichromites, although the ferric iron content is not as high.

Retrogression has also been observed with the occurrence of chrome chlorites and
tremolites with very little wt. % FeOT which could be interpreted as hydrothermal
tremolite in contrast with tremolite that results from the replacememt pyroxene. Also,
higher up in the second chromitite interval, the chromites are more diffused with
increased Cr2O3, Al2O3, but with decreased MgO to 4 to 6 wt. %. It appears that the
upper chromitites underwent higher temperature hydrothermal metamorphism to the
tremolite field in the lower parts but have been more retrogressed in the upper parts of the
upper chromitite. The lower T retrogression in the upper part is probably a later
hydration overprint. The chromites in the upper parts of the zone are more non-uniform,
broken up and enriched in silicate due to late influx of retrogressive fluids. In the two
intervals, since only 12 samples were analysed in the chromitite and the differentiation
and replenishment trends are masked by these retrogressive Cr2O3 and MgO enrichments,
primary igneous signatures are too overprinted to interpret any fine scale cryptic layering.

For variation of major oxides with depth, the lower chromitite interval from

296.30 to 298.80 m contains more primary chromite than the second interval. The
chromites show uniformity in the back scatter images with evidence for primary cores in
well zoned chromites. From 296.80 to 298.40 m, the samples begin with wt. % Cr2O3 at

176
49.59 wt. % Cr2O3 and increase upward to 52 to 54 wt. % Cr2O3 with retrogression.
MgO decreases from 7.95 to 6.62 wt. % MgO in the igneous cores but shows enriched
zonation on the margins to 9.01 wt. % MgO. Other trends include a decrease in wt. %
Al2O3 while increase in wt. % FeO in the igneous core from the first to the second sample
(Figs. 4.41 and 4.42). However there is an increase in wt. % Al2O3, while decrease in wt.
% FeO in the silicate exchanged zoned margins. The alteration rim chromites at 59.06
and 62.75 wt. % Cr2O3 have no wt. % Fe2O3 and low FeO at 23.41 and 24.61 wt. %.
The second chromitite interval is from 318.70 to 339 m. There are three
sequences as seen from the variation in wt. % Cr2O3 from the assays. In the microprobed
chromites, the first chromite sequence is from 319 to 324 m. There is a decrease in wt. %
Cr2O3 in the igneous cores going up the sequence, however, Cr2O3 contents are enriched
to up to 53.36 wt. % Cr2O3 on the diffused margins. MgO increases up to 9.69 wt. %
MgO with retrogressive silicate exchange. Within the overall second interval, alteration
rims report up to 68.03 wt. % Cr2O3 in chromite. Fe2O3 contents in the overall DDH BT09-
17 are more depleted than the Fe2O3 contents of the other drill holes (Fig. 4.43). The
second chromite sequence from 326 to 331 m shows an enrichment in wt. % Cr2O3 in the
cores followed by a decrease in wt. % Cr2O3. With retrogression, the margins are
enriched to 53.9 wt. % Cr2O3. MgO decreases from 7.72 to a low 3.69 wt. % MgO in the
cores along with margins. These chromites are not as uniform as the chromites in the
lower sequences, due to considerable fracturing and silicate exchange. It is interpreted
that primary compositions are not preserved. In the third chromite sequence from 334 to
338 m, MgO increases to 7.37 wt. % MgO probably due to a new pulse along with
retrogressive enrichment in wt. % MgO. Cr2O3 concentrations at 49.47 wt. % are not as
high, however, due to lack of primary chromite signatures. Notably, Fe2O3 becomes
more elevated from 3.14 to 4.47 wt. % Fe2O3 in these more evolved chromites.

5.3.1.4 Big Daddy
Before the main chromitite in Big Daddy DDH FW-08-19, there is a sequence of
dunite, heterogeneous pyroxenite and pyroxenite with intervening chromites. The
chromites microprobed in this section are usually disseminated chromites found in dunite
and sometimes pyroxenite. At 13.50 m depth, there is first a band of primitive chromite
in dunite that contains high wt. % Cr2O3 and MgO (Figs. 5.44 to 5.48). In contrast there

185
is low wt. % Al2O3 and FeO (Figs. 5.49 to 5.50). This chromite band is located in dunite
just above a small layer of pyroxenite and is interpreted to form due to the mixing of a
new dunite pulse with pyroxenite. Another such layer occurs at 20.10 m. At 16.07 m,
disseminated interstitial chromite in dunite is more evolved in composition with lower
wt. % Cr2O3 and MgO and higher wt. % Al2O3 and FeO. The dunite continues to 69.40

m. At first there is differentiation from 16.07 to 35.20 m toward lower wt. % Cr2O3 and
MgO with intervening pyroxenite. Then there is a new pulse of dunite after beginning
somewhere after 33.36 m with higher wt. % Cr2O3 and MgO at 55.62 m depth.
Pyroxenite begins after 64.00 m above a faulted contact with the dunite. Another pulse
of dunite occurs from 73.97 to 84.94 m and contains more primitive chromite at 75.36 m.
From 74.36 to 135.2 m, the interstitial chromite in the host units become steadily more
evolved as there is differentiated pyroxenite that grades into heterogeneous olivine
pyroxene to harzburgite. This represents a mixed unit interpreted to be caused by magma
mixing of a pulse of pyroxenite with dunite to form chromitite in an overlying pulse.
Compositions show increasing wt. % FeO, wt. % TiO2 while decreasing wt. % Al2O3 in
the pyroxenite (Fig. 5.51). Lower wt. % Al2O3 is due to retrogression in the pyroxenite.
From 141.50 to 144.14 m, there is a chromitite layer containing semi-massive chromitite
in cumulus pyroxene and olivine. The chromitite contains the highest wt. % Cr2O3 and
MgO with 53.45 wt. % Cr2O3 and 11.68 wt. % MgO making it the most primitive
chromitite in the sequence. Then compositions are lower again in an overlying
disseminated chromite-bearing dunite. The chromites then become progressively more
evolved from 144.50 to 182.40 m as the dunite grades into heterogeneous olivine
pyroxenite and in turn pyroxenite. Chromite in pyroxenite is vermicular in texture with
low wt. % Cr2O3 and MgO. Within this first sequence, there are ferrichromites that
contain higher wt. % Cr2O3 and wt. % Fe2O3 (Fig. 5.52).
The main Big Daddy interval begins at 183.80 m depth. It is all massive
chromitite and therefore demonstrates a markedly different compositional trend than
Black Thor and Label. MgO and Cr2O3 compositions are more uniform in the chromites
(Figs. 5.53 to 5.56). This is especially reflected in constant Cr2O3 from one zone to
another. The main chromitite interval in the hole is from 183 to 230 m and is divided
into 4 main zones as defined by troughs in wt. % MgO. With constant Cr2O3

194
compositions, Cr/Fe is consistent at 2.25 for magmatic chromite, but tapers off near the
upper contact with pyroxenite to lower Cr/Fe of down to 1.17 (Fig. 5.57). Minor
variability in Cr/Fe is due to more variable wt. % MgO or FeO (Fig. 5.58). Cr-enriched
ferrichromite where present enriches the Cr/Fe ratio. The first zone from 183 to 192 m,
begins with two minor replenishments in wt. % MgO followed by decreasing wt. % MgO
with height from 187 to 192 m. Chromite compositions are at 51 wt. % Cr2O3. The
second zone from 192 to 206 m, begins with a pulse from 192 to 194 m at lower wt. %
MgO followed by three successive pulses beginning at 11.46 wt. % MgO that decreases
successively upward. Chromite compositions are constant at 50 wt. % Cr2O3. The third
zone from 206 to 227 m, starts with a pulse at 11.27 wt. % MgO that decreases with
height from 206 to 211 m. From 211 to 227 m there is a large well defined
differentiation sequence. Chromite compositions decrease subtly from 51 to 47 wt. %
Cr2O3 as the interval approaches the upper contact with pyroxenite. From 227 to 230 m
is a contact zone with a pronounced decrease to 3 wt. % MgO and 41 wt. % Cr2O3 toward
the contact. This zone is probably depleted due to silicate exchange with pale grey to
white globular shaped aggregates of pyroxene. Also, there is more ferrichromite in this
zone indicating higher degrees of hydration.

Al2O3 contents show a different pattern of variation in the Big Daddy interval.
For wt. % Al2O3, the interval can be divided into three zones from 183 to 203 m, from
203 to 216 m and from 216 to 230 m (Fig. 5.59). The first zone shows a general trend of
slightly increasing wt. % Al2O3 from 13.14 to 14.85 wt. % Al2O3. These contents are
antipathetic the decreasing differentiation trend of the Cr2O3 contents. From 203 to 216
m, the Al2O3 contents first decrease and then increase in a concave pattern, due to
replenishment followed by differentiation. Then from 216 to 230 m, there is another
general increase in wt. % Al2O3 toward the contact with differentiation and silicate
exchange with pyroxenite. The difference between the Al2O3 and MgO trends is due to
less variation of Al2O3 and Cr2O3 within the complete convection cycles in massive
chromitite compared to the more variable pattern of the Black Label and Thor intervals.
Ferrichromites that are plotted have very low wt. % Al2O3. For wt. % Fe2O3 variation,
contents are below 10 wt. % Fe2O3 and therefore do not show the retrogression to Cr-
depleted ferrichromite as in Black Thor and Label (Fig. 5.60).

199
5.3.2.1 Black Label binary chromite chemistry
The Black Label chromites show interesting trends in terms of wt. % Cr2O3 vs.
wt. % MgO. Within DDH BT-09-31, two separate chromitite intervals are delineated as
Layer 1 and Layer 2 (Figs. 5.61 to 5.62). Overall, there is a well defined positive
correlation of increasing wt. % Cr2O3 with increasing wt. % MgO. Layer 1 is the bottom
chromitite horizon from 161 to 203 m and is characterized by both lower and higher
trends of increasing wt. % Cr2O3 with wt. % MgO. Layer 1 overlaps Layer 2 on the
higher trend since here it represents the primary cores of the more massive chromitites
that show igneous evolution from high wt. % Cr2O3 and MgO to lower wt. % Cr2O3 and
MgO. Although, Layer 1 also plots on the lower trend because there is more
differentiation to lower wt. % Cr2O3 and wt. % MgO in the disseminated chromites of
this sequence vs. the more primitive larger grains of the massive chromites.

A general observation of the Black Label chromites is that chromitites are not as
high grade as that of Black Thor and Big Daddy. This is due to the amount of
intercumulus pyroxene content in the ore that causes the chromites to be more silica-
enriched than the more primitive Black Thor and Big Daddy chromites. In the lower left
of the plot, a number of Cr-depleted ferrichromites have been detected that have low
MgO and a drop in Cr2O3 compared to the other chromites. In contrast, Cr-enriched
ferrichromites are plotted off the trend and contain abnormally high wt. % Cr2O3 but low
wt. % MgO.

There are several paths for chromite evolution as the primary grains undergo
diffusion at their margins and in turn contain alteration replacement rims with
retrogression. One path is from Layer 1 (chromite evolution 1). First the chromite
crystallized out of the melt to form the primary core composition. With diffusion
towards the margin, Mg and Cr contents are leached and exchanged with surrounding
silicate. In turn, the chromite is retrogressed to a very MgO and Cr2O3-depleted
ferrichromite at the rim. Another common example is that of chromite evolution 2 where
an original chromite grain undergoes silicate exchange/diffusion at the margin thereby
leaching both Cr and Mg components, but gaining Al and Fe components. Another path
that could happen involves a chromite in Layer 2. A more primitive chromite is
crystallized out of the melt. As it undergoes diffusion, Cr is again leached, but this time,

Figure 5.61. Binary plot of Cr2O3 vs. MgO wt. % for Black Label DDH BT-09-31 with
paths of chromite evolution shown.
Figure 5.62. Black Label layers 1 and 2 of DDH BT-09-31. The primary, higher Cr2O3
and MgO cores of massive chromite from layer 1 are overlapped by the chromites of
layer 2.
0
10
20
30
40
50
60
70
0 2 4 6 8 10 12
Cr2O3 wt. %
MgO wt. %
Series1
Chromite evolution 1
Chromite evolution 2
Chromite evolution 3
0
10
20
30
40
50
60
70
0 2 4 6 8 10 12
Cr2O3 wt. %
MgO wt. %
Layer 1
Layer 2
200

201
Mg is gained. Although there are sometimes increases in Mg and Al or sometimes even
increases in Cr, the path mostly taken is that of diffusion to leach Cr and Mg and gain Al
and Fe to eventually be replaced by ferrichromite. So this grain is eventually replaced by
a Cr-enriched and high ferric iron-bearing ferrichromite as the last composition on the
replacement rim.

For wt. % Al2O3 vs. wt. % MgO variation, wt. % Al2O3 is not well correlated with
wt. MgO, but more or less shows a constant composition for the primitive chromite
compositions as seen by the overlap of Layers 1 and 2 at lower wt. % Al2O3 and higher
wt. % MgO (Fig. 5.63). In Layer 1, many of the more disseminated chromites contain
higher wt. % Al2O3 reflective of silicate exchange with interstitial pyroxene. There is a
well defined positive correlation in the transition of the chromites to Cr-enriched to Cr-
depleted ferrichromites. With increasing Fe2O3, there is a great decrease in wt. % Al2O3
with substitution. Therefore, the Cr-enriched to Cr-depleted ferrichromites show a
substantial decrease in wt. % Al2O3.

FeO shows a well defined correlation antipathetic to MgO (Fig. 5.64). With both
diffusion and differentiation of the primary chromites, there is an increase in wt. % FeO
from core to margin to Cr-enriched or Cr-depleted ferrichromite and from massive to
disseminated chromites that have undergone more silicate exchange.

A Binary plot of wt. % TiO2 vs. wt. % Fe2O3 demonstrates the behaviour of Fe vs.
Ti in the Fe-Ti trend (Fig. 5.65). Most of the samples plot as a cluster with low wt. %
TiO2 at low wt. % Fe2O3. With fractionation of olivine or pyroxene from the magma, the
Fe/Mg ratio and Ti contents of the melt increase so there is enrichment of these elements
in the more differentiated chromites (Barnes and Roeder, 2001). The trend is then
accentuated by the reaction of the chromites with the intercumulus magma to produce the
high TiO2-bearing Cr-depleted ferrichromites (Barnes and Roeder, 2001). With
continuation toward magnetite, the wt. % TiO2 contents decrease again at the highest wt.
% Fe2O3. This trend is common to chromites of MORB basalts and also stratiform
layered intrusion chromitites.

For binary plots of metals, wt. % TiO2 shows a subtle negative correlation with
increasing wt. % Cr2O3 since there is more wt. % TiO2 in the differentiated chromites
(Fig. 5.66). There is a large increase in wt. % TiO2 toward the Cr-depleted

204
ferrichromites. For wt. % TiO2 vs. wt. % FeO, there is a well defined igneous
fractionation trend of increasing wt. % TiO2 with wt. % FeO (Fig. 5.67). Above this
trend are TiO2-enriched Cr-depleted ferrichromites that have high wt. % FeO. For wt. %
ZnO vs. wt. % Cr2O3, the chromites are separated into clusters for Layers 1 and 2 (Fig.
5.68). Layer 1 overlaps the higher and lower wt. % ZnO clusters at low and high wt. %
Cr2O3 respectively, while Layer 2 overlaps the lower wt. % ZnO at higher wt. % Cr2O3.
The decrease in wt. % ZnO with increasing wt. % Cr2O3 is due increase in ZnO with
differentiation. For wt. % NiO vs. wt. % Cr2O3, NiO correlates with Cr2O3 in two layers
(Fig. 5.69). Layer 1 has lower wt. % NiO at lower wt. % Cr2O3 than Layer 2.

5.3.2.2 Black Thor BT-08-10 binary chromite chemistry
Black Thor DDH BT-08-10 displays similar variation to Black Label, with more
Cr-enriched ferrichromites analysed along with Cr-depleted ferrichromites. On a wt. %
Cr2O3 vs. wt. % MgO diagram, there is a well defined correlation of wt. % Cr2O3 with
MgO from the primitive to the differentiated chromites (Fig. 5.70). Typical paths of
chromite evolution are displayed similar to Black Label. The Cr-depleted ferrichromites
plot off the trend at lower wt. % Cr2O3 and wt. % MgO and the ferrichromites plot off the
trend with high wt. % Cr2O3 at lower wt. % MgO. The Black Thor chromites are the
most primitive with compositions reaching 54 wt. % Cr2O3 and 12 wt. % MgO which are
even higher than Layer 2 of Black Label. Although primitive, there is still variation from
massive to disseminate chromites that characterize the igneous evolution of other
stratiform layered intrusions such as the Great Dyke (Wilson, 1982).

For wt. % Al2O3 vs. wt. % MgO, Black Thor shows the same trends as Black
Label with a constant Al2O3 composition for the primitive chromitites and diffusing to
higher wt. % Al2O3 at the margins (Fig. 5.71). The Cr-enriched to Cr-depleted
ferrichromites plot on a well defined trend of decreasing Al with substitution of Fe3+. For
wt. % FeO vs. wt. % MgO, there is a well defined negative correlation with substitution
from the massive to disseminated chromites. Notably, the wt. % FeO contents are lower
in Black Thor than Black Label (Fig. 5.72).

For binary plots of metals, wt. % TiO2 shows a subtle negative correlation with
wt. % Cr2O3 (Fig. 5.73). The TiO2 compositions of Black Thor are lower than Black
Label. Also displayed are the high TiO2 Cr-depleted ferrichromites at low wt. % Cr2O3

209
and the low TiO2 ferrichromites at high wt. % Cr2O3. Wt. % ZnO increases with
decreased wt. % Cr2O3 due to differentiation (Fig. 5.74). The ZnO contents are lower
than ZnO of Layer 1 in Black Label. The NiO contents of Black Thor are noticeably
lower than Black Label for both layers of Black Label (Fig. 5.75. Wt. % MnO shows a
slight negative correlation with wt. % Cr2O3. This is due to MnO increasing with
differentiation (Fig. 5.76).

5.3.2.3 Black Thor BT-09-17 binary chromite chemistry
The upper chromitite of DDH BT-09-17 show similar binary variation of major
oxides as the other chromite deposits but contains trends of chromite enrichment rather
than depletion due to retrogression. On a wt. % Cr2O3 vs. wt. % MgO diagram, there is
increased wt. % Cr2O3 with wt. % MgO similar to the other deposits, only the chromites
evolve in the direction from lower to higher wt. % Cr2O3 and wt. % MgO with
retrogression (Fig. 5.77). This can be seen in the chromite evolution 1 trend on the
diagram where core to margin compositions increase from 51.70 to 52.21 wt. % Cr2O3 in
one of the grains. The later alteration rims of the chromites have even higher wt. %
Cr2O3 compared to the Cr-enriched ferrichromites in the other deposits. Chromites
enrich to as high as 68.03 wt. % Cr2O3. Notably, there are two separated chromite
composition clusters on the diagram. Most of the chromites contain more primitive and
higher wt. % Cr2O3 and wt. % MgO while the lower compositions are from more evolved
chromites higher up in the second chromitite interval in the drill hole.

For wt. % Al2O3 vs. wt. % MgO variation, there are trends of increasing wt. %
Al2O3 with wt. % MgO from the cores to rims due to retrogression (Fig. 5.78). Al2O3
compositions are higher compared to the other chromites of Black Thor DDH BT-08-10
to as high as 18.57 wt. % Al2O3. This higher Al2O3 content is probably due to
enrichment of Al2O3 with higher retrogression that overprints the primary chemistry.
From primary chromite core to alteration rim, there is a well defined positive correlation
of decreasing wt. % Al2O3 with decreasing wt. % MgO. This trend shows these rim
chromites are behaving the same as Cr-enriched to Cr-depleted ferrichromites in the other
deposits ie. Al is substituting with Cr. For wt. % FeO vs. wt. % MgO variation, there is a
well defined negative correlation of wt. % FeO and MgO that is characteristic of all the

213
deposits (Fig. 5.79). Notably, the alteration rim chromites are even more depleted in wt.
% FeO and fall off the trend with decreasing wt. % MgO.

For other oxides, wt. % TiO2 increases with decreasing wt. % Cr2O3 (Fig. 5.80).
Therefore, wt. % TiO2 does not increase with retrogression from core to margin in the
chromites. ZnO is variable but also increases with decreasing wt. % Cr2O3 (Fig. 5.81).
NiO is low in these chromites since the pyroxenites are not elevated in Ni ppm (Fig.
5.82). MnO increases with decreasing wt. % Cr2O3 like the other oxides (Fig. 5.83).

5.3.2.4 Big Daddy binary chromite chemistry
The Big Daddy chromites show relatively uniform compositions for major
element and metals in contrast to the other deposits. For wt. % Cr2O3 vs. wt. % MgO
variation, there is a positive linear correlation of increasing wt. % Cr2O3 with increasing
wt. % MgO in the igneous chromites (Fig. 5.84). The lower wt. % MgO-bearing
chromites have more scattered wt. % Cr2O3 contents than most of the chromites in the
high MgO region. These chromites are from disseminated chromites hosted as minor
cumulus phases in the dunites, heterogeneous pyroxenites and pyroxenites located below
the main massive chromitite. The different contents of these chromites is due to
differentiation in those pulses. Then from 7.33 to 11.68 wt. % MgO, there are chromites
in the massive chromitite that plot on a well defined trend of increasing Cr2O3 with MgO.
The slope of the trend is small compared to the other chromite deposits since there is not
as much variation in the more complete convection cycles of these massive chromites. A
few chromites plotting from 35 to 40 wt. % Cr2O3 are from the more retrogressed
chromites in the pyroxenites. Also plotted are a few Cr-enriched ferrichromite with high
wt. % Cr2O3 contents.

For wt. Al2O3 vs. wt. % MgO variation, most of the Al2O3 contents are constant
with respect to wt. % MgO since there is little pyroxene to promote pyroxene-chromite
substitution of Al2O3 (Fig. 5.85). The Al2O3 contents plot from 12 to 14 wt. % Al2O3
with lesser variation for the massive chromitite interval. The Al2O3 contents are lower
than Black Label and Black Thor since there is less differentiation. Notably, wt. % Al2O3
does not plot above 16 wt. % Al2O3 as it does in the other deposits, even in the
disseminated chromite. The disseminated and massive chromites have compositions
from 11 to 15 wt. % Al2O3. However, Al2O3 is higher in the intermediate chromitite at

218
161.50 m depth. In the samples with more intermediate modal % chromite i.e. chromite
ranging in between massive and disseminated chromite, the chromitites are hosted by
heterogeneous pyroxenite and dunite. The chromitites probably mineralized in a magma
driven toward more pyroxene stability rather than being constantly primitive due to
repetitive replenishment of chromite pulses that are closer to olivine stability as in the
massive chromitite interval. And the disseminated chromites primarily mineralized in
cumulus olivine dunite sequences where there is less Al2O3 content. Notably, there is
lower wt. % Al2O3 in the disseminated chromites while higher wt. % Al2O3 in the
intermediate chromites of e.g. Black Thor which supports this observation.
For wt. % FeO vs. wt. % MgO, there is similar separation of disseminated vs.
massive chromite regions that are visible in the wt. % Cr2O3 vs. wt. % MgO variation
diagrams (Fig. 5.86). There is a general well defined trend of decreasing wt. % FeO with
increasing wt. % MgO with substitution of the elements from more primitive to
differentiated chromites. From 7.33 to 11.68 wt. % MgO, there is a large bunch of
analyses with lower wt. % FeO that represent the massive chromites.

For binary plots of metals, there is a slight negative correlation of decreasing wt.
% TiO2 with increasing wt. % Cr2O3 with evolution of the chromites (Fig. 5.87). Higher
wt. % TiO2 samples represent evolved chromites of the disseminated chromite-bearing
host lithologies located beneath the main zone. The negative correlation is also reflected
in the wt. % ZnO vs. wt. % Cr2O3 (Fig. 5.88). The ZnO contents are elevated to 0.2 wt.
% ZnO as in other deposits except for Layer 1 of Black Label. There are many samples
of elevated ZnO above 0.2 wt. that reflect the more differentiated chromites in the host
rocks below the main chromitite. The wt. % NiO vs. wt. % Cr2O3 shows a well defined
correlation of increasing wt. % NiO with increasing wt. % Cr2O3 reflecting the igneous
variation of the chromites (Fig. 5.89). NiO contents are high to 0.4 wt. % NiO which is
similar to the higher wt. % NiO of Layer 2 in Black Label. The high NiO contents reflect
the predominance of primary chromite that is present at these stratigraphic levels of Big
Daddy and Black Label. MnO clusters at between 0.4 and 0.8 wt. % MnO at 50 wt. %
Cr2O3 (Fig. 5.90). There is also a negative correlation of decreasing wt. % MnO with
decreasing wt. % Cr2O3 reflecting higher MnO in the more differentiated disseminated
chromites.

222
5.4 Laser ablation ICP-MS analysis of chromite
Laser ablation ICP-MS analysis was carried out on chromites from three drill
holes from the three deposits: Black Label DDH BT-09-31, Black Thor DDH BT-08-10
and Big Daddy DDH FW-08-19. There were 142 laser point analyses taken from 35
samples with up to 5 to 6 analyses taken per sample. The goal of the laser ablation work
was to characterize the trace element signatures and variability of the three deposits with
possible insights into using these signatures for an exploration vector. Trace elements of
Sc, Ti, V, Mn, Co, Ni, Zn, Ga are reported and plotted on chromite normalized to
chromite in MORB trace element plots. Binary variation of these elements with Cr is
reported below. Another output of the analysis is an analysis of Ru, Rh, Pd, Os, Ir and Pt
PGE in the deposits. However, the PGE in most of the samples are below detection
limits, so they are not reported below. See Appendix 6 for the total suite of elements
analysed by laser ablation.

5.4.1 Chromite/Chromite in MORB trace element plots
The laser geochemical results of the three deposits were analysed at the GSC
facility in Ottawa May 16 to 18 and December 18 to 21, 2012. Results were first
organized on an excel spreadsheet with care to subtract bad analyses. Chromite/chromite
in MORB-normalized diagrams were then plotted for a useable suite of elements based
on Pagé’s work on the Thetford chromitites (Pagé, 2009).

The MORB chromite normalized patterns of the chromites reflect that of layered
intrusion chromitites with large positive Ti anomalies and increased Fe contents and large
negative Sc anomalies. There is also evolution in the patterns from more primitive
komatiite to more evolved intrusion patterns where komatiites typically contain lower but
positive Ti, negative Ni and negative Sc anomalies (Pagé and Barnes, 2012). The Black
Label chromitites have high positive Ti anomalies indicating fractionated magma
chemistry (Fig. 5.91). Zn and Co are elevated, again indicating these chromitites being
more evolved. The Black Label chromitites are highest in Fe content and lowest in Mg
content. There is more elevated Zn content in the disseminated chromite of Black Label.
There are distinct negative Ni anomalies at Black Label in contrast to the other
chromitites which indicates these chromitites are more evolved.

224
At Black Thor, there are 2 subsets, a more differentiated and primitive sample
(Fig. 5.92). The primitive komatiitic sample has a lesser positive Ti anomaly and lesser
Zn and Co similar to the Great Dyke pattern, though being enriched in Fe (Jiménez et al.,
2012). The more differentiated suite has a greater positive Ti anomaly with greater Zn
and Co, more like Bushveld. V contents of the chromitites are high, in common with
layered intrusion chromites in contrast to more primitive komatiite chromites.

The Big Daddy chromitites consistently show positive Ti anomalies, but contain
the most depleted Zn and Co, probably reflecting their primitive nature (Fig. 5.93). They
are not, however, as primitive as the first subset of Black Thor. Notably, the Sc contents
are more elevated. Mn contents are higher in Big Daddy and Black Label than Black
Thor since they are more differentiated.

5.4.2 Binary trace element variation
The chromitites show trends of the elements vs. Cr that are indicative of
fractionation from the more massive to disseminated chromites. Fractionation trends are
displayed by increases of Ti, V, Co, Ga, Zn, Mn vs. Cr while decreases in Ni and Sc vs.
Cr. Specific results from the three deposits are presented below.

The Black Label chromitites show the most fractionated magma chemistry of the
three deposits (Fig. 5.94). Trace element concentrations include 2350 to 6012 ppm Ti,
794 to 1448 ppm V, 516 to 2392 ppm Zn, 2086 to 3016 ppm Mn, and 110 to 542 ppm Ni.
For binary variation, fractionation trends are displayed by negative correlations of Zn, V
and Mn with Cr and a positive correlation of Sc with Cr. Sc behaves incompatibly
similar to Ni in these deposits. Ni appears to show a positive correlation and generally
increases with Cr. Although showing fractionation with depleting trends of Cr in
komatiitic chromites such as Alexo, Ga shows an enriching trend suggestive of it
behaving incompatibly like Ni and Sc (Méric et al., 2012). Ga shows this positive
correlation in all the deposits. Ti and Co vs. Cr plots no significant trend.

The Black Thor chromitites are the most primitive of the deposits with trace
element concentrations that include 1125 to 2792 ppm Ti, 819 to 1277 ppm V, 575 to
1577 ppm Zn, 1125 to 2792 ppm Mn, and 526 to 1112 ppm Ni (Fig. 5.95). For binary
variation, fractionation trends are displayed by negative correlations of Ti, Zn, Mn and
Co with Cr and positive correlations of Ni and Sc with Cr. Ti shows two negative

225
0.1
1
10
Al
Ga
Ti
Ni
Mg
Zn
Co
Mn
FeOT
V
Sc
Cr
Chromite
/
Chromite
in
MORB
Figure 5.93. Chromite in MORB normalized trace element plot of Big Daddy DDH
FW-08-19. Normalizing values of Pagé and Barnes (2009).

226226
Figure 5.94. Binary plots of Cr vs. Ti, V, Zn, Mn, Ni, Co, Sc and Ga ppm for Black
Label DDH BT-09-31.

227227
Figure 5.95. Binary plots of Cr vs. Ti, V, Zn, Mn, Ni, Co, Sc and Ga ppm for Black
Thor DDH BT-08-10.

228
correlation trends for higher and lower Ti concentrations representative of two different
sample subsets of the deposit, one being more primitive than the other. Zn and Mn show
well defined correlations. V appears to show a weak negative correlation. Ga again
shows a negative correlation. Ni and Sc also show well defined positive correlations
indicative of fractionation.

The Big Daddy chromitites show less but similar variability as the other deposits
(Fig. 5.96). Trace element concentrations include 2336 to 3923 ppm Ti, 940 to 1425 ppm
V, 381 to 769 ppm Zn, 1758 to 3209 ppm Mn, and 668 to 1482 ppm Ni. Ni is higher and
reflects the primitive character of the deposit like Black Thor. Mn contents are higher
than the other deposits. Many of the Ni contents are high since the samples are all from
massive chromite. For binary variation, correlations are less well defined but show
negative correlations for Ti, Zn and possibly Mn with Cr. Correlations are positive for Ni
and Sc with Cr. Ga shows a variable but negative correlation.

230
CHAPTER 6
DISCUSSION

6.1 Introduction
For discussion of the McFaulds Lake deposits, the chromites are first plotted on
tectonic discrimination diagrams to compare the chromites with other deposits of the
world and indicate the type setting. Origin of chromite as it pertains to these deposits is
then discussed in terms of an evaluation of Irvine’s (1975) model, followed by a
discussion of silicate inclusions leading up an evaluation of Irvine’s (1977) proposal for
chromite genesis. Magma mixing is proposed for origin and is further refined by
advocating the double diffusive convection model. Postcumulus chromite growth is then
discussed and an evaluation is made of the conduit theory for chromite origin. Finally,
the late hydration overprint is discussed in terms of chromite ore modification.

6.2 Tectonic discrimination of chromite
6.2.1 The Cr# vs. Mg# plot
Chromites can be distinguished between komatiitic, layered intrusion and other
environments such as ophiolitic by means of the Cr# vs. Mg# catio ratio plot (Figs. 6.1
and 6.2). In comparison to other chromites of the world, the McFaulds Lake chromites
plot well in the fields of stratiform mafic intrusions and komatiite with the exception of
the ferrichromites. In comparison to komatiite chromites, the McFaulds Lake chromites
are similarly high in Cr/Al for the most primitive chromites. The primitive chromites of
McFaulds Lake are most similar to the Great Dyke chromites. Other komatiitic
chromites such as those from the Selukwe dataset, the Hartley Complex and the Wedza
Complex and the Shurugwi dataset are however, slightly more Cr/Al-rich due to high Cr
and low Al and more Mg-rich. There is not much pyroxene in the komatiitic magmas to
exchange Al into the chromite structures. Also, lack of differentiation tends to make
these deposits plot at a higher Mg composition. There is still substantial variation in Mg#

Figure 6.1. Cr # vs. Mg # plot of McFaulds Lake chromites with other layered intrusion
and komatiite chromites of the world. World chromite data is from Barnes and Roeder
(2001).
Figure 6.2. Cr # vs. Mg # plot of McFaulds Lake chromites with other chromite deposits
of the world. World chromite data is from Barnes and Roeder (2001).
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
0.8
0.9
1
1 0.8 0.6 0.4 0.2 0
Cr/(Cr+Al+Fe3+)
Mg/(Mg+Fe2+)
Layeredintrusion Greenschistkomatiite McFauldsLakeDeposits
0.00
0.10
0.20
0.30
0.40
0.50
0.60
0.70
0.80
0.90
1.00
1.00 0.80 0.60 0.40 0.20 0.00
Cr/(Cr+Al+Fe3+)
Mg/(Mg+Fe2+)
McFauldsLake
Deposits
Selukwe
Hartley
Wedza
Bushveld
GreatDyke
Shurugwi
Kemi
Inyala
231

232
in the Great Dyke deposits, but only up to a Mg# composition of 0.218. The McFaulds
Lake deposits then follow a trend toward decreasing Cr# with decreasing Mg# as in
evident in other stratiform layered intrusions. However, other stratiform complexes that
follow this trend do not plot at high Cr# and high Mg# compositions. A similar
stratiform complex that follows a trend of decreasing Cr# with decreasing Mg# is the
Bushveld Complex. Although having the same trend, the Bushveld chromites have
overall lower Cr# than McFaulds Lake. The lower Cr# of Bushveld is due to the
predominance of pyroxene to exchange Al with the chromite to lower the Cr#.

With increasing differentiation i.e. as the chromites go to lower Mg# composition
along the increasing Fe-Ti trend, there are lower Cr#s in the McFaulds Lake chromites.
Since there is a strong correlation of decreasing Cr# with decreasing Mg# in the
McFaulds Lake chromites, this would indicate magmatic evolution typical of a
differentiated intrusion. The McFaulds Lake deposits plot on an overall trend of
primitive komatiite to more differentiated with increasing Fe-Ti and finally to more
pyroxene-dominated differentiated compositions. The primitive McFaulds Lake
chromites are similar to the Great Dyke komatiitic chromites; they become more
differentiated along an increasing Fe-Ti trend similar to Great Dyke followed by
Bushveld; and then decrease Cr# with differentiation and pyroxene fractionation similar
to Bushveld chromite.

Another thick chromitite deposit, the Kemi Intrusion chromitite deposit is plotted
for comparison. Although similar in thickness, the Kemi deposit is lower in grade at
lower Cr# than the McFaulds Lake deposits and rather plots similar to the Bushveld
complex. For comparison to the main chromites, the Cr-enriched to Cr-depleted
ferrichromites of McFaulds Lake are also plotted. There is a much larger dataset for
these secondary chromites in McFaulds Lake than for other chromites of the world.
Unusual trends in Cr# enrichment with decreasing Mg# is evident in the Cr-enriched
ferrichromites which is significant for higher grade chromite ores. The trend toward Cr-
enrichment occurs with retrogression of the chromite rims. In contrast to Cr-enrichment,
retrogression also produces a secondary chromite trend to low Cr# compositions with low
Mg# in the Cr-depleted ferrichromites.

233
6.2.2 The Ternary Cr-Fe3+-Al plot
The ternary Cr-Fe3+-Al plot is also used for tectonic discrimation of chromites.
On a Cr-Fe3+-Al plot, the McFaulds Lake deposits plot well in the field for komatiites and
in the komatiitic part of the layered intrusions (Fig. 6.3). They plot near the corner of
high Cr but lower Fe3+ and low Al. The lower Fe3+ and Al is typical of low Al-bearing
undifferentiated komatiites. Although lower in Fe3+, there is still more Fe3+ in the
McFaulds Lake chromites than in the komatiite chromites. This is similar to the Mg#Cr#
diagram in that the McFaulds Lake deposits follow an Fe-Ti trend with more
differentiation than komatiite chromites. However, the broad overlap of the McFaulds
Lake deposits with the komatiite field clearly shows the deposits have komatiite affinity

i.e. primary chromite of komatiite composition. Like the Cr#-Mg# plots, there are also
fields for the Cr-enriched to Cr-depleted ferrichromites. All the secondary chromites plot
with low Al since Al is either substituted for Cr or Fe3+ in the chromite structure. The
Cr-enriched ferrichromites plot at compositions intermediate between Cr and Fe3+ while
the Cr-depleted ferrichromites plot toward the Fe3+ end. There is a subset of high Cr, low
Fe3+ and low Al ferrichromites near the Cr apex of the plot. These represent the Cr-
enriched ferrichromites of the upper chromitite of DDH BT-09-17 that follow a different
trend than the other secondary chromites of the other deposits.
6.3 Origin of chromite: An Evaluation of Irvine’s 1975 model
The origin of the McFaulds Lake chromite deposits is linked to the petrography
and geochemistry of the host rocks and ores themselves. The deposits as a whole may be
classified with stratiform magmatic Cr/PGE ores in layered complexes (Duke, 1988).
Stratiform chromite deposits are formed by magmatic segregation during fractional
crystallization (fractionation) of mafic-ultramafic magma. The precise reasons why
massive chromite cumulate layers form have not been entirely understood. In the first of
Irvine’s models (Irvine, 1975) he suggested a mechanism whereby a chromite saturated
picritic tholeiite liquid becomes more siliceous by contamination (assimilation) with
granitic material or alternatively by blending with a more siliceous differentiate of the
parent magma, thereby causing chromite to precipitate. In this model, the original
magma is contaminated while coprecipitating olivine and minor chromite. A period

Al2O3 0.0 0.1 0.2 0.3 0.4 0.5 0.6 0.7 0.8 0.9 1.0
Fe2O3
0.0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
0.8
0.9
1.0
Cr2O3
0.0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
0.8
0.9
1.0
Layered intrusion
Greenschist komatiite
McFaulds Lake deposits
Figure 6.3. Ternary Cr-Fe3+-Al plot of the McFaulds Lake chromites with other layered
intrusion and komatiite chromites of the world. World chromite data is from Barnes and
Roeder (2001).
234

235
follows when chromite precipitates alone, and then, because the liquid is enriched in
silica, orthopyroxene crystallizes instead of olivine (Irvine, 1975).

In the case of the McFaulds Lake deposits, initial crystallization of an olivinechromite
cumulate is indicated by dunite with disseminated chromite followed by the
transition into massive chromite alone. However, what is not explained by this model is
how the magma migrates into chromite-alone stability. It is assumed that this occurs with
decreasing temperature as this is the dominant control of fractional crystallization.
However, this does not explain the sudden onset of massive chromite from the
disseminated chromite-bearing dunite. The magma needs to be directly shifted into the
chromite-only field. A mechanism for driving melt chemistry from the chromite-only
field to pyroxene is by crustal contamination. A contaminant would raise the silica
content of the olivine magma so that it shifts directly into chromite stability. This would
ideally work in the case of a chromite-laden pulse of magma after crystallization of
chromite and olivine, that injests some silica-rich country rock to directly raise the silica
of the melt to pyroxene stability. Although this model explains the transition of olivine to
massive chromite, there is no explanation for the sudden break from chromite back into
the pyroxene stability field. In other words, there are two modes of magma emplacement
occurring one after the other which is an unlikely scenario. The appearance of
intermittent chromitite beds after disseminated chromite suggests that there were
intermittent pulses of magma to separate out chromite layers rather than a single magma
batch being fractionated into chromite stability. There must have been episodic pooling
and dithering of the magma to the right composition to cause the rainout of chromite
layers eventually forming the massive chromitite zone.

There are several problems with Irvine’s 1975 model. As suggested by Irvine
(1977) and Mondal (2010), it takes an enormous amount of silica to migrate the melt to
pyroxene stability. Rollinson (1997) in his discussion of the komatiitic chromites in
Inyala, Zimbabwe, counters this argument by saying that for komatiitic melts, the melts
have a high melting temperature sufficient to assimilate silica in the formation of
chromite from olivine along with the later surrounding pyroxenites. There the
pyroxenites are in the transition zone of dunite with country rock. In McFaulds Lake, the
chromite compositions plot similarly to komatiitic chromites of the Great Dyke yet

236
contain pyroxenites similar to the intrusion in Inyala. Also, from the primitive mantle
multielement plots, it can be observed that the dunites are of komatiitic affinity, with
crustal contamination signatures evident of incorporation of TTG. However, the
pyroxenites at McFaulds Lake appear to contain pyroxenite in an ordered layered series
from dunite to pyroxenite with leucogabbro melted roof rock. From the primitive mantle
multielement plots, it can be seen that the pyroxenites appear to be originated from
komatiitic melts that have been contaminated by TTG, similar to dunite but with more
contamination. However, both are part of the same series of intrusives that have
incorporated TTG. Since there was inheritance of a crustal contamination signature in
the dunite below the chromite intervals, this would suggest that TTG assimilation was
already inherent in the magmas before chromite crystallization.

The leucogabbro has been argued as to not be a part of the layered series but as
melted roof rock to the intrusion. True, the leucogabbro has distinct evolved signatures
from the dunite and pyroxenite; however, there also appears to be a crustal contaminant
signature of TTG in the leucogabbro as well. In drill core, the leucogabbro contains
textures of large scale silicification of an original gabbro that are probably from the
injestion of TTG or other country rock since these are non-igneous. However, this
implies that the gabbro existed and was overprinted by silicification, not that the gabbro
itself originated as a result of silicification. Roof rock assimilation is evidenced by
typical granophyric textures of coarse pink K-spar patches that occur in some of the
feldspathic zones. Therefore the upper gabbro likely developed as a “typical
granophyres” in the roof of the intrusion. It represents the crustally contaminated border
of the intrusion and not the pyroxenite. Other clues to it being the roof of the intrusion
are its large extent in the Ring of Fire intrusion and its abrupt change from pyroxenite, as
opposed to it being a gradational replacement zone. Therefore, since the pyroxenite is
not located at the contact of the wallrock, it is probably not a transition replacement zone
of chromite with wall rock as implied for the origin of komatiitic chromite in Inyala by
Rollinson (1997).

Another problem with the Irvine (1975) model is that it is only applied to cases of
silica addition. Often in chromitites, there is the sequence of dunite to chromitite to
pyroxenite which implies a migration of the melt with lowering of temperature and silica

237
contamination from olivine to chromite to pyroxene on the liquidus. However, not all
chromitites occur in this sequence order. In the second layer of Black Label, there is
pyroxenite before the chromitite which is followed in turn by oikocrystic harzburgite and
dunite. In the first layer of Black Label DDH BT-09-31, the oikocrystic harzburgite is a
transitional unit with crystallization of more intercumulus pyroxene from dunite to
pyroxenite. In the second interval of that drill hole however, the oikocrystic unit is
transitional from pyroxenite to oikocrystic unit/chromitite to dunite with a small pulse of
dunite in between the pyroxenite and oikocrystic unit. This explains the onset of cumulus
olivine rainout.

In Big Daddy DDH FW-08-19, there is a sequence of pyroxenite followed by the
transitional heterogeneous pyroxenite unit, then chromitite followed by dunite resulting
in the sequence order of pyroxenite to chromitite to dunite. In the second chromitite layer
of DDH BT-09-17 there is first pyroxenite followed by cumulus pyroxene with chromite,
then chromitite with minor dunite and then pyroxenite. In these scenarios, the chromitite
is related to the migration of the melt from pyroxene to chromite to olivine. Notably,
most chromitite layers occur in the sequence from dunite to chromitite to pyroxenite.
Since this reversal in crystallization order involves an increase in temperature, the
migration of the melt to eventual olivine could only work with magma mixing rather than
a fractionation mechanism. There is no way of depleting the melt of silica except for
some sort of mixture with a primitive melt which is inferred to be the mechanism for
chromite origin.

Another problem with the model is that the chromite is related to the magma
chemistry of the host rocks and not the assimilant. If a new dunite pulse was
contaminated by TTG to mineralize chromite, the presence of variable plagioclase
content with variable contamination would cause variable Cr contents of the ores.
However, in the Big Daddy massive chromitite interval, the chromites that were probably
derived from various replenishments have a consistent Cr2O3 composition up section.
The chromites all have primitive Cr2O3 compositions related to the chromite that are
primitive and closer to olivine stability rather that being lowered by plagioclase content
of an assimilant. In their discussion of the Bushveld chromitites, Naldrett et al. (2009)
show that Al2O3 content of chromite mineralized in equilibrium with plagioclase will be

238
buffered by the high Al2O3 content of plagioclase. The effect is to raise the Cr/(Cr+Al)
or lower the Al2O3 content of the chromite since the chemical potential of Al2O3 is over
its maximized value and is buffered by plagioclase (Naldrett et al., 2009). In the Big
Daddy massive chromitite, there is no enrichment or depletion in Al2O3 in the chromite
that would result due to the presence of plagioclase, as would be present in a crustally
contaminated dunite pulse.

In the sequences of dunite to chromitite to pyroxenite, it may be argued that there
was replacement of pyroxene by olivine to drive the melt into chromite stability. This is
the mechanism thought to be the origin of some podiform chromitites. In the harzburgitic
mantle the migration of an intercumulus melt causes replacement of pyroxene,
incorporation of silica and the precipitation of pods of chromitite (Matsumoto and Arai,
2001). Or in a layered intrusion sequence, the influx of a primitive melt could dissolve
and assimilate the roof pyroxenite of an intrusion and precipitate chromitite (Pagé, 2010).
However, there appears to be several stacked sequences of dunite to chromitite to
pyroxenite where there are large thicknesses of the later pyroxenite. It is unlikely that the
large sequences of pyroxenite are all a result of roof contamination when there are later
higher and more primitive sequences of chromitite in Black Label Layer 2 for example.
Also the occurrence of some reversed crystallization orders of pyroxenite to chromitite to
dunite and the presence of cumulus chromite in pyroxenite makes it unlikely that the
pyroxenite was a result of roof assimilation.

The evidence that is missing is the lack of xenoliths in drill core that would be
injested by the magma for incorporation into the melt. Mungall (2008) outlines the
presence of iron formation xenoliths for the Eagle’s Nest deposit and proposed the same
incorporation of contaminant in the formation of the Blackbird deposit chromites. The
assimilation of TTG is inherent to the trace element geochemistry of the McFaulds Lake
dunites and pyroxenites. Iron formation has been observed as xenolith in the Black
Creek chromite deposit (Lavigne, pers. communication, 2013). However, there have
been no xenoliths detected in the McFaulds Lake chromite layers that would explain the
formation of the large chromite layers.

Another means proposed for chromite formation is straight fractionation. This
would explain the presence of cumulus chromite and olivine in disseminated chromite

239
bearing dunite. Though, often in deposits such as Big Daddy, there is chromite
disseminated in dunite followed by thick massive chromitite before overlying pyroxenite.
What would cause a chromite-only crystallization change from chromite + olivine?
There appears to be no mechanism of dithering and keeping the intercumulus melt in the
chromite only field in order to produces up to 40 m thickness of chromitite. And of
course the sequence of pyroxenite to chromite to dunite is not explained.

6.4 Silicate Inclusions in Chromite
There has been evidence used to support chromite origin by silica addition by
means of the presence of silicate inclusions with minerals such as albite and amphibole.
This interpretation was made in Irvine (1975). The presence of serpentine, chlorite or
tremolite would be explained as the result of replacement of olivine. However, silicate
inclusions of albite and amphibole are foreign to the surrounding retrograded serpentines
and tremolites of the intrusive dunites and pyroxenites. The Kemi deposit in Finland is a
chromite deposit similar in thickness to the McFaulds Lake deposits. Alapieti et al.
(1989) described the Kemi deposit in detail and concluded that it is a stratiform chromite
deposit in an ultramafic layered intrusion. He proposed that chromite crystallization was
initiated by silica addition/salic contamination. Evidences for silica addition were round
silicate inclusions of serpentine, amphibole or albite in chromite grains. The presence of
albite inclusions in chromite hosted by dunite suggested entrapment of wallrock
contaminant. Spandler et al. (2005) discuss the presence of mineral inclusions of
enstatite, aspidolite (Na-phlogopite), magnesiokatophorite (Na-Ca amphibole), albite and
diopside. Spandler et al. (2005) referenced Page and Zientek (1987), proposing that Na
amphiboles and micas significantly more Na-rich than the primary amphibole and
phlogopite of the surrounding cumulates, are exotic, related to contamination of the
primary magma by a Na-rich trondhjemitic melt.

In the McFaulds Lake chromites, silicate inclusions of serpentine and tremolite
have been observed in the chromites. The inclusions of serpentine and tremolite in the
chromites of this study have been documented to undergo sintering as evidenced by the
concentric growth of chromites around olivines and also adcumulus growth with the
presence of incomplete chromites growing around silicate. In these cases, the resultant
inclusions have compositions and sometimes cleavage planes that are the same as the

240
surrounding tremolite silicate. Therefore, these inclusions are shown to be a result of
sintering similar to silicate inclusions of chromites in the Bushveld Complex (Hulbert and
Von Gruenewaldt, 1985; Fig. 6.4). However, exotic inclusions of chromian diopside,
chromian magnesiokatophorite, chromian Na-phlogopite and albite have also been found
in the chromites. This would appear to suggest they are exotic inclusions involved in the
origin of the chromite that were a result of contamination. The McFaulds Lake dunites
and pyroxenites have trace element compositions that show crustal contamination of
komatiite by Na-rich TTG. However, the magnesiokatophorites analysed have high TiO2
contents similar to that of late igneous amphiboles in ultramafic intrusions. Primary
pargasites, for example, often have high TiO2 concentrations (Embey-Isztin, 1976).
Borisova (2012) in his discussion of silicate inclusions in the Oman ophiolite chromitites,
discusses that the high Ti and Cr contents of the amphiboles indicate either a magmatic or
high T hydrothermal environment of formation, since these elements are less mobile in
the presence of low T aqueous fluids. So these amphiboles would be magmatic.

Another observation is that primary pargasite occurs as a relic grain interior to
tremolite in the host silicate to the chromite in sample 486163 that has silicate inclusions
of the same pargasite composition. This is evidence that the mineral inclusions are
residual amphiboles similar to that of the surrounding host rock and are therefore not
exotic. A similar scenario could be suggested for the Na-phlogopite although the Naphlogopite
was not found in the host silicate. Though Cr-bearing Na-, titanian
phlogopites occur as late stage igneous phases in other olivine-chromite cumulates such
as the host rocks to the B chromitites in the Stillwater Complex (Page and Zientek, 1987).
High Cr and Ti contents in phlogopites have been shown to be enriched by metasomatism
in zoning trends of phlogopites of South Africa (Field et al., 1989). If the McFaulds Lake
inclusions were a result of high T metasomatism, this would affect the chemistries of the
chromites themselves with enrichment in silica and titanium. However, titanium
distribution has shown to be less at the cores of the chromites rather than being enriched.
The lower Ti as well as primitive high Cr and high Mg contents suggest that the
chemistries of the chromites are primary residual melt rather than enriched by
metasomatism. Another evidence of the phlogopite being postcumulus is the presence of
similar K phlogopites in the surrounding host rocks and evidence of chromite in the

241
Fig. 6.4. Annealing process for the formation of silicate inclusions/atoll structures in
chromite. From Hulbert and Von Gruenewaldt (1985).

242
intermediate stages of enveloping phlogopite minerals (See petrography chapter, silicate
inclusions). Such evidence of the annealing of chromite around phlogopite has also been
documented in chromites of the Western Laouni mafic intrusion in Algeria (Lorand and
Cottin, 1987).

Sometimes the magesiokatophorite has been subsequently altered or the
magnesiokatophorite replaces original clinopyroxene which is different alteration then
the low T hydration of silicate surrounding the chromite. This shows that the silicate
inclusions are often isolated from the silicate surrounding the chromite and reflects a
different alteration. Often Na-katophorites have been found in silicate inclusions where
there is no igneous amphibole surrounding the chromite. This could be explained by
possible slumping of pulses that could have mobilized the chromite from the
surroundings. In such a circumstance, the chromite composition would still be relatively
similar to the surrounding host rock olivine or pyroxene magma. Another explanation
that seems more plausible is that the minerals formed from residual melt encapsulated in
the growing chromite. This explanation is discussed below in the discussion of Sharpe’s
(1983) thesis.

The high Ti and Cr compositions of the silicate inclusion-bearing amphiboles and
phlogopites appear to be mantle compositions. On a Cr2O3 vs. Al2O3 plot of the
phlogopites analysed, the minerals plot in the primitive mantle box and follow a trend of
high Mg compositions similar to kimberlites. Also the Ti and Cr-enriched
magnesiokatophorites and pargasites are similar to such amphiboles found in mantle
nodules of kimberlites of the Jagersfontein and Kimberley kimberlites (Field et al., 1989).
Page and Zietek (1987) discuss similar mantle-like compositions for the hornblendes and
phlogopites of the Stillwater Intrusion. They reference Arima and Edgar (1981) for the
solubility of titanium of phlogopites in mantle compositions. However, Page and Zietek
(1987) state that the phlogopites certainly did not crystallize at high pressure and
temperature mantle regimes. In their analysis of postcumulus hornblende and phlogopite
compositions with height of the Stillwater Intrusion, they have shown that these
compositions reflect the chromite content of the surrounding rocks. McElduff and
Stumpfl (1991) have proposed that these minerals found in silicate inclusions form in the
same process of postcumulus amphibole and phlogopite in the layered chromitites of the

243
Troodos Complex. Lorand and Cottin (1987), in their study of the silicate inclusions in
chromites of the Western Laouni mafic intrusion, also concluded that the inclusions are
postcumulus like the surrounding postcumulus amphiboles and phlogopites and are a
result of residual liquids and late magmatic fluids.

Therefore, the silicate inclusion amphiboles and phlogopites should mimic the
chromite contents of the host rocks like those of the Stillwater Intrusion. On a plot of wt.
% MgO and wt. % Cr2O3 with height in DDH BT-09-31, it is shown that the Layer 2
chromites are more primitive than the Layer 1 chromites with higher wt. % MgO and wt.
% Cr2O3. With the same variation in the phlogopites, it is also shown that the Layer 2
silicate inclusion phlogopites have higher wt. % MgO than the Layer 1 phlogopites. The
wt. % Cr2O3 would show a reverse trend due to the substitution of Mg with Cr in
phlogopite. For variation of Mg # with height in the same drill hole for pargasiteedenites
compositions, it is also shown that Layer 2 silicate inclusion amphiboles have
higher Mg # than the Layer 1 amphiboles.

It might be argued that phlogopite and amphibole mantle nodules were
incorporated by the chromites from the varying primitive nature of the pulses that formed
these layers. However, it is shown that the chemistry of the chromite in the Layer 1
chromitite reflects the mineralogy of the host oikocrystic harzburgite that lowers the
Cr/Fe content of the chromites in that layer. Therefore, the lower Cr and Mg chromites
of that layer are not reflective of a less primitive pulse. Also, it would remain to be
explained why there would be mantle nodules incorporated in the chromites if the
chromite itself crystallized in the magma chamber. The fractionation trends in the
chromites give strong evidence that the chromites formed in a magma chamber rather
than in mantle-like podiform chromitites. The newly formed chromites would have to
peculiarily extract a large amount of mantle nodules from the surrounding host rock that
has no evidence of the presence of mantle nodules itself. In fact, the igneous amphiboles
that have been found with similar compositions to the silicate inclusion amphiboles are
relic postcumulus amphiboles like those in the Stillwater Intrusion. This shows that the
phlogopites and amphiboles in the silicate inclusions are derived as residual melts
encapsulated by the chromite and reflect the differentiated layers rather than as mantle

244
nodules in the chromites. The chromite and titanium contents are derived from the
chromite rather than forming under high pressure and temperature regimes of the mantle.

The presence of evolved albite in the inclusions would also preclude mantle
origin. Albite would not crystallize as late igneous phases in the ultramafic McFaulds
Lake complex like the amphiboles and phlogopites. Therefore, the origin of albite needs
to be explained. It is suggested that the same Na-rich melt that produced the Namagnesiokatophorites
was involved in the crystallization of albite as Na-rich residual.
One suggestion in the past from Irvine (1981) is that the albitic and other “granitic”
inclusions formed as a result of an enhanced silica immiscibility effect with oxidation of
chromite in the presence of FeO and Fe2O3. In such a circumstance, it might happen that
the mixing lines of chromite between olivine and pyroxene will intersect the solvus and
precipitate the silica-rich immiscible liquid as inclusion. Another theory for precipitation
of albite is the reequilibration of previous inclusions due to metasomatism of the
chromites. Often there are are other salt species present in these inclusions that could
allude to ingress of later fluids. The inclusions appear to be wholly enclosed by the
chromite, and some fractures appear to be late with no retrogression which argues against
a pathway for these migrating fluids. However, other silicates such as tremolites,
chlorites and talcs that crystallized within the chromites formed the same way as later
hydration metasomatism of the silicates and chromites. Clues to there being
metasomatism of ionized salts are the presence of chlorites that require silicon from an
outside source that can not be provided from the chromite spinels themselves.

Although there is evidence of metasomatism with retrogression, it is unlikely that
the albite formed in a similar way. First of all, the retrogressive fluids are unrelated to
the high alkali compositions of the albites. Also, in sample 486349, albite inclusions
appear to have igneous textures in association with chromium titanian
magnesiokatophorites and phlogopites. Since the magnesiokatophorites and phlogopites
are interpreted as being magmatic, this is suggested for the albite as well. Albite, like
phlogopite, has not been found outside of the inclusions. Also, it is not a late stage
igneous mineral of an intrusion like igneous amphibole and phlogopite.

One thesis from Sharpe (1983) on chromitites in the Thetford Ophiolite Complex
describes trends in chemistries of chromites and olivines toward secondary fluid

245
inclusion trains occurring in both chromite and olivine. The effect of the fluids on
chromite was to slightly enrich the grains in ferrous and ferric iron, while decrease in Cr,
Mg and Al. The effect of the fluids on olivine was to decrease the SiO2 and MgO of
olivine while increase in K2O, CaO and NaO (Sharpe, 1983). From those observations,
Sharpe (1983) concluded that the fluid that flowed through the rocks after formation
contained significant amounts of Na, Ca and possible some iron. Further analysis of
primary inclusions in chromite has shown that the fluids caused enrichment in Na2O,
MgO, SiO2 and CaO, decrease in Al, Cr and Fe while no significant change in K or Ti.
In comparing to inclusions in other deposits, Sharpe (1983) suggests the inclusions are
not primary silicates that were included in the chromites, but were a result of later fluid to
precipitate the serpentine, talc, chlorite, sulfides, pargasitic amphiboles, albite and sodic
layer silicates described in these other complexes (Watkinson and Mainwaring, 1980 in
Sharpe, 1983).

In the McFaulds Lake chromites, these types of silicates are found in the
chromites, which suggests they were later incorporated into the chromites due to
encapsulation of residual melt and later hydration. The enrichment in Na2O, MgO and
CaO would not be involved in forming the Na-katophorites after silicate is included since
similar pargasite was found as late stage amphibole in the silicate host before being
included in the chromite. However, Na-katophorites are not like the typical pargasites
with lower Na2O and CaO found as later stage igneous amphibole in complexes such as
the Stillwater Complex. Sharpe (1983) suggested that the fluid inclusion trains observed
in the Thetford chromites and olivines were from magmatic fluids. Clues to these fluids
as being magmatic are the alkali and CaO along with MgO enrichment toward the
inclusion trains. Clues to these being fluids rather than igneous melt are the textures of
bubbles of fluid trains hosting the fluids and the enrichment or depletion in elements of
the chromite and olivine toward these trains.

In the McFaulds Lake chromites, some of the inclusions are found as trains along
growth planes in the chromites, in a similar habit to the fluid inclusion trains to the
Thetford chromites. Their distribution along a growth plane in the chromite suggests
incorporation of fluid during growth of the chromites since it is unlikely the chromite
grew around aggregates of silicate all along the edge of the chromite (Fig. 3.29,

246
petrography chapter). Therefore the association of the inclusions with the growth planes
suggests these were real magmatic fluids/residual melts. Sharpe (1983) mentions how
there was no change in TiO2 toward the inclusions. This suggests Ti was not mobile but
represents a magmatic component to the inclusions rather than being a metasomatic
feature. The Na-magnesiokatophorites of the McFaulds Lake chromites have high MgO,
Na2O and CaO similar to enrichments in these elements provided by the magmatic fluids
of Sharpe (1983). Since the amphiboles are igneous with high TiO2 and have peculiarly
high MgO, Na2O and CaO than regular pargasites, it is interpreted these inclusions as
well as katophorite found in the silicate host are derived from residual melt. Naphlogopite
may have been derived from similar fluids. K2O was enriched by these fluids
in the olivines of Sharpe (1983) and was probably also enriched in the formation of
phlogopite.

Albite may have crystallized from these residual melts. Notably, in the fluids of
Sharpe (1983), there is also enrichment in Al2O3 and a high enrichment in SiO2. These
elements along with Na2O would result in the formation of the albite in the inclusions. It
may be that the albite grew in the inclusion or could have been the result of magmatic
fluids being incorporated along fractures. Fractures have been found to occur along
possible points of entry into silicate inclusions. Notably, retrogressive zoning has not
been seen along these fractures like the retrogression that is involved in the formation of
later chlorite within the chromites. However, these fluids are a different composition
than the retrogressive fluids and would not cause the same extent of depletion in Cr, Mg
while enrichment in Fe as the retrogressive fluids. Sharpe (1983) notes these trends in
the chromites are subtle in the case of these magmatic fluids. Albite has not been found
like amphibole and phlogopite as late stage igneous phases in the silicate host to the
chromite. This is probably due to albite forming from residual melts specific to to the
chromite it is encapsulated in. Usually, albite is found in cases of granophyres and
incorporation of wall rock in the intrusion. Since there is no indication of wallrock
contamination in the immediate surrounding dunites and pyroxenites, and cracks have
been found in association with the silicate inclusions, the albite probably grew within the
silicate inclusions from residual melt.

247
This may or may not be the case for the igneous amphiboles and phlogopites since
the growth and incorporation in some cases incorporated pargasite whereas in other cases
magnesiokatophorite is found in the inclusion but not in surrounding silicate. Either the
chromites were later mobilized in a different location than surroundings with slumping or
filter pressing or the magnesiokatophorite grew in these cases in the inclusion. It appears
more probable that the amphibole grew within the inclusion since chromite surrounds
other exotic minerals such as the Na phlogopites. Either way, all these minerals are late
stage phases to the intrusion, and since there is not a magmatic chemical association of
the chromite with these minerals, they all crystallized as melt encapsulated by the
chromite. It could have been argued that in some circumstances, the negative crystal
faces of the silicate inclusions within the chromite make them in equilibrium with
growing chromites. However, closer examination shows that these negative crystal faces
of the inclusions surround an inclusion of multiple minerals and are not related to single
crystal growths in the chromite. Therefore, these structures are interpreted to be wholly
related to the crystal face structure of the chromite itself. The nature of how the chromite
grew around the silicate is either by annealing or adcumulus growth of individual
chromites.

There are other references to katophorite, Na-phlogopite and albite silicate
inclusions in chromite being formed from precipitation of magmatic fluids. McElduff
and Stumpfl (1991) argue the inclusions in the Troodos chromitites are intimately linked
to a reducing chloride-rich fluid within the magmatic system where chromite is either
transported within this fluid or extracted from the melt. An Na-rich and Ca-rich hydrous
phase probably separated from the melt due to decreasing pressure related to the opening
of the system (McElduff and Stumpfl, 1991). Within the Troodos chromitites, the
layered complex chromites have different compositions of silicate inclusions than the
lower mantle podiform chromites. The podiform chromites bear orthopyroxene,
clinopyroxene, hornblende, olivine, serpentine and chlorite while the chromites in the
layers bear pargasitic amphibole, serpentine, chlorite and albite (McElduff and Stumfl,
1991). The latter set of inclusions is more similar to the pargasite, serpentine, chlorite
and albite found in McFaulds Lake chromites. Inclusions in Troodos have been noted to
become more Na and Fe-rich toward these layered cumulate chromites. The

248
compositional difference of the inclusions is probably reflective of the different
environments of formation – the layered chromites being more evolved and alkalic than
the podiform mantle chromites.

The association of these inclusions with layered chromite suggests the inclusions
are related to the magma chemistry of the chromite evolution, rather than being exotic
assimilants. Li et al. (2005) discuss the inclusions of the Merensky Reef and explain the
Ti and Na-rich compositions as being due to volatiles that formed with dissolution of
rutile and pyroxene as the fluids were expelled from the underlying cumulus pile. In the
Merensky Reef chromites, silicate inclusions have been found to contain Na phlogopite
that is more Na-rich than the matrix, similar to the case of there being Na phlogopites
only in the inclusions of the McFaulds Lake chromites. Li et al. (2005) report oxygen
isotopic data of the inclusions as having a bulk d18O value of 7 ‰. Plagioclaseorthopyroxene,
orthopyroxene-chromite and orthopyroxene-phlogopite delta values
suggested equilibration temperatures near 1200 °C using the fractionation factors of
Zheng (1991, 1993) in Li et al. (2005). This shows that higher T magmatic fluids were
involved rather than low T fluids in the precipitation of these alkali minerals. The
addition of Na-K rich fluid occurred during chromite crystallization on the floor of the
magma chamber (Li et al., 2005).

It appears that the exotic minerals in the silicate inclusions crystallized from
residual melt encapsulated by the growing chromite. In sample 486211, there appears to
be an association of silicate inclusion with the finer more disseminated grains rather than
the larger chromites. The observation of more silicate inclusions in chain-like
disseminated chromite was also made in the semi-massive chromitites of this study.
Also, inclusions are found along growth planes within original chromites. Since the
inclusions are preferentially found in smaller, later chromites, this would suggest that
there are multiple generations of chromite in the samples: the first being primary
magmatic chromite crystallization of larger, primitive chromites in the melt followed by
further growth of chromite that encaptured the melt that later precipitated the silicate
inclusions. The later growth of chromite that encaptured magmatic fluids is suggested by
the presence of enriched Cr2O3 in the inclusions of diopside, magnesiokatophorite and
phlogopite. The fact that there is Cr2O3 in these minerals suggests these minerals

249
incorporated Cr2O3 from pre-existing chromite. Since magmatic fluids have been shown
by Sharp (1983) to cause subtle exchange with chromite, it is possible that the chromites
in the presence of inclusions have slightly more diffused compositions. Although, there
has not been evidence observed for this in these chromites, perhaps since diffusion is
subtle.

The primary silicate inclusion minerals have unique compositions. The
phlogopites and igneous amphiboles appear similar to metasomatic phlogopites and
amphiboles in the upper mantle. Although these inclusions are not from the upper
mantle, they probably formed from essentially similar magma chemistries. Page and
Zientek (1987) concluded that the postcumulus phlogopites and amphiboles derived their
chromium from the chromites themselves. Lorand and Cottin (1987) concluded that the
minerals are a result of dissolution of chromite. In their discussion of metasomatic
minerals in peridotite nodules of kimberlites, Erlank et al. (1987) suggest these minerals
inherit Cr from the Cr-spinel with the Mg being of peridotite heritage. An overall
reaction for the formation of metasomatic minerals in the upper mantle is Olivine +
enstatite + garnet + diopside1 + Cr-spinel + fluid (K2O etc., H2O, CO2) . phlogopite +
K-richterite ± diopside2 + Cr-spinel2 ± calcite ± LIMA, ilmenite, rutile, armalcolite,
sulphides. The same magnesian olivines and pyroxenes + chromite + fluids are probably
involved in the formation of the silicate inclusion minerals. Notably, the pyroxenes,
amphiboles, phlogopites, and chlorites probed in this study all have very magnesian
compositions. These minerals would be linked to the magnesian heritage of the host
magma to the chromite. Albite, which has a more crustal-like composition, is suggested
to be derived from the transformation of plagioclase toward its Na-end member due to
hydrothermal fluids (Lorand and Cottin, 1987). This is also suggested by the presence of
Na-phlogopite and Na-magnesiokatophorite in the inclusions alone as opposed to the
surrounding silicate host rock.

6.5 Origin of chromite: Irvine’s 1977 magma mixing model
Since there are problems with the theory of silica addition alone, it is proposed
that the chromitites crystallized by means of magma mixing of two different magmas. In
the case of the McFaulds deposits, one difference between the magmas is the lesser vs.
more crustally contamination in the pyroxenite vs. dunite. Irvine (1977) explains that in a

250
magma chamber, there was first differentiation causing accumulation of dunite to
pyroxenite, and then a new replenishing olivine-laden magma pulse mixes with the
residual melt, left after pyroxene accumulation, to drive the melt into the chromite
stability field to rainout chromite (Fig. 6.5). Eventually with fractionation the melt will
migrate into the pyroxene only field. This order of crystallization is seen in the
petrography of the oikocrystic harzburgite/semi-massive chromitites where olivine
crystallized first followed by chromite which is in turn overgrown by intercumulus
pyroxene. Specifically, Irvine (1977) demonstrated that if a new input of magma was
injected into one that had reached a higher degree of fractionation, the resultant mixing
action could inhibit the fractional crystallization of silicate minerals such as olivine and
orthopyroxene and permit the crystallization of chromite alone. As illustrated in Figure
6.5, the mixing of liquid A which is on the olivine – chromite cotectic, with liquid D on
the orthopyroxene field may, provided that points on the mixing line lie above the
liquidus surface, culminate in a hybrid magma such as AD which will intersect the
liquidus in the chromite field on cooling. Hence it will crystallize chromite alone while it
moves to point X on the olivine – chromite cotectic, and thereafter it will continue to
crystallize chromite and olivine.

It has been shown that the decrease in the solubility of chromite in basaltic
magma in equilibrium with chromite per degree centigrade fall in temperature is greater
at high (1,300°C – 1,400°C) than at low (1,100°C – 1,200°C) temperature. Due to this
concave – upward curvature of the solubility curve, the mixing of two magmas at
different temperatures saturated (or nearly saturated) in chromite places the resultant
mixture above the saturation curve, which suggests that point AD in Figure 6.5 is likely
to lie above the liquidus. The suggestions by Irvine (1977) are consistent with
observations on chromitites in layered intrusions. Most significant amongst these
observations is the fact that most of these chromitite layers occur at the base of well
defined cyclic units (e.g. Bushveld Complex and Great Dyke in Southern Africa) or
at/near the base of similar cyclic units. Further evidence comes from the textures of the
underlying rock units which indicate a common cotectic crystallization of chromite with
olivine or orthopyroxene showing that the magmas previously in the chambers were

251
Figure 6.5. Phase Relations in the System Olivine-Silica-Chromite as determined by
Irvine (1977) illustrating the consequence of mixing primitive magma (A) with well
fractionated (D) and slightly fractionated (B) variants of the same primitive magma.
From Naldrett et al. (1990) in: Gowans (2009).

252
saturated with respect to chromite. In the case of the McFaulds Lake chromitites, the Cr-
saturated magma would be the melts that accumulated either the dunite or the pyroxenite.

There is evidence for magma mixing for the McFaulds Lake chromitites in the
different multielement and PGE chemistries between the host dunites and pyroxenites of
the three chromite deposits. The differences in trace element patterns are due to evolved
and more crustally contaminated vs. primitive and less crustally contaminated magmas
before the onset of chromite crystallization. Barnes and Maier (1999) have shown that in
the Bushveld Complex, the magma mixing of a high-MgO basalt or U-magma that is
SiO2 and LILE-enriched and the A- or tholeiitic magma would result in the
mineralization of the Merensky Reef PGE sulphide zone. Other evidence of there being
two magmas are in the higher PGE, lower Pd/Ir of the U-magma in contrast to the lower
PGE and higher Pd/Ir of the A-magma (Barnes and Maier, 1999). The terms of the two
magmas involved are derived by studies on the J-M Reef by Todd et al. (1982) where U-
type refers to an ultramafic magma that is PGE-rich and A-type refers to an anorthositic
magma that is sulphur-rich. There is evident contrast in the behavior of the elements
between the dunite and pyroxenite of the three deposits. For the trace element
compositions, the dunites are more trace element and REE-depleted and provide
primitive fresh magmas to the more evolved pyroxenites (Fig. 6.6). Contrasting REE
contents are evident in other deposits such as the more crustally contaminated upper
peridotites vs. the websterites of the Kemi Intrusion in Finland (Linkermann, 2010).

Mungall (2012) further explains the model as the mixing of S-undersaturated,
high IPGE-bearing magma with S-saturated low IPGE, higher Pt/Pd restite, in this case,
the mixing of a parental picrite with mantle residue. In the case of the McFaulds Lake
chromite deposits, there was mixing of a S-undersaturated, higher IPGE:PPGE U-type
olivine-bearing magma with S-saturated, lower IPGE:PPGE A-type pyroxene-laden
magma. In the case of Black Label, there would be the magma mixing of a highly Sundersaturated
dunite with the highest S-saturated pyroxenite of the three deposits (Fig.
6.7). Contrasting PGE contents of dunite vs. pyroxenite are also evident in the higher
IPGE:PPGE peridotites vs. the lower IPGE:PPGE websterites of the Kemi Intrusion
(Linkermann, 2010). For Black Thor, the dunite is not as highly undersaturated which
probably makes it more capable of precipitating PGE sulphide. Pyroxenite is less highly

254
S-saturated. In this case, a S-saturated, crustally contaminated pyroxene magma probably
mixed with S-undersaturated, less crustally contaminated dunite magma to cause
chromite crystallization. The case is similar with Big Daddy, only there is more evidence
of LILE enrichment within the dunites and pyroxenites which is probably a local
phenoma since this signature is not found in all the samples. In terms of petrography,
intermediate compositions of heterogeneous pyroxenite in Big Daddy and oikocrystic
harzburgite in Black Label show intermediate trace element and PGE chemistries
between the dunites and pyroxenites of the deposits.

At McFaulds Lake, a U-type olivine-laden magma, represented by dunite, is the
main carrier of Cr2O3 with the amount of Cr2O3 increasing rapidly with the amount of
olivine (Sharpe and Irvine, 1983). In the deposits, disseminated chromite-bearing dunites
commonly contain finer intercumulus to cumulus chromite that surrounds the primary
olivine grains. The A-type pyroxenite, in contrast, is close to saturation with chromite
even when Cr-free. Therefore there is not more than trace Cr2O3 in the pyroxene-laden
magma before there is crystallization of chromite (Sharpe and Irvine, 1983). This trace
chromite is characterized by the disseminated chromite in pyroxenite. The mixing of Crundersaturated
olivine magma with Cr-saturated residual pyroxene magma will then
cause the precipitation of chromite that segregate into layers.

Textures of interstitial and net-textured chromite may suggest evidence for
separation of an immiscible oxide melt. The separation of an immiscible oxide melt, as
described by Pavlov (1977) is the process of liquation of an ore-silicate melt and the
crystallization of the two separated liquids, essentially silicate and essentially oxide in
nature. In this definition, it is noted that the two liquids are just separated without any
particular order of crystallization. In the Black Label and Black Thor sequences, it was
noted that the chromite crystallizes post olivine from the melt left behind in the interstices
of the olivine cumulate. This makes sense if the melt is driven toward chromite stability
after separation of cumulus olivine. Therefore, any olivine cumulate can leave behind an
immiscible chromite melt.

In their discussion of podiform mantle chromites, the same interstitial chromite
textures are evident due to this unmixing (Ballhaus, 1998). However, although this is
evident in disseminated chromites, there needs to be a condition where massive chromite

255
is formed without there being wholesale mantle melting (Ballhaus, 1998). That is, if
immiscible oxide melts were separated out of an olivine magma everywhere, there would
be a common occurrence of chromite with dunite. However, the massive chromitite
horizons are typically found between dunite and pyroxenite sequences with distinct
chemistries as far as Cr-saturation. It would be more probable for separation of an
immiscible oxide melt under certain conditions where the magma reaches Cr stability
near certain evolved olivine magmas and certain primitive pyroxene magmas. However,
the limited occurrence of massive chromite within these lithologies suggests the
chromites are a product of the specific mixing of two different magmas and is more site
specific than would be suggested by separation of an oxide melt.

The magma mixing of differing trace element and PGE-bearing magmas is more
difficult to explain for chromitites since chromites host PGE as alloys in their structure in
contrast to the silicates and have very little trace element and REE (Barnes and Maier,
1999). Therefore, the chromites can not be represented as magma compositions with
olivine and pyroxene. The very thick chromitite intervals also make them harder to
explain for a simple mixing model since some condition needs to keep the magma
dithering in chromite stability. Therefore another mechanism is needed to explain the
presence of the thick chromitite layers: namely, double diffusive convection after
repetitive injections of magma.

6.6 Evidence for magmatic differentiation by double diffusive convection: The
electron microprobe results.
6.6.1 Magmatic differentiation
Past microprobe studies demonstrate that chromite compositions vary
substantially with respect to changes in Mg#, Cr/(Cr+Al), Cr3+/(Fe3++Fe2+) and elemental
Cr3+, Fe3+ and Al contents. Research has shown that Cr, Cr/Al, Cr/Fe and Mg# typically
decreases while Al and Fe increases from basal chromitites upward in stratigraphy
(Cameron, 1982, 1977; Irvine, 1975; Eales and Reynolds, 1986; Jackson, 1969).
Commonly there is increase in Cr and Cr/Al while Fe decreases, making Cr/Fe increase
while the Mg# decreases (Eales and Reynolds, 1986; Teigler and Eales, 1993; Teigler,
1999; Engelbrecht, 1985). The explanation for the general decrease in Cr, Cr/Al, Cr/Fe
and Mg # and general increase in Al and Fe relates to disseminated chromitites hosted in

256
more evolved magma ie. from dunite at the bottom, to pyroxenite, to leucogabbro at the
top. Increasing Cr, Cr/Al, and lower Cr/Fe towards the top of intervals relates to
differention from primary dunite to pyroxenite, and then a new pulse of magma mixes
with the residual melt to drive this mixed magma batch into the chromite stability field
and causes rainout of new chromite towards the tops of some intervals. Eales and
Reynolds (1986) and Naldrett (2009) also document trends in enrichment in Cr/Al in the
UG 2 chromitite and explain the increase as due to Al declining in the spinel phase after
plagioclase is nucleated in the liquid.

In the McFaulds Lake chromites, there is evidence of magmatic differentiation in
the form of cascading upward decreasing trends in MgO and Cr2O3, while increasing FeO
and Al2O3 with height in layers, one on top of the other with pulses evident at the
decimeter scale. These trends are particularly evident in the Black Label and Black Thor
drill intercepts analysed. From one pulse to the next, there are enrichment trends in MgO
and Cr2O3, while decreasing FeO and Al2O3. Since there is an association of increasing
MgO with Cr2O3 and there is no plagioclase observed in the zones, the interpretation of
increasing Cr/Al in the deposits as due to the buffering by plagioclase can be discarded.
Rather, since MgO decreases with Cr2O3 and chromite is known to be a petrogenetic
indicator of the melt, it is interpreted that these trends are due to replenishing pulses of
magma followed by differentiation trends of the magma afterward (Irvine, 1965).

Evidence that the chromite is chemically related to the host rock are the high vs.
low Al2O3 content of the Black Label Layer 1 vs. Layer 2, from which greater Al2O3
reflects greater pyroxene. In Layer 1, the greater silicate content also lowers the Cr/Fe
ratio with more disseminated chromite. A few primary olivines have also been probed in
the two layers where olivines of Layer 1 are more evolved with Fo #s of 80 to 85 whereas
olivines of Layer 2 are more primitive with Fo #s of up to 94. Another evidence of these
major oxide trends being due to magmatic differentiation is that they are common in
layered intrusions and have relatively good antipathetic correlations to each other: MgO
being antipathetic with FeO and Cr2O3 being antipathetic with Al2O3 due to direction
substitution of the elements in the tetrahedral and octahedral sites of the chromite
structure. These direct correlations have also been documented from other intrusions
such as the Bushveld Complex (Stowe, 1994).

257
From disseminated to massive chromite, there are trends toward homogeneity in
Cr2O3 as can be seen in the Big Daddy massive chromitite intercept. Although there is
less of a decrease of Cr2O3 upward in each pulse, there is still a more direct decrease in
MgO. This phenomenom has not been studied to any extent in other massive chromitite
intervals of the world. Since there is no plagioclase in the surrounding lithologies to
buffer the Al and cause an increase in Cr, it is proposed that the lesser decrease upward of
Cr in these cycles is due to double diffusive convection. The theory is explained below.

6.6.2 Double diffusive convection mineralization
Double diffusive convection is a type of magma mixing where a flux of one
property of a system is imposed on the gradient of another property with a different
molecular diffusivity to produce a series of convecting layers (Campbell, 1996). A
magma with a compositional density gradient when cooled from above will break up into
two horizontal convective layers separated by an interface or boundary layer across
which heat and composition are transported by molecular diffusion. Heat is transferred
across the interfaces and causes instability and convection in the layers above and below,
while the composition of the layer changes little to preserve “stable” density steps
between the layers (Fig. 6.8). Total density is greatest in the bottom layer and density
contrasts in a system will increase in time between individual double diffusive convection
systems (Fig. 6.8).

There is a trend of increasing density in the bottom layer while decreasing density
in the top since there is a loss of heat in the bottom layer while a gain of heat in the top
(Fig. 6.8). In a layered intrusion chromite-PGE interval, the gain in density in the bottom
layer is shown by replenishment with increasing Cr, and Cr/Al in the chromitite upward
while the decreasing density in the top layer is shown by less decreasing Cr and reverse
grading in the chromitite downward. An example of this system in progress is the top vs.
bottom chromitite intervals in DDH BT-08-10. For PGE, top and bottom peaks in PGE
first mineralize with initial sulphur saturation in the respective top and bottom convective
layers in a double diffusively convecting chromite-PGE mineralizing system (Fig. 6.9).

At the early stages, the PGE contents increase more so in the bottom convective
layer while decrease in the top convective layer due to the respective increasing density
of mineralization in the bottom convective layer while decreasing the density in the top

258258
Figure 6.8. Double diffusive convection. a) In the magma chamber, density of

crystallization is greatest toward the bottom convective layer, while temperature is

initially the lowest in bottom convective layer. The density contrasts in the chamber

cause development of the separate convection cells. b) With time, a series of double

diffusion convection systems develop in a step-wise manner with density increasing

toward the bottom layer due to settling mineralization and contrast in temperature. With

time, the bottom convective layer increases in temperature with burial of cumulate and/or

mineralization (Campbell, 1996).
Figure 6.9: Double diffusion
convection cells in the magma
chamber with associated
mineralization: a) The boundary
layer is contained between top and
bottom convective layers of a
double diffusive convection
system. Upwellings of magma
heat the bottom of the overlying
top layer which in turn cycles
down into the bottom convective
layer. b) Details of boundary
layer: Heat first transports up with
fluid, then cools down and
crystallizes refractory chromite
and PGE in top and bottom peaks
of the respective top and bottom
convective layers. With time
there is an increasing velocity in
top convective layer thereby
increasing the mineralization,
while decreasing velocity in the
bottom convective layer. This is
due to the temperature differences
between the top and bottom layers
(Rice and von Gruenewaldt,
1994).

259
convective layer (Fig. 6.9). Eventually, however, the PGE will increase from the top
boundary layer downward since temperature drives higher velocity flow of magma in the
top layer, while the bottom layer obtains slower velocity magma with more crystal
accumulation (Fig. 6.9: Rice and von Gruenewaldt, 1994). Even though there is less
velocity for mineralization with time in the bottom convective layer, there will still be a
trend of less decreasing Cr upward since more mineralization in the top convective layer
will be coupled by gravitational settling of this mineralization downward which
accumulates the PGE in the bottom layer (Fig. 6.10: Rice and von Gruenewaldt, 1994).
Therefore, with time there will be a pattern of increasing chromite-PGE inward ie. from
the top convective layer downward and from the bottom convective layer upward in the
most evolved chromite-PGE intervals.

In the McFaulds Lake chromites of the Big Daddy interval, it can be seen that
there are less decreasing Cr2O3 contents while MgO decreases to a further extent.
Although this phenomenon is has not been studied in any detail, one thesis by Johnson
(2012) on the study of the podiform chromitites in Kazakhstan also considers prominent
changes in Mg # vs. Cr # with depth of the chromitite. Johnson (2012) gave two
proposals for this pattern: the first that there could be reequilibration of chromite with
olivine in order to decrease the Mg # or that this was a result of increased chromite to
olivine with densification of the magma upward in the profile. Johnson (2012) notes that
the fine-scale layering and structural continuity of the massive chromitite would need to
be preserved under these conditions.

For the Big Daddy massive chromitite, it is suggested that the pattern is not due to
chromite reequilibrating with olivine because there is no cumulus olivine present in the
massive chromitite. However, there are definitely higher chromite to olivine contents.
Therefore, there is probably densification of the magma with the actual preservation of
fine-scale layering in these compositions which makes them truly magmatic. Further
explanation of the double diffusive convection with the densification of the magma is
proposed. One factor critical for this convection to occur is the contrasting diffusivities
between a Cr-saturated olivine magma and a Cr-undersaturated pyroxene magma. The
olivine magma would have a higher diffusivity then the pyroxene magma. With a new
pulse of olivine magma mixed into the pyroxene magma, the diffusion of Cr from the

260
Figure 6.10: Double diffusive chromite-PGE mineralization. Separate systems develop
with step-wise chromite-PGE mineralization where refractory chromite and PGE
mineralize with increasing velocity of magma in the top convective layer, thereby
increasing mineralization with gravitational settling in the bottom convective layer. Over
time, the bottom convective layer mineralization will continue to be replenished from
rainout from the top convective layer. Therefore patterns of increasing chromite-PGE
from the top layer downward and bottom layer upward will develop with development of
each step-wise double diffusive convection system grading upward in the magma
chamber (Rice and von Gruenewaldt, 1994).

261
olivine magma to the pyroxene magma will cause Cr saturation and crystallization. After
Cr is saturated in the underlying pyroxene magma, there will in turn be convective
overturn of the resulting melt upward that will be less Cr-saturated and less dense. The
next olivine magma layer higher up in sequence will mix with this less dense melt and the
process will continue higher up in stratigraphy. There will be periodic interruptions in
this sequence by new replenishments of olivine magma as evident by peaks in MgO
contents within the overall differentiation trend. Noticeably in the 3rd pulse of the Layer
1 in Black Label, there is also more of a transition of the regular fractionating pulses to
this double diffusive convecting condition. This would then progress to the more
complete mineralization of the Big Daddy massive chromitite intervals. The double
diffuse convection is also documented by the primary top and bottom peak PGE
mineralization of many of the chromitite intercepts in all the drill holes analysed. These
peaks of PGE that are commonly offset by the chromite mineralizations are due to
primary individual sulphur saturating conditions of the PGE with the surrounding
silicates at the beginning of the bottom layer going upward and the top layer mineralizing
downward.

6.6.3 Formation of massive chromite by post-cumulus growth
In the petrography of intermittent chromitite beds, semi-massive chromite and
massive chromite, there are observations in the chromite grains that alludes to post-
cumulus growth of chromite following the pulsing events. In the intermittent chromitite
beds, there are textures of layers with first chromite only, followed by cumulus olivine
that contains intercumulus finer grained chromite. Textures of chromite interstitial to
cumulus olivine suggest the chromite formed after cumulus olivine segregation. In semi-
massive chromite, net to chain-like textures of intercumulus chromite within olivine also
suggests this in situ crystallization. In the semi-massive chromites, the abundance of
silicate inclusions within the chromites of these chains suggests the growth of adcumulus
chromite. It was suggested earlier in this chapter that the occurrence of silicate inclusions
in smaller chromites vs. no inclusions in larger chromites points to two generations of
chromite: one being the early magmatic chromite and the second being a second-stage
chromite that encaptured residual melts from the expulsion of these fluids from the
cumulus pile. The fact that these silicate inclusions formed from expulsion of fluids after

262
cumulus segregation makes sense if their occurrence is after the larger primary chromite
grains.

The presence of chromite growing in equilibrium with later igneous phases also
suggests that chromite may have crystallized in the presence of H2O. Azar (2010) cites
Bannister et al. (1998) in her thesis on the Blackbird chromitites that H2O lowers the
liquidus temperature of chromite and associated olivine or pyroxene phase crystallization.
This may suggest that the crystallization temperatures for growth of chromite are in fact
lower than that as proposed from magmatic models of Irvine. Bannister et al. (1998)
notes in her study of chromite in the Paricutin lava flows that when orthopyroxene
crystallizes in equilibrium with chromite, the orthopyroxene dissolves Cr of the chromite
to raise the Cr content of the orthopyroxene.

In the silicate inclusion samples, Cr-bearing pyroxene was observed in a silicate
inclusion. Earlier it was suggested that the fact that there is Cr in the pyroxene,
amphiboles and phlogopites suggests these silicates incorporated the Cr from the preexisting
chromite. Although there was pre-existing chromite, the chromite probably grew
in equilibrium with the silicates as suggested by Bannister et al. (1998), by the Cr content
in the silicates and by the fact that the magmatic fluids were encaptured in a growing
chromite grain. Since Cr is also found in the amphiboles and phlogopites, it is suggested
that the chromite also grew in equilibrium with these late igneous phases and that
chromite probably also grew at lower crystallization temperatures. The lower
crystallization temperatures and the presence of the silicate inclusions in chromite
together suggest that H2O was involved in the crystallization of chromite and associated
igneous phases at least in the area of the silicate inclusions.

A hydrous component to chromite crystallization has been suggested by authors
such as Johan (1986) and Boudreau (1999) in their discussion of hydrous silicate
inclusions. A hydromagmatic model may be suggested for the chromitite deposits as a
whole. The presence of a large amount of chromite with little magma volume may be
explained by H2O that raises the Cr content of the melt to promote chromite
crystallization. This may suggest why there is plagioclase-bearing leucogabbro that
occurs early after a relatively small intrusive sequence of dunite-chromitite-pyroxenite in

263
the Ring of Fire Intrusion. H2O may have lowered the liquidus of orthopyroxene and in
turn plagioclase crystallization according to the model of Bannister et al. (1998).

More evidence for in situ crystallization is observed in the massive chromite. In
massive chromite, the chromites that were probed have more primitive larger grains and
also more differentiated smaller grains. It was noted that there was more diffusion to
lower Mg and Cr in the smaller grains. However, the fact that there is a general
association of lower Mg and Cr with the smaller grains could be evidence that they were
later grown in the intercumulus of the larger grains. In Big Daddy DDH FW-08-19, the
Cr contents of the chromitite horizon appear homogeneous up the interval while there
appears to be more variation in Mg content. The fact that the Mg contents are decoupled
from the Cr contents shows that there was probably double diffusive convection involved
in mineralizing complete chromite layers that were a result of pulses.

However, even though there is considerable primitive pulsing as seen in the Mg
variation with height, there is also evidence of homogenization of these pulses, especially
in the large differentiated section of the hole. There are numerous Mg pulses, but Mg
contents seem to rise from below and move up through these mini-pulses. In other
words, there are not perfect differentiations represented by these pulses. This is probably
evidence of adcumulus growth of chromite after intitial segregation of primary chromite.
Another clue for adcumulus chromite is the chromite layer at the top of the section of
DDH BT-08-10. The last of the chromite has a sharp boundary with the overlying dunite.
Double diffusive convection could explain the formation at the top convecting layer,
however, there would still be some sort of differentiation after that top layer. It is
probably that chromite was formed in the intercumulus and migrated upward until
trapped by an impermeable barrier at the overlying dunite sequence. Also, the adcumulus
textures that fill the voids in the massive chromitites can be explained by further growth
of the magmatic chromites.

In terms of silicate content, in Black Label DDH BT-09-31, there are a number of
sections of oikocrystic harzburgite bearing chromite that is intercumulus to olivine but is
overgrown by orthopyroxene. It was determined that the crystallization sequence was
then olivine . chromite . intercumulus orthopyroxene. In the massive chromitites,
there is often tremolitized intercumulus pyroxene in the matrix of the chromites. The

264
formation of amoeboid intercumulus pyroxene after chromite might be showing that the
chromite continued to form from the reaction of the olivine and chromite with the
surrounding melt. In this case, it would be a Cr and pyroxene-bearing liquid. After
chromite is mineralized from the mixing of the Cr and pyroxene-bearing melt, the melt
goes into pyroxene stability and pyroxene crystallizes. It is noteworthy, that the
chromitite in Black Label Layer 1 reflects the textures of oikocrystic pyroxene in the host
oikocrystic harzburgite. Therefore, primary chromite probably formed with the mixing
of this pyroxene-bearing oikocrystic unit with dunite. Many of the samples reflect
primary chromite after this mixing event. However, possibly where samples show
chromite more into the intercumulus pyroxene farther away from the primary cumulus
olivine, and where chromite has encapsulated inclusions, the chromite probably formed
from this reaction.

In Black Thor DDH BT-08-10, some of the intercumulus pyroxene in the massive
chromitite has been probed to be chromian diopside whereas other times it is
orthopyroxene. Diopside has been observed as an interstitial phase to chromitites in the
Uralian-Alaskan complexes of Asia (Krause et al., 2007). In these chromitites, the
diopsides contain enriched La/Lu contents relative to cumulus diopside in neighbouring
clinopyroxenites. Enriched diopsides have also been observed on the rims of cumulus
diopside in the clinopyroxenites. Krause et al. (2007) concluded that the enriched rim
and interstitial diopsides are fractionated residual melt in the pore space of the solidifying
cumulate and are accessory minerals. The diopside would represent a hydrous fluid
enriched in LREE which developed during the final crystallization of the pore liquid
(Krause et al., 2007). In the McFaulds Lake chromites, hydrous melts that formed along
with chromite crystallization have been documented in the silicate inclusions. Within
these inclusions, there is also the presence of chromian diopside which gives evidence for
it being a late stage igneous phase. Notably, the diopsides are chromian diopsides which
implies the incorporation of Cr post-magmatic the primary chromite.

6.7 Evaluation of the conduit model
The McFaulds Lake chromites are high in grade with 50 wt% Cr2O3 in many of
the layers with very thick intercepts. Also there has been evidence documented of
magmatic breccias and deformations with sulphide mineralization, as at Black Label,

265
which alludes to some dynamic emplacement of the layers. There also needs to be a
significant amount of magma to cause the precipitation of so much chromite. Conditions
for the amount of Cr required in the magma to mineralize the amount of Cr have been
discussed by Naldrett (2009) and are shown in Fig. 6.11.

Fig. 6.11 Figure showing thickness, grade and wt% Cr in the 36 m-thick ore zone at Big
Daddy, the tonnes of chromium this would amount to over each square m of the sill, and
the value of magma required to produce this chromium, assuming that the magma
contained 0.2 wt% Cr (a reasonable estimate for the magma likely to have produced the
sill). – Naldrett (2009a)

The argument is that if there is so much chromite – a 36 m zone in Big Daddy –
then there needs to have been a lot of magma to have produced so much chromite by
gravitational processes. However, there does not have to be so much magma if there was
a central pooling of the magmas in a conduit before being injected into layers. And the
layers would still be settled out as differentiation cycles similar to that observed in the
deposits. A key to debating such a case for the McFaulds deposits is to document the
olivine and pyroxene silicate mineral chemistries upward in the layers along with the
chromite. If olivine and pyroxene differentiate along with the chromite, then they
probably mineralized by gravitational processes. If chromite was mineralized in the
conduit, it would not settle out in association with the magma chemistry of the
surrounding silicates which would have been gravitationally settled. In the McFaulds

266
intrusion, most of the olivine and pyroxene has been replaced by serpentine-tremolitechlorite,
so an in-depth study on silicate is not possible. A few olivines in samples from
Layers 1 and 2 have been probed to have compositions relative to the primary chromite
chemistries in those layers: Layer 1 having Fo #s of 80 to 85 in contrast to the more
primitive chromite-bearing Layer 2 which has Fo #s of up to 94. Hence, this is evidence
for the association of more primitive olivine with more primitive chromite layers. Also
there is evidence of magmatic variation of pargasitic amphibole and phlogopite in the two
layers of DDH BT-09-31.

In spite of no detailed study on primary silicates of McFaulds Lake, the olivine
and pyroxene chemistries have been studied in another massive chromitite deposit,
namely the 8 m-thick Ipueiro-Medrado chromitites in Brazil. These chromites have
chemistries that relate to the silicate chemistries and have been proposed to mineralize by
gravitational processes (Marques, 2003). Therefore, for other massive chromitites, it
appears there is direct correlation of silicate-oxide that suggests gravitational segregation.

However, another important point about McFaulds Lake is that the chromite is
komatiitic. Massive chromite from a different komatiitic chromite occurrence in Nunavut
has been microprobed to compare with the McFaulds Lake deposits. It has compositions
of 52 to 55 wt. % Cr2O3, 26 to 27 wt. % FeOT, 11 to 12 wt % Al2O3 and 6 wt. % MgO.
Diffusion of the chromitite is even similar with depletion of Cr2O3 and FeOT to 48 and

25.75 wt. % respectively and enrichment in Al2O3 and MgO to 16 and 7 wt. %
respectively. These compositions are very similar to the higher temperature
hydrothermally retrogressed upper chromitite of DDH BT-09-17. Low-Mg komatiites can
have up to 0.4 % or 3500 to 4000 ppm Cr in the magma, more than the basalts in the
above diagram at 0.2 % (Baird et al., 1996).
The dunite and pyroxenite lithologies hosting the Cr deposits have been
demonstrated to be aluminum-undepleted komatiite. More work needs to be done to
investigate the primary magma chemistry of the intrusion. However, the chemistries of
the cumulates show that the system is not basaltic as Naldrett (2009) proposed but
contains more primitive magmas with higher partial melting conditions and therefore
contain higher Cr to generate more chromium reserves. Other similar komatiitic-hosted
thick chromitite deposits of the world include Ipueiro-Medrado, Kemi, Selukwe and

267
Nkomati SA (Mungall, 2010). Notably, these deposits are mineralized by many
injections, one on top of the next, so there could have been many scenarios of mixing of
new pulses with old ones to dither the magma in chromite stability.

Therefore, it is assumed that major amounts of chromite can be generated by a
komatiite magma if there is this constant dithering. Although, to generate so much
magma interaction, there should be conduit sites for feeders to the zones. As a general
picture, the intrusion becomes more evolved from NW to SE from Black Label to Black
Thor, while laterally the chromite mineralization branches off in doublets in the
pyroxenites as it tends to do in more evolved lithologies moving NW from Big Daddy to
Black Label and from Black Thor BT-09-10 to Black Thor BT-09-17. In the Black Thor
zone specifically, there are 3 separate zones that differ laterally along strike: the SW
zone, the Central Zone, and the NE zone with Upper-Upper Zone (Fig. 6.12). Areas
where these zones intersect are domains of discontinuity. In the discontinuity between
the SW and Central Zone, there appears to be NW-SE oriented displacements. These are
probably faults. However, along with the fault displacement, the chromitite zones vary
differently along both sides of the fault. Toward the SW, the chromitites become more
massive while toward the NE, the zones branch off in doublets. Since the zones occur
along the same orientation along strike on both sides of the faults, it is possible that these
are feeder conduit sites for the magmas that injected into the chambers to mineralize the
chromite. Notably, the intrusion has been overturned so care needs to be taken in this
interpretation. However, given the preservation of the primary intermittent bedding and
layering of the zones, it is possible that this is accurate. Discontinuities have been shown
to be possible feeder sites in other complexes such as that of the discordant IRUP (ironrich
ultramafic pegmatite) localities in the Bushveld Complex (Reid et al., 2012).

6.8 Retrogression of chromite with hydration of the intrusion
The McFaulds Lake chromites have textures resulting from pervasive hydration,
causing complete serpentinization and uralitization of host dunite and pyroxenite
respectively. Along with hydration of silicates, there was reconstitution of the primary
chromite ores to form either Cr-enriched or Cr-depleted ferrichromite and associated
chromian chlorite. The host silicate to the chromite deposits have very few primary
silicates preserved. There are a few primary olivines and orthopyroxenes preserved with

0 250 1,000
Metres
500
NE Zone, Upper-Upper
Central Zone
SE Zone
Figure 6.12. Residual gravity map with chromitite zones plotted and labeled. Possible
feeder conduit sites are indicated by arrows in areas of discontinuity. From
Tuchscherer (2010).
268

269
compositions suggestive of cumulus segregation of a magnesian magma. Olivines have
been replaced with serpentine as evidenced by the pseudomorphing of serpentine on
original cumulus olivine grains. Pyroxenes have been replaced by tremolite and talc as
evidenced by tremolitization along the cleavage planes of orthopyroxene. Chemical
compositions of serpentine are lizardite to antigorite and amphiboles after pyroxene are
pristine magnesian tremolites. Another retrogressive mineral includes chlorite that
occurs in association with chromite. The textures of serpentine after olivine suggest
temperatures of formation of around 300-350 °C of H2O hydration of the silicates
(Winter, 2001).

Unlike the almost total replacement of the host silicates, the chromites are
preserved with original cumulus associations of chromite in disseminated to massive
chromite layers throughout the drill holes. Although, the ores have been modified and
reconstituted first by diffusion with retrogressive fluids with further replacement to either
Cr-enriched ferrichromite with chromian chlorite or Cr-depleted ferrichromite. Diffusion
has the effect of depleting the primary chromites of Cr2O3 and MgO while enriching the
grains in Al2O3 and FeO. Backscatter images of lighter areas on the margins of the grains
and along cracks in the grains give evidence of variation in the chromite compositions
with retrogression. The retrogression would be a result of fluids as the diffusion occurs
from core to rim and along cracks where there is fluid access.

Three types of ferrichromite serve to either enrich or deplete the original
chromites in Cr2O3. In the bulk of the samples analysed, there is either enrichment or
depletion in ores with hydration. Evidence of the association of ferrichromite with the
hydration that produced serpentine is not seen in massive chromitite due to absence of
silicate. However, the massive chromitites occur in the same section as the serpentinized
disseminated chromite-bearing dunites so are inferred to undergo the same overprint. Cr-
enriched ferrichromites serve to enrich the ores to compositions of up to 65 wt. % Cr2O3.
Chlorite laths accompany ferrichromite developed interior to the primary chromite grains.
The occurrence of chlorites within the primary chromite suggests breakdown and
replacement of the chromite. Specifically, there must have been Si mobility in order to
produce the chlorite.

270
Similar ferrichromite and chlorite relations in chromitites has been documented in
other studies. Beeson and Jackson (1969) and Onyeagocha (1964) suggest the reaction:
chromite + olivine + pyroxene + H2O = ferrichromite + chlorite + magnetite + serpentine.
In the McFaulds Lake chromites, this reaction is indicated by the simultaneous
serpentinization and tremolitization with ferrichromitization and chloritization of the
chromites. Cr-enriched ferrichromite and chlorite are not found in association with
serpentine but rather in association with interstitial chlorite or tremolite. So there was no
reaction to produce both the chlorite and ferrichromite with serpentine. Bliss and
MacLean (1975) suggest there was first serpentinization. A later reaction of chromite
with serpentine produces the ferrichromite and chlorite at higher grades of alteration.
There is no evidence in the immediate vicinity of these ferrichromites to suggest higher
degrees of alteration except for the tremolitization in DDH BT-09-17. Since there are
pervasively serpentinized dunites within the same section as the massive chromites,
higher degrees of hydration probably play no role.

However, in the chromites analysed, there are no associations of the ferrichromite
and chlorite with serpentine and also no relations of the minerals with olivine and
pyroxene. This is since the altered chromites occur within massive chromitites with no
surrounding silicate rock (except for the chlorite interstitial the chromite). The chlorites
are pristine Mg clinochlores with high MgO to 35 wt. %, but with low FeOT at 1 to 2 wt.
%. For mass balancing, it is inferred that the Mg and Al diffuse from the chromite into
chlorite, while the Fe and Cr diffuse into the ferrichromite. There is lowering of the Cr
and Mg from core to margin of the chromite grains with diffusion of these atoms into
chlorite. Al and Fe however go up with substitution with Cr and Mg respectively. There
must also be some SiO2 in the metasomatizing fluids to cause the enrichment of SiO2 in
the chlorites. The SiO2 is probably transported with the ingress of hot water.

After retrogression of the chromites to Cr-enriched ferrichromite, there was
oxidation of the grains to Cr-depleted ferrichromite. Cr is degraded along with Mg and
Al, while Fe increases with an especially large enrichment in ferric iron to 13 wt. %
Fe2O3. This trend is seen in the last chromite evolution of samples 486044 and 486126 in
Black Thor. It cannot be said that the Cr-depleted ferrichromite in these samples formed
the same way as the bulk of Cr-depleted ferrichromites found in the drill hole intervals.

271
However, the association of Cr-depleted ferrichromites with more retrogressed
disseminated chromites, the tendency to form chromian magnetite with further
retrogression, and the fact that these grains have relics of previous chlorite suggests that
these grains are similar to most of the other Cr-depleted ferrichromites. The only
difference is that most of the other Cr-depleted ferrichromites have been depleted to
within the 30 percentile range of Cr2O3. Chromian magnetites are known to form as
further retrogression from ferrichromite in other deposits of the world (Ashley, 1975 and
Kapsiotis et al., 2007). The Cr-depleted ferrichromites are not exactly chromian
magnetites but show the same tendency toward enrichment in ferric iron and depletion in
Cr. Some magnetites have been found in the chromites of this study as well as magnetite
veins cross-cutting chromite are a result of retrogression along with the magnetite with
serpentine.

The chromitites of DDH BT-09-17 are the third type of ferrichromite observed in
the McFaulds Lake chromites analysed. These upper chromitites have ferrichromites of high Cr-enrichment while depletion in FeO to 68 wt. % Cr2O3 and 20 wt. % FeO. The high Cr-enrichment along with lowering of FeO served to enrich not only the Cr content of the ores, but the Cr/Fe ratio as well. In most ferrichromites, there is a trend toward Fe-enrichment along with Cr-enrichment with hydration. The McFaulds Lake chromites have in general undergone this retrogression to enrich the Fe in these secondary chromites. However, there is a lowering of Fe in the case of DDH BT-09-17.

The lowering of FeO with ferrichromite is not well documented in the literature.
One suggestion by Hamlyn and Keays (1979) regarding the Panton Sill in Australia is
that the lowering of FeO in those chromites occurred with postcumulus reequilibration of
the chromite. Although, it is not understood why there would be reequilibration of
chromite to reduce the FeO here while enrich the FeO in chromites in the other drill hole
intercepts, since they have the same mineral assemblages. An earlier paper by Hamlyn
(1975) mentions that the Panton Sill chromites with this trend are the case of higher
temperature chromite. Metamorphosed more aluminous spinels have undergone higher
grades of amphibolite metamorphism to cause precipitation of Fe-depleted ferrichromite
with hornblende. The higher T metamorphism would occur as a result of metasomatism
under conditions of lower oxygen activity which would result in a reduction of FeO in the

272
ferrichromite. In DDH BT-09-17, there is evidence that the chromitites underwent higher
T metamorphism in the thermal aureole of a neighbouring cross-cutting gabbro that itself
underwent autohydration. The heat from the gabbro would reequilibrate the chromite to
higher metamorphic conditions toward that seen in the Panton Sill, though not
crystallizing hornblende. Hydrothermal tremolite and epidote-zoisite and sphene
mineralogy of the gabbro constrain metamorphism in the upper greenschist field to above
500 °C (Apted and Liou, 1983).

In association with the Cr-enriched ferrichromite, there is pristine MgO-rich
tremolite that is interpreted to be prograde. The tremolite shows textures of zoning in the
grains from a core Cr2O3-enriched core to a Cr2O3-depleted margin. This shows that the
tremolite is not just a replacement of clinopyroxene, but that there was an earlier Cr-
enriching event. Chromian-enriched tremolites are seen elsewhere in the McFaulds Lake
chromites as chromian tremolites after chromian pyroxene. However, the crystal zoning
present and MgO-rich chemistries suggests these tremolites are hydrothermal. It may be
that there are other hydrothermal tremolites elsewhere in drill core. However, the
presence of this phase along with the ferrichromite and higher T epidotes and sphenes in
the gabbro suggests the condition of higher T hydrothermalism of both gabbro and
altered chromite.

In general, it is shown that the Ring of Fire Intrusion underwent complete
hydration to eradicate primary chemistries of olivine and pyroxene. This autohydration
occurred as a result of subsolidus cooling of this synvolcanic komatiitic sill.
Autohydration had the effect of convecting water from the seawater interface down and
from the bottom of the intrusion upward through stratigraphy. The intrusion cooled from
the base of the intrusion upwards from magmatic temperatures of 1300°C at olivine and
chromite crystallization to to temperatures of 950°C in the roof gabbro. Encapsulation of
residual melt crystallized with the sintering of chromites at lower temperatures of 700°C.
Finally, the intrusion hydrated with the circulation of water rich in SiO2 and CO2, as low
as 350°C with modification to serpentine. The fluids cooled the intrusion from the
bottom dunites upward to the latest leucogabbros. The leucogabbros were the last to cool
and retained their heat to 500°C while the lower cumulates were cooled to 350°C.
Therefore, conditions of prograde modification of the upper chromitites in DDH BT-09

273
17 were retained and preserved the higher T assemblages of tremolite, epidote, titanite,
high Cr/Fe ferrichromite that are present in both gabbro and chromitite.

This autohydration supports that the Ring of Fire Intrusion is a subvolcanic sill.
The intrusion is overlain by mafic volcanics and later intermediate volcanic that have
been age dated to be coeval with the upper ferrogabbro. Other clues to synvolcanic
volcanism are the komatiitic chemistry of the intrusion, the lack of thick stratigraphy that
would be more suggestive of large layered intrusions, and the occurrence of thin chert
horizons in the pyroxenites of some holes drilled in the Black Horse stratigraphy. These
cherty silicalites represent the silicification barriers to the convecting fluids that one
might see in a hydrothermal VMS system. They are found in pyroxenites which are in
turn overlain by silicified volcanics of this subvolcanic to volcanic system.

274
CHAPTER 7
CONCLUSIONS

7.1 Conclusions
A number of conclusions can been drawn from the study of the McFaulds Lake
chromite deposits. One is that the electron microprobe analyses on the chromite minerals
give evidence of magmatic variation. Magmatic chemistries of the chromite minerals are
displayed by linear enrichment of wt. % Cr2O3 vs. MgO from disseminated to massive
chromite. Linear variations are also evident in the negative linear correlation of FeO vs.
MgO. The variability of Cr2O3 and MgO with down hole depth give evidence that
chromite mineralized by means of repeating successive primitive pulses or
replenishments followed by differentiations with height of the intrusion. Evidence of
replenishments are the occurrence of periodic Cr2O3 and MgO peaks or increases that are
followed by decreases of Cr2O3 and MgO with differentiation before there is another
replenishment. These pulses occur at the cm to metre scale in the chromitites.

The Black Thor and Big Daddy chromites are higher grade and distinguished
from the Black Label chromites. The compositions of the Black Thor and Big Daddy
chromites range from 49 to 53 wt. % Cr2O3 while the Black Label chromites range from
46 to 50 wt. % Cr2O3. The Black Thor and Big Daddy chromites also have higher Cr/Fe
at 1.53 to 2.90 in contrast to the lower Cr/Fe of Black Label at 0.98 to 2.42. In the Black
Label chromites, there are textures of pyroxene oikocrysts and olivine aggregates with
wavy layering suggestive of dynamic deposition with magma mixing with oikocrystic
pyroxene-bearing ultramafics. With greater modal % silicate, there are lower Cr2O3 and
MgO contents which makes the ore lower grade than the Black Thor and Big Daddy
chromites. The Black Label chromites are also distinguished from the Black Thor and
Big Daddy chromites in the laser ablation analyses. There are higher negative Ni

275
anomalies and higher positive Ti and Fe anomalies suggestive of more fractionated
chromites.

The massive chromitite of Big Daddy DDH FW-08-19 shows more subtle change
in Cr2O3 vs. depth in contrast to the more varying Cr2O3 compositions from the massive
to the disseminated chromites in Black Label DDH BT-09-31 and Black Thor BT-08-10.
Even though, there is subtle change in wt. % Cr2O3 in the massive chromite, pulses are
still evident in the variation of wt. % MgO with depth. The high Cr2O3 and MgO
compositions of the chromites and less variation from core to rim rule out the possibility
that these chromites have been reequilibrated to mask primary compositions. Also there
is the same variation in core chromite compositions in the massive Big Daddy chromites
as the massive chromites of the Black Label and Black Thor intercepts. Therefore, the
similar Cr2O3 compositions of the Big Daddy chromites are probably a result of real
igneous processes. A theory for subtle decrease of wt. % Cr2O3 upward is that these
chromites are a result of a cascading effect of double diffusive convection cells upward.
Repeating convection cells cause chromite deposition in upward succession whereby the
more progressively filled cells have more primitive Cr2O3 compositions. Upward in
stratigraphy, the double diffusive convection effect wanes and differentiation is evident
by the slightly decreasing Cr2O3 compositions before the next pulse takes place.

The chromites mineralized as both primitive settled chromites and later in situ
chromites. In some of the replenishments of the Big Daddy chromites, there are
distinctly higher MgO compositions than the MgO compositions in the chromites higher
in a pulse. The distinction of high, early MgO compositions from lower, later MgO
compositions support evidence of there being two generations of chromite: an early
primitive settled chromite and a later in situ crystallized chromite. The occurrence of
distinct high MgO compositions vs. lower MgO compositions at the same depth in some
instances indicates that the variability of core compositions is due to some chromites
being early settled chromites while others follow with later in situ crystallization of the
interstitial melt. There is variation from lower to higher core wt. % Cr2O3 and MgO
compositions in all the chromite intercepts which indicates that this succession in
chromite mineralization in characteristic of all types of chromite. For textural evidence,
massive chromites often contain very primitive cores of large grains that are the early

276
settled chromites along with later smaller chromite cores that are later in situ chromites
with lower Cr2O3 and MgO chemistries. Textures of chain and net-textured chromites in
semi-massive chromites support the crystallization of chromites interstitial to cumulus
olivines.

Round silicate inclusions in some chromites vs. no inclusions in others supports
the interpretation that there was an early deposition of primary settled chromite followed
by in situ chromite that encaptured late igneous melt exsolved from a compressed
cumulus igneous pile. The silicate inclusions have igneous amphibole and phlogopite
with high Ti compositions that identify original igneous minerals. The prevalence of
these inclusions in chain and net-textured semi-massive chromites suggests these
chromites are later in-situ chromites that encaptured residual liquid. The idea that the
primary core chromites do not have these inclusions and that the inclusion are late
igneous phases of the intrusion rules out the possibility that they are remnants of exotic
contaminants that were involved in chromite crystallization.

The chromites reached stability by magma mixing between the olivine and
pyroxene fields, rather than by means of salic contamination. This is suggested by the
fact that silicate inclusions are related to magmatic fluids introduced with compression of
the igneous pile, the fact that the chromites occur between dunite and pyroxenite
lithologies in any order, the fact that disseminated cumulus chromite sometimes occurs in
pyroxenite before a massive chromite interval (e.g. DDH BT-09-17), the lack of evidence
of assimilated xenoliths, the occurrence of both pyroxene and olivine inclusions in
juxtaposed chromites and the distinction of trace element and full spectrum PGE
signatures of dunite vs. pyroxenite.

There is variation of decreasing wt. % Cr2O3 and MgO in the chromites from core
to margin of chromite grains that is evidence of zoning in the chromites. Since the
location of this zoning is prevalent on outer margins, along crack of grains, in smaller
grains and surrounding silicate inclusions, the zoning is attributed to retrogression rather
than silicate exchange with primary intercumulus silicate. The decrease in wt. % Cr2O3
and MgO is due to silicate exchange with interstitial and rim retrogressive chlorites. This
diffusion is part of the modification of the chromite with hydration.

277
The primary chromites were later retrogressed to rim ferrichromite and chlorite.
Mg and Cr ions are leached from the chromite while Al is enriched due to reaction
forming ferrichromite and chlorite. The formation of ferrichromite and chlorite occurs
along with the serpentinization of the dunites and tremolitization and chloritization of the
pyroxenites. These reactions occur as the intrusion underwent greenschist subsolidus
hydration at 300-350°C.

In the chromites of DDH BT-08-17, there is different variation with diffusion
from chromite core to rim to lower wt. % Cr2O3, but higher wt. % MgO. The variation of
Cr2O3 and MgO with depth do not show much evidence of magmatic fractionation.
There is evidence of zoned tremolite interstitial the chromite grains in massive chromite
in this interval. Since there is increase in wt. % MgO rather than decrease and there is
zoned tremolite, it is proposed that this upper chromitite underwent higher temperature
retrogression than the chromites in the other intercepts. The chromitite in this intercept is
intercalated with gabbro. Petrography of the gabbro shows tremolite replacement of
pyroxene, epidote-saussurite replacement of plagioclase and sphene mineralogy that
support higher temperature retrogression in the gabbro. The bulk rock chemistry of the
gabbro shows that it contains nil Ni and Cr and is therefore not saturated to warrant
chromite mineralization. The higher T retrogression of the gabbro, the nil Ni and Cr and
the intercalation of massive with no disseminated chromite in gabbro support the
interpretation that the gabbro intrudes the upper chromitite, and that the heat of the
gabbro caused prograde alteration to higher degrees C in both the gabbro and surrounding
chromitite. Therefore, the diffusion to higher wt. % MgO from core to rim in the
chromites is due to higher T retrogression. Along with diffusion to higher wt. % MgO,
there was retrogression to higher wt. % Cr2O3 in the altered ferrichromite rims. It is
proposed that higher T retrogressive fluids caused Cr2O3 enrichment in the ferrichromite
rims to these chromite. These ferrichromites have the highest Cr2O3 compositions and
serve to enrich the chromite ores in the interval.

7.2 Summary
From the study of the McFaulds Lake chromite a sequence of events can be deduced:

1.
Regional WNW-ESE trending faults and NNE-SSW oriented faults related to
rifting are the locus of the magma to the Ring of Fire magma chamber.

278
2.
As the komatiitic Ring of Fire magma intruded the Oxford-Stull Terrane
basement TTG, there was crustal contamination of the magma to produce large
negative Nb-Ta and Zr-Hf anomalies in the geochemical signatures of the
komatiitic magma.
3.
The feeders of the Ring of Fire intrusion intruded in NW-SE oriented faults that
are seen as displacement of the linear chromite zones.
4.
In the McFaulds Lake sequence of the Ring of Fire magma chamber, there was
first the pulsing and settling of primitive dunite. On the roof of the initial magma
chamber, there was pyroxenite. In the Black Label sequence, primitive pulses of
magma represented by the dunite mixed with pyroxene under dynamic conditions
to crystallize oikocrystic harzburgite. In this dynamic environment, there was
magma mixing of pyroxene in the primitive olivine pulse to dither the magma into
the Cr field and crystallize the Black Label Layer 1 chromitite within the
oikocrystic harzburgite. The dynamic features of the oikocrystic harzburgite are
also suggested by magmatic breccias and wavy, pyroxene-rich textures in the
Black Label chromite. The oikocrystic pyroxene has the effect of decreasing the
Cr/Fe ratio of the chromite ore.
5.
With differentiation of pyroxenite and additional mixing to produce oikocrystic
harzburgite, there was the introduction of a primitive Mg pulse of magma to
migrate the magma into Cr stability again in the Black Label Layer 2 chromitite.
This chromitite is more primitive and reflects the chemistry of this dunite pulse.
Dunite is being differentiated in this chamber at this time. It is Cr-saturated, and
when there is slight dithering of the magma to a composition closer to pyroxene,
another chromititie horizon will form such as the Black Label Layer 3 chromitite.
6.
There is a large sequence of primitive dunite between the Black Label and Black
Thor sequences. This dunite is probably very primitive and well below Cr
saturation.
7.
As the dunite sequence evolves in composition, the magma approaches Cr
stability and mineralizes disseminated interstitial chromite followed by
intermittent pulses of interstitial chromite in dunite in the DDH BT-08-10. New

279
chromite layers separate out of the magma as the melt migrates into Cr stability
from the more evolved olivine.

8.
Further in BT-08-10 sequence, the melt migrates in the Cr field closer to pyroxene
and the chromite itself grades into pyroxenite. There is a massive layer at the top
of the sequence where there is olivine-only crystallization. Not far above this
sequence, there is only pyroxenite. The evidence of there being a large sequence
of pyroxenite after this chromite interval and that the pyroxenite has higher
degrees of crustal contamination of TTG that affects it differently than the
underlying dunite suggests to some extent that the pyroxenite was a later
differentiate that a primitive olivine magma mixed in to cause chromite saturation.
At first chromite is disseminated with evolved dunite; however, the presence of
cumulus pyroxene evident in the drill core along with the associated development
of a massive layer of chromite suggests dithering occurred from a pyroxene to
chromite magma with the mixing in of olivine.
9.
In other nearby areas of the same intrusion at Big Daddy DDH FW-08-19, there is
massive chromitite hosted in pyroxenite. The intermittent pulses in the Black
Thor-Big Daddy deposits as a whole build up into layers upwards and outwards
within double diffusive convective cycles of magma. These convection cycles
cause separation of chromite into semi-massive net-textured chromitites followed
by massive chromitites. Along with crystallization of semi-massive and massive
chromite, there is the exsolution of magmatic fluids from the cumulus pile that are
captured by the growing chromite grains. Further modification of the chromite
includes adcumulus growth of the in situ chromites unto massive chromite.
10. In the layers higher up in the Black Thor sequence, there is primarily pyroxenite.
Some mini-pulses of dunite cause the magma to migrate into chromite stability
again from pyroxene to mineralize the upper chromitites such as in DDH BT-0917.
11. Later in the upper chromite sequence of BT-09-17, there was the intrusion of
gabbro into the upper chromitite that underwent higher T prograde modification
of the upper chromitite. Within this chromite, ferrichromite is enriched to up to
68 wt. % Cr2O3 and hydrothermal tremolite becomes stable in nearby silicate.

280
12. As the subvolcanic Ring of Fire Intrusion underwent subsolidus cooling, there
was autohydration by fluids that circulated from the seawater interface down
through the stratigraphy of the intrusion. The primary olivines and pyroxenes of
the dunite and pyroxenite retrogress into serpentine, tremolite, talc and chlorite.
In the chromitites themselves, the original magmatic signatures of the chromites
are well preserved with some areas of retrogression where there is zoning in the
grains and replacement rims. In the zoned chromites, Mg and Cr are diffused out
of the chromites causing enrichment in Fe and Al. Further retrogression results in
diffusion of Fe and Cr that causes the crystallization of enriched Cr ferrichromite
rims to the chromite. In this reaction, Mg and Al diffuses and dissolves from the
chromite into the chlorite associated with the ferrichromite.
13. Further retrogression of the chromites causes the formation of Cr-depleted
chromite which is more oxidized and has less Cr. Often, the Cr-depleted
ferrichromite is found in association with more Cr-depleted disseminated
chromites in the Black Label and Black Thor olivine-chromite cumulates. As
hydrous fluids advanced upward in stratigraphy, the gabbros and upper chromitite
were the last to cool and undergo retrogression to produce the MgO-depleted
chromites in the upper part of the upper chromitite.
14. The Ring of Fire Intrusion was finally overturned as a result of late Kenoran
granodiorite diapirism in the Oxford-Stull Terrane. This caused the steep plunges
and overturning of the stratigraphy in the Black Label-Black Thor and Big Daddy
sequences. Deformation fabrics often overprint the chromitites in massive
chromites, together with Cr-enrichment in chromian chlinochlore and
kaemmererite vein alteration.